Stable 1. Particle size, PDI and zeta potential of cubic QUL

|  | DLS (nm) | PDI | Zeta potential (mV) |
| --- | --- | --- | --- |
| mean value | 157.08±1.215 | 0.204±0.012 | -38.12±0.071 |

Each repetition was performed as a separate, independent experiment, n=6.

Stable 2. Accuracy and precision for the analysis of QU

| biological sample | concentration（μg/mL） | Intra-Day（n=6） |  |  | Inter-Day（n=6×3） |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Mean（x±s） | RSD（%） | RE（%） |  | Mean（x±s） | RSD（%） | RE（%） |
| plasma | 0.01 | 0.0090±0.00095 | 10.54 | -10.02 | 0.010±0.0017 |  | 16.43 | 2.01 |
|  | 0.02 | 0.09±0.0025 | 13.24 | -3.81 | 0.020±0.0021 |  | 10.20 | 1.65 |
|  | 2 | 1.95±0.22 | 11.28 | -2.53 | 1.91±0.16 |  | 8.17 | -4.29 |
|  | 4 | 4.15±0.41 | 9.94 | 3.74 | 4.12±0.45 |  | 11.02 | 2.89 |

Each repetition was performed as a separate, independent experiment, n=6.

Stable 3. Extractive recovery of QU in rat plasma

| biological sample | concentration （μg /mL） | Recovery |  |
| --- | --- | --- | --- |
|  |  | （x±s%） | RSD（%） |
| plasma | 0.02 | 99.55±2.71 | 2.72 |
|  | 2 | 94.87±6.59 | 6.94 |
|  | 4 | 96.15±3.00 | 3.12 |

Each repetition was performed as a separate, independent experiment, n=6.

Stable 4. Matrix effects of QU

| biological sample | concentration （μg /mL） | Matrix effects |  |
| --- | --- | --- | --- |
|  |  | （x±s%） | RSD（%） |
| plasma | 0.02 | 93.76±9.45 | 10.07 |
|  | 2 | 95.53±3.11 | 3.26 |
|  | 4 | 94.06±7.22 | 7.68 |

Each repetition was performed as a separate, independent experiment, n=6.

Stable 5. Stability of QU (n=6)

| biological sample | concentration (μg /mL) | Room temperature stability |  | Frozen (−80 °C) for 30 Days |  | Freeze–Thaw Cycles |  | Auto-Sampler Stability |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Mean（x±s） | RE（%） | Mean（x±s） | RE（%） | Mean（x±s） | RE（%） | Mean（x±s） | RE（%） |
| plasma | 0.02 | 0.022±0.0049 | 10.21 | 0.022±0.0039 | 8.57 | 0.019±0.0085 | -6.30 | 0.022±0.00037 | 9.59 |
|  | 2 | 2.01±0.15 | 0.58 | 1.85±0.28 | -7.60 | 1.74±0.22 | -1.38 | 1.87±0.26 | -6.28 |
|  | 4 | 4.29±0.22 | 7.18 | 3.93±0.42 | -1.82 | 3.67±0.26 | -8.35 | 4.36±0.072 | 8.89 |

Each repetition was performed as a separate, independent experiment, n=6.

Stable 6. Mouse mortality and percent reduction in mortality

| Groups | Mortality rate | Decrease in mortality rate | Percentage reduction in mortality |
| --- | --- | --- | --- |
| Nor | / | / | / |
| Mod | 50.00% | / | / |
| QUL-L | 37.5% | 12.5% | 25% |
| QUL-H | 25% | 25% | 50% |
| QU | 37.5% | 12.5% | 25% |
| NiF | 25% | 25% | 50% |
| Dex | 12.5% | 37.5% | 75% |

Each repetition was performed as a separate, independent experiment, n=6.