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Figure S1 Schematic Illustration of DAO Man-PBA-DAO and Man-2PBA-DAO Synthesis. Infrared spectra of


Table S2 Relationship between nanoparticles with different ratios of TPGS and Man-PBA-DAO and particle size
	TPGS : Man-PBA-DAO (w/w)
	Size (nm)
	PDI

	[bookmark: _Hlk200220371]1.0 : 0.02
	[bookmark: OLE_LINK3]79.66 ± 6.580
	0.281 ± 0.044

	1.0 : 0.06
	95.22 ± 4.574
	0.263 ± 0.031

	1.0 : 0.10
	62.34 ± 9.236
	0.332 ± 0.019

	1.0 : 0.14
	114.8 ± 13.77
	0.222 ± 0.039

	1.0 : 0.18
	134.2 ± 8.570
	0.198 ± 0.045


Table S3 Relationship between nanoparticles with different ratios of TPGS and Man-2PBA-DAO and particle size
	TPGS : Man-2PBA-DAO (w/w)
	Size (nm)
	PDI

	1.0 : 0.65
	147.3 ± 3.279
	0.346 ± 0.014

	1.0 : 0.70
	193.6 ± 1.476
	0.441 ± 0.007

	1.0 : 0.75
	119.9 ± 3.318
	0.293 ± 0.003

	1.0 : 0.80
	471.6 ± 21.05
	0.761 ± 0.050

	1.0 : 0.85
	407.4 ± 0.613
	0.733 ± 0.126
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Figure S4. CAC1 and CAC2 of nanoparticles with TPGS/MB-PBA-DAO=1:0.10 (Left) and TPGS/MB-2PBA-DAO=1:0.75 (Right)
[image: ]

Figure S5. Nanoparticle chromatogram (Left) and Cur chromatogram (Right)
[image: ]
Figure S6. Cur standard curve

Chromatographic conditions 
Cloum: YMC-Pack ODS-AQ (250 × 4.6 mm, S-5 μm, 12 nm, YMC, JP)
Mobile phase: aceto nitrile and 4% acetic acid solution ‘50:50, v/v’ 
Flow rate: 1.0 mL/min. 
The injection volume: 10 μL 
Detection wavelength: 450 nm
Tempreture: 35 ℃
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