Supplementary Material

Supplementary Figure 1 Zetasizer dynamic light scattering (DLS) size measurement of KM encapsulated Pea Protein Nanoparticles by Berry Extract crosslinking (KM-PP-BE-NP)

Supplementary Figure 2 Zetasizer dynamic light scattering (DLS) zeta potential (ZP) measurement of KM encapsulated Pea Protein Nanoparticles by Berry Extract crosslinking          (KM-PP-BE-NP).

## Stability study

The stability of KM encapsulated pea protein nanoparticles was monitored over a ~six-month period by measuring the hydrodynamic size and zeta potential of the nanoparticles. 600 mg/L of sodium benzoate and 350 mg/L of potassium sorbate, food grade preservatives were also added to the nano-formulations to extend shelf-life. The nanoparticles were refrigerated (5°C ± 3°C) in glass or plastic containers with a tight seal. Negligible change in size and zeta potential confirmed the stability of nanoparticles for long term storage. In the present study, stability of KM-encapsulated pea protein nanoparticles was assessed over a ~six-month period using both dynamic light scattering (DLS) measurements and gas chromatography–mass spectrometry (GC-MS). This enabled evaluation of temporal consistency in hydrodynamic size, zeta potential, and KM content throughout storage. The DLS size and ZP measurements over a ~six-month period for KM encapsulated Pea Protein Nanoparticles by Berry Extract crosslinking (KM-PP-BE-NP) is shown in Supplementary Table 1.

Supplementary Table 1 Stability study of KM encapsulated Pea Protein Nanoparticles Berry Extract crosslinking (KM-PP-BE-NP) by monitoring size and zeta potential (ZP).

| Serial No. | Time point | DLS Size (nm) | PDI | ZP (mV) |
| --- | --- | --- | --- | --- |
| 1 | 0 | 358 | 0.2 | -12 |
| 2 | 1 week | 301 | 0.2 | -13 |
| 3 | 2 weeks | 306 | 0.2 | -13 |
| 4 | 1 month | 372 | 0.2 | -8 |
| 5 | ~2 months | 314 | 0.2 | -14 |
| 6 | ~3 months | 307 | 0.2 | -13 |
| 7 | 8 months | 334 | 0,2 | -13 |

Gas chromatography–mass spectrometry (GC-MS) procedure: The neat Ketone Molecule (KM) was diluted 1,000 times by adding 1000 µL of pyridine. 200 μL of this solution was derivatized with 200 μL BSTFA [N,O-bis(trimethylsilyl)trifluoroacetamide] + 1% TMCS (chlorotrimethylsilane) reagent by incubating at 50 ℃ for an hour. The derivatized samples were then analyzed using a ThermoTRACE 1300 Gas Chromatograph coupled to a Thermo Trace GC/GCQ mass spectrometer with a scan range from 50 to 500 m/z (Thermo Scientific, Inc., Waltham, MA, USA). 1 μL of sample was injected into the GC column with a 35 min run time. Separation was achieved with a temperature program of 40 ℃ as the starting point, then ramped up to 10 ℃/min to 280 ℃ and held at 280 ℃ for 10 min, on a 30 m TG-5SILMS column (Thermo Scientific, 0.25 mm ID, 0.25 um file thickness) and a constant flow of 1 ml/min of helium gas. Using neat KM a calibration curve was generated to quantify KM in the nanoparticles and monitor changes during the stability study. For nanoparticle GC-MS sample preparation, 100 µL of the KM encapsulated Pea Protein Nanoparticles by Berry Extract crosslinking (KM-PP-BE-NP) was dried under nitrogen gas (to remove solvent) and mixed with 100 µL of pyridine. Then 1 μL of sample was injected into the GC column for KM quantification. There was negligible change in the amount of KM measured (~250 mg/ml) at the end of the study in comparison to the beginning, confirming the stability of nanoparticles for long term storage.

Supplementary Figure 3 1H NMR of Ketone Molecule (KM) in D2O.

Supplementary Figure 4 1H NMR of water soluble Pea Protein (PP) in D2O.

Supplementary Figure 5 1H NMR of mangiferin in CD3OD.

Supplementary Figure 6 1H NMR (expanded) of mangiferin and water soluble Pea Protein (PP) reaction mixture in CD3OD/D2O (arrows indicate change in the mangiferin protons).

Supplementary Figure 7 1H NMR (expanded) of mangiferin, water soluble Pea Protein (PP) and KM reaction mixture in CD3OD/D2O.

Supplementary Figure 8 1H NMR of epigallocatechin gallate (EGCG) in D2O.

Supplementary Figure 9 1H NMR (expanded) of epigallocatechin gallate (EGCG) and water soluble Pea Protein (PP) reaction mixture in D2O (arrow indicate change in EGCG proton).

Supplementary Figure 10 1H NMR (expanded) of epigallocatechin gallate (EGCG), water soluble Pea Protein (PP) and KM reaction mixture in D2O.

Supplementary Figure 11 1H NMR of quercetin in CD3OD.

Supplementary Figure 12 1H NMR (expanded) of quercetin and water soluble Pea Protein (PP) reaction mixture in CD3OD/D2O (arrow indicate change in quercetin proton).

Supplementary Figure 13 1H NMR (expanded) of quercetin, water soluble Pea Protein (PP) and KM reaction mixture in CD3OD/D2O.

## Supplementary Figure 14 Keonte Molecule (KM) hydrogen bonding with protein and phytochemical.