Table 1s. Zn content (wt.%) in synthesized materials determined by EDS method

|  | Nominal Zn content (mol%) | Nominal Zn content (wt.%) | Experimental Zn content (wt.%) | Standard deviation (wt.%) | %RSD |
| --- | --- | --- | --- | --- | --- |
| 0.1ZnHA | 0.1 | 0.65 | 0.59 | 0.13 | 22.03 |
| 0.4ZnHA | 0.4 | 2.58 | 2.51 | 0.22 | 8.76 |
| 1.0ZnHA | 1.0 | 6.35 | 6.77 | 0.71 | 10.49 |
| 1.8ZnHA | 1.8 | 11.20 | 10,12 | 1.25 | 12.35 |

Figure 1s. EDS characterization of the 0.6ZnHA sample showing elemental distribution. Main image represents STEM micrograph (2× enlarged) with elemental maps displaying spatial distribution of calcium (Ca), phosphorus (P), oxygen (O), and zinc (Zn).

Figure 2s. Curve fitting results for the 700-490 cm-1 region of the representative spectrum of the 06ZnHA sample.

Table 2s. Results of the curve fitting for the 700-490 cm-1 region with the assignments of the lines.

| line | wavenumber (cm-1) | % of the total (700-490 cm-1) area |  |  |  |  |  |  |  |  | Assignment[51, 52] |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | HA | 0.1ZnHA | 0.2ZnHA | 0.4ZnHA | 0.6ZnHA | 0.8ZnHA | 1.0ZnHA | 1.4ZnHA | 1.8ZnHA |  |
| 1 | 628 | 17.1 | 13.5 | 14.7 | 15.3 | 14.9 | 13.8 | 12.8 | 10.7 | 10.1 | librational mode of structural OH groups |
| 2 | 615 | - | 4.8 | 4.7 | 7.3 | 8.1 | 6.9 | 7.6 | 9.8 | 11.7 | PO43- labile and poorly crystalline |
| 3 | 603 | 28.6 | 26.3 | 26.8 | 20.1 | 16.9 | 15.9 | 14.4 | 15.8 | 14.6 | regular apatitic PO43- environment |
| 4 | 582 | - | 2.8 | 3.6 | 3.5 | 5.9 | 5.5 | 5.9 | 6.5 | 6.7 | terminal PO43- groups on the crystal surface |
| 5 | 575 | 16.9 | 17.7 | 15.8 | 13.2 | 13.9 | 13.4 | 13.5 | 13.5 | 14.5 | regular apatitic PO43- environment |
| 6 | 565 | 35.2 | 28.8 | 26.6 | 28.4 | 28.0 | 28.1 | 27.2 | 23.9 | 25.8 | regular apatitic PO43- environment |
| 7 | 538 | 2.2 | 6.1 | 7.8 | 12.2 | 12.4 | 16.6 | 18.4 | 19.8 | 16.6 | P-OH groups (non-apatitic) |

Figure 3s. Curve fitting results for the 1250-900 cm-1 region of the representative spectrum of the 06ZnHA sample.

Table 3s. Results of the curve fitting for the 1250-900 cm-1 region with the assignments of the lines.

| line | wavenumber (cm-1) | % of the fitted area |  |  |  |  |  |  |  |  | Assignment [61,51,52] |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | HA | 0.1ZnHA | 0.2ZnHA | 0.4ZnHA | 0.6ZnHA | 0.8ZnHA | 1.0ZnHA | 1.4ZnHA | 1.8ZnHA |  |
| 1 | 1145 | 5.0 | 4.5 | 6.5 | 8.1 | 16.7 | 17.4 | 17.9 | 23.3 | 16.9 | HPO42- |
| 2 | 1110 | 14.6 | 18.6 | 18.7 | 16.7 | 10.4 | 8.9 | 18.1 | 11.1 | 14.5 | poorly crystalline apatite |
| 3 | 1097 | 7.7 | 9.3 | 10.4 | 13.9 | 7.9 | 10.6 | 6.1 | 13.1 | 14.9 | PO43- labile and poorly crystalline |
| 4 | 1060 | 18.9 | 19.1 | 20.5 | 22.5 | 22.0 | 18.9 | 13.2 | 11.4 | 10.5 | poorly crystalline apatite PO43- environment |
| 5 | 1030 | 32.4 | 26.5 | 25.1 | 23.9 | 20.2 | 20.2 | 23.6 | 18.9 | 19.2 | regular apatitic PO43- environment |
| 6 | 1002 | 16.6 | 17.3 | 13.2 | 10.7 | 19.0 | 18.3 | 12.8 | 14.7 | 16.5 | regular apatitic PO43- environment |
| 7 | 961 | 4.8 | 4.7 | 5.6 | 3.9 | 3.8 | 5.7 | 8.3 | 7.5 | 7.5 | υ1 PO43- |

Table 4s. Peak fitting results and assignments for the 1H BD ssNMR spectra     [51,57,58].

| line | ppm | assignments |
| --- | --- | --- |
| 1 | 7.06 | P-OH groups |
| 2 | 5.41 | surface adsorber water |
| 3 | 0.52 | disordered OH groups in c-channels |
| 4 | 0.01 | well-ordered structural OH groups |

Figure 4s. Curve fitting results for the 1H BD ssNMR spectrum of the 06ZnHA sample.

Figure 5s. Curve fitting results for the 31P BD (left) and 31P CP (right) ssNMR spectra of the 06ZnHA sample.

Table 5s. Results of the curve fitting for 31P (BD and CP) NMR experiments.

| line | ppm | % of the signal area |  |  |  |  |  |  |  |  | Assignment [55,56] |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | HA | 0.1ZnHA | 0.2ZnHA | 0.4ZnHA | 0.6ZnHA | 0.8ZnHA | 1.0ZnHA | 1.4ZnHA | 1.8ZnHA |  |
| BD |  |  |  |  |  |  |  |  |  |  |  |
| narrow component | 3.1 | 94.8 | 85.3 | 66.7 | 55.4 | 53.2 | 47.5 | 44.3 | 19.3 | 4.9 | 31P nuclei from crystalline core |
| broad component | 3.8 | 5.2 | 14.7 | 33.3 | 44.6 | 46.8 | 52.5 | 55.7 | 80.7 | 95.1 | 31P nuclei from hydrated Surface layer |
| CP |  |  |  |  |  |  |  |  |  |  |  |
| narrow component | 3.1 | 57.2 | 55.9 | 49.4 | 42.3 | 18.9 | 18.7 | 29.1 | 4.5 | 0.9 | 31P nuclei from crystalline core |
| broad component | 3.9 | 42.8 | 44.1 | 50.6 | 57.7 | 81.1 | 81.3 | 70.9 | 95.5 | 99.1 | 31P nuclei from hydrated Surface layer |