Supplementary Table 1. Quantitative ICP-MS results of CMP.
	Sample No.
	Cu Content (wt%)
	Mo Content (wt%)

	1
	16.67
	20.03

	2
	17.61
	21.23

	3
	16.08
	19.39

	4
	16.21
	19.81

	5
	15.89
	19.28

	6
	16.27
	19.91

	Average
	16.46%
	19.94%


Notes: The metal element content in the material CMP was measured using inductively coupled plasma mass spectrometry (ICP-MS). The material contains approximately 16.46% Cu and 19.94% Mo per 100g.
