Supplementary Table 1. Quantitative ICP-MS results of CMP.

| Sample No. | Cu Content (wt%) | Mo Content (wt%) |
| --- | --- | --- |
| 1 | 16.67 | 20.03 |
| 2 | 17.61 | 21.23 |
| 3 | 16.08 | 19.39 |
| 4 | 16.21 | 19.81 |
| 5 | 15.89 | 19.28 |
| 6 | 16.27 | 19.91 |
| Average | 16.46% | 19.94% |

Notes: The metal element content in the material CMP was measured using inductively coupled plasma mass spectrometry (ICP-MS). The material contains approximately 16.46% Cu and 19.94% Mo per 100g.