Supplementary Table 1. Optimization results of the HBC–2% carteolol formulation ratios

| Parameter | 10:1 | 10:2 | 10:3 | 10:4 | 10:5 | 10:6 | 10:7 | 10:8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HBC:2% carteolol ratio (v/v) | 10:1 | 10:2 | 10:3 | 10:4 | 10:5 | 10:6 | 10:7 | 10:8 |
| Gelation temperature (°C) | 18 | 19 | 19 | 22 | 23 | 26 | No gelation | No gelation |
| Appearance and homogeneity | Homogeneous; no visible precipitation | Homogeneous; no visible precipitation | Homogeneous; no visible precipitation | Homogeneous; no visible precipitation | Homogeneous; no visible precipitation | Homogeneous; no visible precipitation | Homogeneous; no visible precipitation | Homogeneous; no visible precipitation |
| Low-temperature appearance | Transparent at low temperature | Transparent at low temperature | Transparent at low temperature | Transparent at low temperature | Transparent at low temperature | Transparent at low temperature | Transparent at low temperature | Transparent at low temperature |
| Appearance after gelation or at 37°C | Slightly yellow and opaque after gelation | Slightly yellow and opaque after gelation | Slightly yellow and opaque after gelation | Slightly yellow and opaque after gelation | Slightly yellow and opaque after gelation | Slightly yellow and opaque after gelation | Slightly yellow and opaque at 37°C but without gelation | Slightly yellow and opaque at 37°C but without gelation |
| Gelation at 37°C | Yes | Yes | Yes | Yes | Yes | Yes | No | No |
| Clinical suitability | Not selected; low carteolol loading | Not selected; low carteolol loading | Not selected; low carteolol loading | Acceptable but lower carteolol loading | Acceptable but lower carteolol loading | Selected final clinical formulation | Not selected; impaired gelation | Not selected; impaired gelation |

Note: HBC, hydroxybutyl chitosan. A 1 mL aliquot of thermosensitive HBC dressing was mixed with different volumes of 2% carteolol ophthalmic solution. Gelation temperature was determined using the test-tube inversion method after equilibration at 4°C and stepwise heating from 10°C. The 10:6 ratio was selected because it represented the highest carteolol-containing ratio that maintained homogeneous mixing, absence of visible precipitation, and stable gelation at 37°C. Ratios of 10:7 and 10:8 were not selected because they failed to gel at 37°C.