1. CHEMICAL CHARACTERIZATION OF FULLERENE NANOMATERIAL

1.1 MOLECULAR DOCKING AND MD SIMULATIONS

1.2 NMR SPECTRA

1.3 FT-IR SPECTRA

1.4 MASS SPECTROMETRY

1.5. DLS MEASUREMENTS

1.6 XPS SPECTROSCOPY

2. BIOLOGICAL STUDIES

Figure S1 The possible binding site of HDGF in BTK, identified by docking.

1H-NMR(d1-CDCl3, ppm, 500 MHz): 3.96(d, J= 5.2 Hz, 4H, -CH2); 3.29(s, 2H, O=C-CH2-C=O); 1.49(s, 9H, t-Bu).

13C-NMR(d1-CDCl3, ppm, 125 MHz): 168.59; 167.11; 82.46; 42.25; 42.15; 28.03

Figure S2

1H-NMR spectrum of malonate 1.

Figure S3

13C-NMR spectrum of malonate (1).

1H-NMR(d1-CDCl3, ppm, 500 MHz): 3.98(d, J= 5.2 Hz, 4H); 1.49(s, 9H, t-Bu).

13C-NMR(d1-CDCl3, ppm, 125 MHz):169.60(COOR); 168.64(COOR); 164.94(NH-C=O); 145.83(C60-sp2); 145.73(C60-sp2); 145.32(C60-sp2); 145.17(C60-sp2); 144.71(C60-sp2); 144.52(C60-sp2); 143.81(C60-sp2); 142.98(C60-sp2); 142.21(C60-sp2); 142.20(C60-sp2); 142.13(C60-sp2); 142.11(C60-sp2); 140.98(C60-sp2); 140.95(C60-sp2); 139.29(C60-sp2); 82.43(C(CH3)3); 71.51(C60-sp3); 42.15; 42.05; 29.66; 28.12 (C(CH3)3.

Figure S4

1H-NMR spectrum of  [60]fullerene monoadduct 2

Figure S5

13C-NMR spectrum of  [60]fullerene monoadduct 2

13C-NMR(d2-D2O, ppm, 125 MHz): 174.5; 169.76; 145.23; 141.56; 71.63; 40.66

Figure S6

HRMS spectrum of malonate (1).

Figure S7

HRMS spectrum of fullerene monoadduct (2).

Figure S8

Spectrum of fullerene hexakisadduct (3)

Figure S9

A high-resolution XPS spectrum of O1s line of HDGF

Figure S10

DLS measurement of the fullerene nanomaterial HDGF at pH=3 (c=0.1 mg/mL)

Figure S11

DLS measurement of the fullerene nanomaterial HDGF at pH=6 (c=0.1 mg/mL)

Figure S12

DLS measurement of the fullerene nanomaterial HDGF at pH=9 (c=0.1 mg/mL)

Figure S13

DLS measurement of the fullerene nanomaterial HDGF in cellular medium containing FBS (c=0.1 mg/mL, day 0)

Figure S14

DLS measurement of the fullerene nanomaterial HDGF in cellular medium containing FBS (c=0.1 mg/mL, day 3)

| Element | Atomic concentration (at. %) | Assigned bond | Binding energy (eV) | Contribution of individual chemical bonds for the given element (%) | The approximate atomic concentration of individual chemical bond (at. %) |
| --- | --- | --- | --- | --- | --- |
| C | 71.90 | Si–C | 282.6 | 3.91 | 2.8 |
|  |  | C–C, C–H | 284.8 | 85.14 | 61.2 |
|  |  | C–O, C–N, to –C–OH | 286.6 | 6.38 | 4.6 |
|  |  | C=O | 288.0 | 4.56 | 3.3 |
| N | 3.73 | Pyridinic N | 398.4 | 18.47 | 0.2 |
|  |  | C–N, N–(C=O)– | 399.8 | 81.53 | 3.0 |
| O | 20.32 | Atomic oxygen | 529.2 | 2.79 | 0.5 |
|  |  | C=O, O=C–OH | 530.6 | 4.74 | 0.9 |
|  |  | C–O, C–O–C, O–H, Si–O | 532.5 | 92.47 | 18.8 |
| Si | 4.06 | Si–O | ~102.0 | 4.06 | 4.1 |

Table S1

Chemical composition, atomic concentration, and percentage contributions of chemical state for particular element obtained from the XPS measurements.

| Gene | Forward primer (5’→3’) | Reverse primer (3’→5’) |
| --- | --- | --- |
| BTK | ACAGATTCCGAGGAGAGGTGAGG | GGTCCTTCATCATATACAACCTGGAATGG |
| TLR8 | ACCACCTCAGTCCAGGGAAA | CGAACGCAACCACAGCATAA |
| NFAT | GATGCCAAGCACCAGCTTTC | TGTTGTGGTACAGGCCCAAG |
| ARID3A | AGCATTCGGATCAACAGCCA | CCGTATCTTCCGCCATCCTG |
| LC3 | CAGCATCCAACCAAAATCCC | CACTGACAATTTCATCCCGAAC |
| p62 | AGGACGGGGACTTGGTTG | GGCGGGAGATGTGGGTAC |
| HPRT1 | CAGCCCTGGCGTCGTGATTAGT | CCAGCAGGTCAGCAAAGAAT |

Table S2

Sequences of primer pairs used in determining the mRNA expression of tested genes.