Supplementary materials
Figure S1 Cell viabilities of A375 cancer cells treated with as-prepared Re-CDs which prepared under different temperature (A) and reaction time (B). 

Notes: Data was represented as means ± SD from three parallel tests. (n=3, *p< 0.05). Re-CDs achieved varying degrees of inhibition effect on A375 cancer cell lines. Cell viabilities of A375 cancer cells were descreased with the increasing temperature and reaction time.
Abbreviations: Re-CDs, Re-based carbon dots; A375, malignant melanoma cell line. SD, standard deviation.

[image: image1.png]IR 160-6h
100 4 [ 180-6h
[ 200-6h
801 . .
x
g *
E 60 *
3 *
=
D 40
(¢}
20
0 T T T
0.2 0.5 1.0
Concentration (mg/mL)

Cell Viability (%)

I 200-3h
1007 [ 200-6h
[ 200-10h
N
80 1
* *
N
60 . .
"
40 4
"
20
0 T T T
0.2 05 1.0

Concentration (mg/mL)




Figure S2 The DLS spectrum of Re-CDs.

Notes: From this analysis we could observe that the main diameter distribution in solution of Re-CDs was around 110nm. This result proved the hydrodynamic diameter of Re-CDs nanostructure from another side.
Abbreviations: DLS, dynamic light scattering; Re-CDs, Re-based carbon dots. 


[image: image2.wmf]0

50

100

150

200

250

300

0.0

0.2

0.4

0.6

0.8

1.0

1.2

1.4

 

 

Size (nm)

Concentration (particles/mL) 


Figure S3 The FT-IR spectrum of the CDs prepared by CA and EDA.
Abbreviations: FT-IR, Fourier transform infrared spectroscopy; CDs, carbon dots; CA, citric acid; EDA, ethanediamine.


[image: image3.wmf]4000

3500

3000

2500

2000

1500

1000

500

Wavenumber (cm

-1

)

Transmission (a.u.)

 

 


Figure S4 Cell imaging of A375 cells without Re-CDs.

Notes: Image results showed that there was no inherent fluorescence in A375 cells. 
Cell imaging of A375 cells treated with Re-CDs under ultraviolet (A, 360–380nm), blue (B, 460–480 nm), green (C, 510–530 nm) light excitation and bright field (D).

Abbreviations: Re-CDs, Re-based carbon dots; A375, malignant melanoma cell line.

[image: image4.png]



Figure S5 Cell viabilities (A) and released LDH (B) of other normal cells when treated with different concentration of Re-CDs.
Notes: Concentrations of Re-CDs were also selected at 0, 0.2, 0.5, 1.0mg/mL. Data was represented as means ± SD from three parallel tests. (n=3, *p< 0.05).

Abbreviations: CD, carbon dots; Re-CDs, Re-based carbon dots; HL-7702[L-02], normal human liver cells; NsFb, human normal skin flbroblasts; MCF-10A, normal breast epithelial cells; SD, standard deviation; 
[image: image5.png]Cell Viability (%)

I VICF-10A
[CIHL-7702
100 | NSFbs
80 4
60
40
20
0
0 0.2 0.5 1.0
Concentration (mg/mL)

LDH Release (vs. control)

144

124

101

0.8

0.6

0.4-

0.2+

I 2037
[ MCF-10A
[—JHL-7702

[ NSFbs

I

0.2 0.5 1.0
Concentration (mg/mL)




Figure S6 Cell viabilities of normal cells and different kinds of cancer cell lines (HepG2, MCF-7 and A375) when treated with different concentration of CDs only prepared from citric acid and EDA (A) and ginsenoside Re (B).
Notes: (A) The material ratio of citric acid and EDA in CDs synthesis was the same as it in Re-CDs preparation. Concentration gradient of CDs and ginsenoside Re were also selected at 0, 0.2, 0.5, 1.0mg/mL. Data was represented as means ± SD from three parallel tests. (n=3, *p< 0.05).

Abbreviations: CD, carbon dots; Re-CDs, Re-based carbon dots; MCF-7, human breast adenocarcinoma, Michigan cancer foundation-7; HepG2, human liver hepatocellular carcinoma cell line; 293T, human renal epithelial cell line; A375, malignant melanoma cell line. SD, standard deviation.

[image: image6.png]Cell Viability (%)

. 293T I 2937
[ HepG2 B [ HepG2
CIMCF7 CIMCF-7
1004 EA3T5 1001 [ A375
80+ 801
g
60 2 60
z
=
=
404 T 404
20+ 20
0 0
0.2 05 10 0.2 05 10

Concentration (mg/mL)

Concentration (mg/mL)




Figure S7 ROS generation analysis of normal cells 293T treated with different concentration of Re-CDs. 
Notes: (A). 0mg/mL; (B). 0.2mg/mL; (C). 0.5mg/mL; (D) 1.0mg/mL. ROS generation in normal cells 293T was enhanced with the increasing concentration of Re-CDs treatment. 

Abbreviations: ROS, reactive oxygen species; 293T, human renal epithelial cell line; Re-CDs, Re-based carbon dots.

[image: image7.png]i)

[N N B B B S B

15}

s

Toe "

W

LI B B S B e R B

U0y

DCFH-DA




Figure S8 ROS generation analysis of normal cells MCF-7 treated with different concentration of Re-CDs. 
Notes: (A). 0mg/mL; (B). 0.2mg/mL; (C). 0.5mg/mL; (D) 1.0mg/mL. ROS generation in normal cells MCF-7 was enhanced with the increasing concentration of Re-CDs treatment. 

Abbreviations: ROS, reactive oxygen species; MCF-7, human breast cancer cell line; Re-CDs, Re-based carbon dots.

[image: image8.png]3

0¥

10"

0%

0

0

ke

o
wnoy

ol

e

AT RS

noy

1w

0

102

e

N N

winoy

suau0)

DCFH-DA




Figure S9 ROS generation analysis of normal cells HepG-2 treated with different concentration of Re-CDs. 
Notes: (A). 0mg/mL; (B). 0.2mg/mL; (C). 0.5mg/mL; (D) 1.0mg/mL. ROS generation in normal cells HepG-2 was enhanced with the increasing concentration of Re-CDs treatment. 

Abbreviations: ROS, reactive oxygen species; HepG-2, hepatocellular carcinoma cell line; Re-CDs, Re-based carbon dots.

[image: image9.png]W

w

Ll

o

LS A S N

Toner

% !.m
"
< o
TR ETE TR T
Wwnog. wnod

ooy

DCFHDA




Figure S10 High-content imaging analysis of cancer cell apoptosis and necrosis by Annexin V-FITC/PI double staining method. 
Notes: (A) Samples only treated with different concentration of Re-CDs. (B) Samples treated with Re-CDs and NAC simultaneously. There were clear cell apoptosis and necrosis phenomena in group treated with Re-CDs. When co-incubated with NAC, cell apoptosis and necrosis had decreased.

Abbreviations: NAC, N-acetyl-L-cysteine; Re-CDs, Re-based carbon dots; PI, propidium iodide; FITC, fluorescein isothiocyanate.

[image: image10.png]A. Re-CDs
Hoechst Merge

;

B. Re-CDs+NAC

Hoechst





PAGE  
7

_1595925212.bin

_1595750721.bin

