Supporting Information

A protein corona adsorbed to a bacterial magnetosome affects its cellular uptake

Figure S1. Rabbit anti magnetosomes antibody was prepared and purified by Bioss Company.

Figure S2. Magnetosomes purification using ultrasonic cell disruptor.

Figure S3. Protein plasma concentrations as well as iBAQ intensities of corona proteins identified by LC-MS.

Figure S4. Adsorption of the top three abundant corona proteins of magnetosome was verified by Western blot.

Figure S5. Magnetosome corona protein interaction network.

Figure S6. Enhancement of magnetosome cell uptake in HUVEC cells in the presence of protein corona.

Figure S7 LDL receptor expression and magnetosome uptake comparison.

Figure S8. Confocal images of HUVEC and endothelial cells (EC) cells treated with magnetosomes (20 μg/mL Fe concentration) with or without corona for 5 h.

Table S1. Protein amount on the nanoparticles measured by BCA assay.

Table S2. LC-MS identified corona proteins and their iBAQ intensities.

Table S3. Top 20 plasma proteins.

Table S4. α-helix percentage calculation of ApoE and HSA.

Table S5. GO molecular function enrichment of the abundant proteins on magnetosome corona.

Figure S1. Rabbit anti magnetosomes antibody was prepared and purified by Bioss Company. The specificity of antibody was tested by Western blot. Magnetosomes membrane protein, EC and HUVEC cells protein were extracted by 4% SDS 50mM Tris buffer respectively and separated on 12% SDS-PAGE (15 µg per each sample) for Western blot assay. Membrane was incubated with rabbit anti magnetosomes antibody, and after ECL detection the membrane was stained with G250. Magnetosomes antibody can specifically recognize the magnetosomes proteins, and can distinguish proteins extracted from cultured human cells.

Figure S2. Magnetosomes purification using ultrasonic cell disruptor. (A) The supernatant absorbance was measure at 280 nm and 260 nm to represent the rest protein and nucleic acid mount. The values are not change in the last two steps, reveals that except the membrane binding proteins, there are no excess bacterial protein or nucleic acid on the membrane. (B) TEM image of purified magnetosomes negatively stained with 1% uranyl acetate. (C) TEM image of purified magnetosomes. MMs stands for magnetosomes membranes. (D) TEM image of purified magnetosomes without membrane. The membrane was removed by treated with lysis buffer (6 M guanidine hydrochloride, 50 mM Tris and 2% CHAPS) at 100 °C for 10 min.

Figure S3. Protein plasma concentrations as well as iBAQ intensities of corona proteins identified by LC-MS. Identified PEG-Fe3O4 corona proteins (A) and the most 20 abundant corona proteins (B) iBAQ intensities and relative concentrations in plasma.

Figure S4. Adsorption of the top three abundant corona proteins of magnetosome was verified by Western blot. Protein extractions from equal iron ion amount magnetosome and PEG-Fe3O4 with corona were separated by SDS-PAGE and incubated with antibodies. Protein extracted from bare magnetosome was set as control to make sure the antibodies won’t bind magnetosome membrane protein. The result reveals ApoE, VTN and HSA are adsorbed on magnetosome and PEG-Fe3O4 after plasma incubation. The result consistent with the corona protein amount in Table S1, that PEG-Fe3O4 adhered more plasma proteins than magnetosome.

Figure S5. Magnetosome corona protein interaction network. ECM interactors were obtained and filter from BioGRID, IMEx, IntAct, MINT and UniProt databases. Abuandant corona proteins are colored by their relative abundance.

Figure S6. Enhancement of magnetosome cell uptake in HUVEC cells in the presence of protein corona. Prussian blue staining and intracellular iron concentrations of HUVEC cells (control) incubated with magnetosomes (10 μg/mL Fe) with or without corona for 3 h. Scale bars 20 μm.

Figure S7 LDL receptor expression and magnetosome uptake comparison. (A) EC and HUVEC cells protein were separated on 12% SDS-PAGE (15 µg per each sample) for Western blot assay. Membrane was incubated with rabbit anti human LDL receptor antibody (Abcam, UK) and mouse anti GAPDH antibody (SouthernBiotech, AL, USA) and detect using ECL reagent. (B) Intracellular Fe amount comparison of EC and HUVEC cellular uptake of magnetosomes before and after human plasma incubation. (C) Western blot analysis of LDL receptor expression in HUVEC cells. The cells were transfected with LDL receptor siRNA (si LDL receptor) or negative control siRNA (negative control) and harvested after 48 h for Western blot analysis. (D) Intracellular Fe amount comparison of HUVEC cell with LDL receptor gene knockdown. Cells were treated with magnetosomes with or without corona for 5 h.

Figure S8. Confocal images of HUVEC and endothelial cells (EC) cells treated with magnetosomes (20 μg/mL Fe concentration) with or without corona for 5 h. Large colocalization of LDL receptors (green) and magnetosomes (MAG, red) signals were found in the presence of corona. Cell nucleus stained with DAPI. Scale bars 10 μm.

| Table S1. Protein amount on the nanoparticles measured by BCA assay. |  |  |  |
| --- | --- | --- | --- |
|  | Magnetosome | Magnetosome + plasma | PEG-Fe3O4 + plasma |
| Protein/Fe (µg/µg)* | 0.377 ± 0.013 | 0.421 ± 0.020 | 0.064 ± 0.016 |
| * Protein amount is normalized by Fe amount in each sample. |  |  |  |

Table S2. LC-MS identified corona proteins and their iBAQ intensities.

| log(2)iBAQ PEG-Fe3O4_1 | log(2)iBAQ PEG-Fe3O4_2 | log(2)iBAQ magnetosome_1 | log(2)iBAQ magnetosome_2 | Majority protein IDs | UniProt names | Protein names | Gene names |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 32.9362 | 32.1914 | 30.2231 | 29.5529 | K7ERI9 | APOC1_HUMAN | Apolipoprotein C-I | APOC1 |
| 31.2679 | 31.6847 | 29.7607 | 30.6996 | P18428 | LBP_HUMAN | Lipopolysaccharide-binding protein | LBP |
| 29.9217 | 31.6168 | 29.3135 | 28.5416 | Q5T985 | ITIH2_HUMAN | Inter-alpha-trypsin inhibitor heavy chain H2 | ITIH2 |
| 30.8688 | 31.2399 | 30.3755 | 30.6328 | P10909-4 | CLUS_HUMAN | Clusterin | CLU |
| 31.0809 | 31.1668 | 30.811 | 31.7447 | P01834 | IGKC_HUMAN | Ig kappa chain C region | IGKC |
| 30.5319 | 31.1301 | 31.7794 | 31.4634 | P02649 | APOE_HUMAN | Apolipoprotein E | APOE |
| 30.5037 | 30.6953 | 28.5046 | 28.5268 | P27169 | PON1_HUMAN | Serum paraoxonase/arylesterase 1 | PON1 |
| 29.1751 | 30.4944 | 28.2703 | 28.265 | P02748 | CO9_HUMAN | Complement component C9 | C9 |
| 29.9867 | 30.4387 | 29.1871 | 28.2997 | C9JV77 | C9JV77_HUMAN | Alpha-2-HS-glycoprotein | AHSG |
| 29.9146 | 30.386 | 29.2991 | 29.0027 | P02675 | D6REL8_HUMAN | Fibrinogen beta chain | FGB |
| 29.543 | 30.3333 | 28.5782 | 27.6897 | P05546 | HEP2_HUMAN | Heparin cofactor 2 | SERPIND1 |
| 28.5809 | 30.3094 | 27.9436 | 27.4747 | P02760 | AMBP_HUMAN | Protein AMBP | AMBP |
| 29.7939 | 30.0571 | 29.376 | 28.831 | P02679-2 | C9JC84_HUMAN | Fibrinogen gamma chain | FGG |
| 28.0942 | 29.9991 | 27.4137 | 26.8318 | P19827 | ITIH1_HUMAN | Inter-alpha-trypsin inhibitor heavy chain H1 | ITIH1 |
| 29.9044 | 29.8925 | 26.0678 | 26.1015 | B0YIW2 | APOC3_HUMAN | Apolipoprotein C-III | APOC3 |
| 29.782 | 29.8875 | 28.96 | 28.4062 | P02671 | FIBA_HUMAN | Fibrinogen alpha chain | FGA |
| 29.1715 | 29.7359 | 29.8563 | 30.0545 | P0DOY3 | IGLC3_HUMAN | Immunoglobulin lambda constant 3 | IGLC3 |
| 29.2702 | 29.5815 | 29.7356 | 29.7444 | P01042 | KNG1_HUMAN | Kininogen-1 | KNG1 |
| 28.7079 | 29.381 | 27.8382 | 27.4977 | P0C0L5 | CO4B_HUMAN | Complement C4-B | C4B |
| 29.1325 | 29.3287 | 29.4533 | 30.4008 | A0A0A0MS08 | A0A0A0MS07_HUMAN | Ig gamma-1 chain C region | IGHG1 |
| 28.1919 | 29.2484 | 28.3096 | 27.5591 | P04114 | APOB_HUMAN | Apolipoprotein B-100 | APOB |
| 28.7828 | 29.1743 | 31.6033 | 31.4225 | P04004 | VTNC_HUMAN | Vitronectin | VTN |
| 28.7209 | 29.1271 | 26.3561 | 27.046 | P11597 | CETP_HUMAN | Cholesteryl ester transfer protein | CETP |
| 28.9217 | 28.9784 | 29.0134 | 29.3093 | P02647 | APOA1_HUMAN | Apolipoprotein A-I | APOA1 |
| 28.2754 | 28.8093 | 25.6742 | 26.8404 | C9IZP8 | C9IZP8_HUMAN | Complement C1s subcomponent | C1S |
| 28.4299 | 28.7985 | 27.1183 | 27.3677 | P55058 | PLTP_HUMAN | Phospholipid transfer protein | PLTP |
| 28.0636 | 28.7522 | 27.4827 | 27.1024 | Q96PD5 | PGRP2_HUMAN | N-acetylmuramoyl-L-alanine amidase | PGLYRP2 |
| 28.7759 | 28.745 | 27.9557 | 29.1403 | P01859 | IGHG2_HUMAN | Ig gamma-2 chain C region | IGHG2 |
| 28.9662 | 28.6408 | 28.1284 | 28.7373 | P01876 | IGHA1_HUMAN | Ig alpha-1 chain C region | IGHA1 |
| 28.3564 | 28.5263 | 30.8208 | 31.9734 | P02768-1 | A0A087WWT3_HUMAN | Serum albumin | ALB |
| 29.1621 | 28.445 | 30.7995 | 30.6943 | P02776 | PLF4_HUMAN | Platelet factor 4 | PF4 |
| 28.4023 | 28.4072 | 26.7585 | 26.4399 | Q12805-2 | FBLN3_HUMAN | EGF-containing fibulin-like extracellular matrix protein 1 | EFEMP1 |
| 26.4407 | 28.3911 | 28.502 | 28.7774 | P59666 | DEF1_HUMAN | Neutrophil defensin 3 | DEFA3 |
| 28.1486 | 28.3719 | 26.6775 | 26.8006 | P08571 | CD14_HUMAN | Monocyte differentiation antigen CD14 | CD14 |
| 27.5458 | 28.3709 | 26.2127 | 25.6913 | O14791-3 | APOL1_HUMAN | Apolipoprotein L1 | APOL1 |
| 28.1369 | 28.295 | 26.5348 | 26.0067 | Q14624 | B7ZKJ8_HUMAN | Inter-alpha-trypsin inhibitor heavy chain H4 | ITIH4 |
| 28.1048 | 28.2808 |  |  | P0DJI8 | E9PQD6_HUMAN | Serum amyloid A-1 protein | SAA1 |
| 28.0547 | 28.1888 | 25.8977 | 25.5894 | P04003 | C4BPA_HUMAN | C4b-binding protein alpha chain | C4BPA |
| 27.8637 | 28.1727 | 26.7808 | 26.7158 | B4DPQ0 | B4DPQ0_HUMAN | Complement C1r subcomponent | C1R |
| 27.3516 | 28.108 | 25.5861 | 25.6936 | A0A0A0MS51 | A0A0A0MS51_HUMAN | Gelsolin | GSN |
| 27.2302 | 27.9539 | 25.4286 | 25.5019 | P23142 | FBLN1_HUMAN | Fibulin-1 | FBLN1 |
| 25.7022 | 27.8354 | 25.4941 | 24.7719 | P00734 | E9PIT3_HUMAN | Prothrombin | F2 |
| 27.2652 | 27.533 | 26.7206 | 27.647 | P02766 | A0A087WT59_HUMAN | Transthyretin | TTR |
| 25.5288 | 27.418 | 25.8468 | 24.682 | P00747 | PLMN_HUMAN | Plasminogen | PLG |
| 27.6197 | 27.4162 | 26.5617 | 26.3157 | D6RD17 | C9JA05_HUMAN | Immunoglobulin J chain | JCHAIN |
| 27.5036 | 27.416 | 26.1663 | 25.4465 | I3L145 | A0A0C4DGN2_HUMAN | Sex hormone-binding globulin | SHBG |
| 26.0503 | 27.3906 | 23.775 | 23.5765 | O00391 | QSOX1_HUMAN | Sulfhydryl oxidase 1 | QSOX1 |
| 26.7023 | 27.3607 | 26.0156 | 25.4176 | P08697 | A2AP_HUMAN | Alpha-2-antiplasmin | SERPINF2 |
| 27.5088 | 27.3406 | 29.8591 | 29.673 | A0A0A0MRJ7 | A0A0A0MRJ7_HUMAN | Coagulation factor V | F5 |
| 26.8286 | 27.3131 | 25.4453 | 25.3117 | P07358 | CO8B_HUMAN | Complement component C8 beta chain | C8B |
| 26.8997 | 27.2036 | 24.2224 | 24.2263 | P55056 | APOC4_HUMAN | Apolipoprotein C-IV | APOC4 |
| 27.5158 | 27.1306 | 26.8891 | 27.6057 | P01624 | A0A087WSY6_HUMAN | Ig kappa chain V-III region POM | IGKV3D-15 |
| 27.5109 | 27.1285 | 23.0539 | 24.1556 | P02749 | APOH_HUMAN | Beta-2-glycoprotein 1 | APOH |
| 27.5648 | 27.1234 | 19.485 | 21.1564 | O75636-2 | FCN3_HUMAN | Ficolin-3 | FCN3 |
| 27.3856 | 27.0985 | 26.5868 | 26.3448 | A0A096LPE2 | A0A096LPE2_HUMAN | Serum amyloid A-4 protein | SAA2-SAA4 |
| 27.114 | 27.0934 | 25.8899 | 26.3949 | A0A0U1RR20 | PRG4_HUMAN | Proteoglycan 4 | PRG4 |
| 26.5266 | 27.0922 | 24.9869 | 25.031 | G3V2W1 | G3V2W1_HUMAN | Protein Z-dependent protease inhibitor | SERPINA10 |
| 26.9045 | 27.0846 | 25.9025 | 26.5238 | V9GYM3 | APOA2_HUMAN | Apolipoprotein A-II | APOA2 |
| 26.1667 | 27.0824 | 25.2099 | 24.59 | P09871 | A0A087X232_HUMAN | Complement C1s subcomponent | C1S |
| 26.4792 | 27.046 | 26.0557 | 26.5829 | P01024 | CO3_HUMAN | Complement C3 | C3 |
| 26.6216 | 26.9797 | 24.6646 | 24.8602 | P30041 | PRDX6_HUMAN | Peroxiredoxin-6 | PRDX6 |
| 26.4333 | 26.9131 | 25.0115 | 24.5863 | P07225 | G5E9F8_HUMAN | Vitamin K-dependent protein S | PROS1 |
| 26.5905 | 26.9095 | 26.4266 | 25.7467 | P63261 | ACTA_HUMAN | Actin, cytoplasmic 2 | ACTG1 |
| 26.9789 | 26.9092 | 26.1644 | 26.3762 | P01619 | A0A0C4DH25_HUMAN | Ig kappa chain V-III region B6 | IGKV3D-20 |
| 26.9951 | 26.8546 | 25.3383 | 25.5 | E9PGN7 | E9PGN7_HUMAN | Plasma protease C1 inhibitor | SERPING1 |
| 26.7418 | 26.7753 | 24.7593 | 24.9256 | A0A087WSY5 | A0A087WSY5_HUMAN | Carboxypeptidase B2 | CPB2 |
| 26.3918 | 26.7283 | 24.6573 | 25.2313 | A0A087X1J7 | A0A087X1J7_HUMAN | Glutathione peroxidase | GPX3 |
| 25.7213 | 26.6558 | 25.0278 | 24.6478 | Q96KN2 | CNDP1_HUMAN | Beta-Ala-His dipeptidase | CNDP1 |
| 26.2319 | 26.5866 | 25.2799 | 25.365 | O00187 | MASP2_HUMAN | Mannan-binding lectin serine protease 2 | MASP2 |
| 26.0039 | 26.4622 | 23.3439 | 23.5407 | P29622 | KAIN_HUMAN | Kallistatin | SERPINA4 |
| 26.1267 | 26.454 | 25.2907 | 25.369 | Q6Q788 | APOA5_HUMAN | Apolipoprotein A-V | APOA5 |
| 26.3267 | 26.3065 | 24.447 | 24.4111 | P80108 | PHLD_HUMAN | Phosphatidylinositol-glycan-specific phospholipase D | GPLD1 |
| 25.3746 | 26.291 | 25.9994 | 26.129 | A2NJV5 | A0A075B6S2_HUMAN | Immunoglobulin kappa variable 2-29 | IGKV A18 |
| 25.9834 | 26.2798 | 25.0388 | 24.9501 | P30043 | BLVRB_HUMAN | Flavin reductase (NADPH) | BLVRB |
| 26.2875 | 26.2565 | 20.968 | 22.6555 | A0A0G2JMB2 | IGHA2_HUMAN | Ig alpha-2 chain C region | IGHA2 |
| 26.1984 | 26.2191 | 25.8295 | 26.1517 | P01860 | IGHG3_HUMAN | Ig gamma-3 chain C region | IGHG3 |
| 25.4473 | 26.0562 | 25.5398 | 25.2271 | E7ERK6 | E7ERK6_HUMAN | Clusterin | CLU |
| 23.8292 | 26.0276 | 24.0557 | 22.9167 | P07360 | CO8G_HUMAN | Complement component C8 gamma chain | C8G |
| 25.7827 | 25.8194 | 25.7595 | 26.1986 | P08493 | MGP_HUMAN | Matrix Gla protein | MGP |
| 25.2935 | 25.7107 | 22.8989 | 23.7636 | P06733 | ENOA_HUMAN | Alpha-enolase | ENO1 |
| 25.8858 | 25.6947 | 26.803 | 27.7242 | P68871 | F8W6P5_HUMAN | Hemoglobin subunit beta | HBB |
| 24.9659 | 25.6769 | 25.3314 | 24.322 | P06727 | APOA4_HUMAN | Apolipoprotein A-IV | APOA4 |
| 25.8665 | 25.6447 | 25.8723 | 25.6586 | P15169 | CBPN_HUMAN | Carboxypeptidase N catalytic chain | CPN1 |
| 24.8702 | 25.6446 | 23.3149 | 22.96 | F5H8B0 | F5H8B0_HUMAN | Coagulation factor VII | F7 |
| 24.5447 | 25.6263 | 25.818 | 26.5026 | A0A024R6I7 | A0A024R6I7_HUMAN | Alpha-1-antitrypsin | SERPINA1 |
| 25.5569 | 25.5788 | 24.1763 | 23.6346 | P32119 | A6NIW5_HUMAN | Peroxiredoxin-2 | PRDX2 |
| 25.6759 | 25.4468 | 26.6684 | 27.3239 | A0A0A0MRZ8 | A0A0A0MRZ8_HUMAN | Ig kappa chain V-III region VG | IGKV3D-11 |
| 25.2952 | 25.4252 | 23.7352 | 23.7314 | H0Y512 | APMAP_HUMAN | Adipocyte plasma membrane-associated protein | APMAP |
| 24.5162 | 25.2955 | 24.9408 | 24.2901 | Q15166 | C9JZ99_HUMAN | Serum paraoxonase/lactonase 3 | PON3 |
| 26.5747 | 25.267 | 25.7797 | 26.1024 | O43866 | CD5L_HUMAN | CD5 antigen-like | CD5L |
| 23.9141 | 25.2499 | 21.4305 | 21.791 | Q06033-2 | A0A087WW43_HUMAN | Inter-alpha-trypsin inhibitor heavy chain H3 | ITIH3 |
| 24.8281 | 25.2116 |  |  | E9PQI5 | CHM4A_HUMAN | Charged multivesicular body protein 4a | CHMP4A |
| 25.3594 | 25.1423 | 25.6213 | 25.6294 | S4R460 | A0A0B4J2B5_HUMAN | Immunoglobulin heavy variable 3/OR16-9 (non-functional) | IGHV3OR16-9 |
| 25.1187 | 25.135 | 24.2585 | 23.9558 | Q9BWP8-8 | COL11_HUMAN | Collectin-11 | COLEC11 |
| 24.8922 | 25.1221 | 27.7426 | 27.1342 | J3KNB4 | CAMP_HUMAN | Cathelicidin antimicrobial peptide | CAMP |
| 24.8646 | 25.1019 | 24.5791 | 25.3665 | P06310 | A0A075B6S6_HUMAN | Ig kappa chain V-II region RPMI 6410 | IGKV2D-30 |
| 25.0903 | 25.0803 | 25.3211 | 25.3471 | E7EUT5 | E7EUT5_HUMAN | Glyceraldehyde-3-phosphate dehydrogenase | GAPDH |
| 25.2295 | 25.0328 | 25.4572 | 26.1873 | P69905 | G3V1N2_HUMAN | Hemoglobin subunit alpha | HBA1 |
| 24.3079 | 25.0153 | 24.1181 | 24.0439 | P35858 | ALS_HUMAN | Insulin-like growth factor-binding protein complex acid labile subunit | IGFALS |
| 24.4678 | 25.0014 | 25.8086 | 25.5652 | P10646 | C9JBB3_HUMAN | Tissue factor pathway inhibitor | TFPI |
| 24.5216 | 24.9413 | 25.564 | 25.3856 | P35908 | K22E_HUMAN | Keratin, type II cytoskeletal 2 epidermal | KRT2 |
| 24.6461 | 24.9203 | 25.2155 | 24.8411 | Q99969 | C9J8S2_HUMAN | Retinoic acid receptor responder protein 2 | RARRES2 |
| 24.486 | 24.9072 | 22.1186 | 20.4289 | P04180 | J3QSE5_HUMAN | Phosphatidylcholine-sterol acyltransferase | LCAT |
| 23.6493 | 24.6999 | 26.0678 | 26.6733 | P02790 | HEMO_HUMAN | Hemopexin | HPX |
| 24.651 | 24.6237 | 22.8554 | 23.6184 | A0A0B4J231 | A0A0B4J231_HUMAN | Immunoglobulin lambda-like polypeptide 5 | IGLL5 |
| 22.4527 | 24.5598 | 23.6992 | 23.3253 | B5MDF5 | B4DV51_HUMAN | GTP-binding nuclear protein Ran | RAN |
| 23.6587 | 24.4865 | 26.0309 | 25.3522 | P61224-2 | B7ZB78_HUMAN | Ras-related protein Rap-1b | RAP1B |
| 24.7413 | 24.3984 | 20.0387 | 22.5851 | A0A0C4DH35 | A0A0C4DH35_HUMAN | Immunoglobulin heavy variable 3-35 (non-functional) | IGHV3-35 |
| 23.6063 | 24.3574 | 21.7091 | 20.8128 | P07357 | CO8A_HUMAN | Complement component C8 alpha chain | C8A |
| 22.0767 | 24.3541 | 23.8255 | 22.4277 | P08519 | APOA_HUMAN | Apolipoprotein(a) | LPA |
| 24.3126 | 24.3056 | 22.2665 | 23.8304 | P01764 | HV303_HUMAN | Ig heavy chain V-III region 23 | IGHV3-23 |
| 23.7701 | 24.2802 | 21.127 | 19.9512 | P20851-2 | C4BPB_HUMAN | C4b-binding protein beta chain | C4BPB |
| 25.7613 | 24.2733 | 25.4742 | 25.4277 | A0A0B4J1X5 | A0A075B7E8_HUMAN | Ig heavy chain V-III region BUT | IGHV3-74 |
| 24.1166 | 24.2153 | 22.0834 | 22.8977 | Q86UX7-2 | URP2_HUMAN | Fermitin family homolog 3 | FERMT3 |
| 23.2172 | 24.1499 | 22.8584 | 21.8646 | A0A0G2JPR0 | A0A0G2JPR0_HUMAN | Complement C4-A | C4A |
| 23.6101 | 24.0539 | 21.686 | 21.0822 | P02747 | C1QC_HUMAN | Complement C1q subcomponent subunit C | C1QC |
| 24.7465 | 24.0531 | 25.2263 | 24.1045 | O14960 | D6RD58_HUMAN | Leukocyte cell-derived chemotaxin-2 | LECT2 |
| 24.3022 | 24.0111 | 23.7054 | 24.1575 | P01011 | AACT_HUMAN | Alpha-1-antichymotrypsin | SERPINA3 |
| 22.4373 | 24.0052 |  |  | Q9UGM5 | E9PG08_HUMAN | Fetuin-B | FETUB |
| 24.0318 | 23.985 | 22.2559 | 21.8509 | Q9Y490 | TLN1_HUMAN | Talin-1 | TLN1 |
| 23.7917 | 23.9482 | 22.009 | 21.9833 | Q15113 | PCOC1_HUMAN | Procollagen C-endopeptidase enhancer 1 | PCOLCE |
| 20.0293 | 23.9443 | 23.4519 | 24.1622 | P01019 | ANGT_HUMAN | Angiotensinogen | AGT |
| 23.9728 | 23.9299 | 22.7654 | 22.351 | Q5T4F6 | A0A0C4DFP6_HUMAN | Cartilage acidic protein 1 | CRTAC1 |
| 24.1097 | 23.9235 | 19.6295 | 21.2237 | Q08830 | FGL1_HUMAN | Fibrinogen-like protein 1 | FGL1 |
| 23.4378 | 23.8957 | 23.9238 | 23.2574 | P02730-2 | A0A0A0MS98_HUMAN | Band 3 anion transport protein | SLC4A1 |
| 23.7254 | 23.8937 | 25.0132 | 25.554 | P06312 | KV401_HUMAN | Ig kappa chain V-IV region | IGKV4-1 |
| 23.072 | 23.8327 | 25.5702 | 25.4572 | Q13103 | C9J6K0_HUMAN | Secreted phosphoprotein 24 | SPP2 |
| 23.4216 | 23.776 | 22.9198 | 23.0187 | Q9BXN1 | ASPN_HUMAN | Asporin | ASPN |
| 23.9213 | 23.7494 | 21.0616 | 21.7834 | P07996 | TSP1_HUMAN | Thrombospondin-1 | THBS1 |
| 24.1285 | 23.7417 | 21.2893 | 22.1324 | P15291-2 | B4GT1_HUMAN | Beta-1,4-galactosyltransferase 1 | B4GALT1 |
| 24.3239 | 23.7314 | 19.8175 | 21.537 | B1ALD9 | B1ALD9_HUMAN | Periostin | POSTN |
| 22.5312 | 23.7139 | 25.3427 | 25.5071 | P04196 | HRG_HUMAN | Histidine-rich glycoprotein | HRG |
| 25.5087 | 23.5837 | 22.9755 | 22.1025 | P0DP01 | A0A0B4J2H0_HUMAN | Ig heavy chain V-I region HG3 | IGHV1-3 |
| 23.9436 | 23.5793 | 19.9806 | 17.057 | E7ER44 | E7EQB2_HUMAN | Lactotransferrin | LTF |
| 24.1868 | 23.5168 | 24.1528 | 23.4956 | P48061-2 | SDF1_HUMAN | Stromal cell-derived factor 1 | CXCL12 |
| 22.6096 | 23.5074 | 22.4244 | 21.8006 | P00739 | A0A0A0MRD9_HUMAN | Haptoglobin-related protein | HPR |
| 23.0381 | 23.5005 | 25.4025 | 25.1668 | A0A075B6I0 | A0A075B6I0_HUMAN | Immunoglobulin lambda variable 8-61 | IGLV8-61 |
| 22.4219 | 23.4825 | 22.2744 | 22.1954 | A6NMS2 | A0A0B4J207_HUMAN | Ribose-phosphate pyrophosphokinase 1 | PRPS2 |
| 23.5229 | 23.4492 | 25.5873 | 25.1969 | C9JMX4 | A6XND0_HUMAN | Insulin-like growth factor-binding protein 3 | IGFBP3 |
| 21.5193 | 23.4225 | 25.8019 | 26.3958 | A0A087X0Q4 | A0A075B6P5_HUMAN | Ig kappa chain V-II region FR | IGKV2-40 |
| 24.1063 | 23.4209 | 21.7819 | 21.802 | G3V4U0 | FBLN5_HUMAN | Fibulin-5 | FBLN5 |
| 21.9837 | 23.3362 | 23.5188 | 24.5292 | G3V482 | G3V264_HUMAN | Plasma serine protease inhibitor | SERPINA5 |
| 23.3784 | 23.2924 | 22.1795 | 22.5934 | P01042-2 | KNG1_HUMAN | Kininogen-1 | KNG1 |
| 24.266 | 23.2169 |  |  | P0DJI9 | SAA2_HUMAN | Serum amyloid A-2 protein | SAA2 |
| 24.0634 | 23.2136 | 22.4345 | 23.3807 | C9JX71 | APOD_HUMAN | Apolipoprotein D | APOD |
| 25.8761 | 23.1607 | 22.8128 | 20.7747 | A0A0B4J1V0 | A0A0B4J1V0_HUMAN | Immunoglobulin heavy variable 3-15 | IGHV3-15 |
| 21.525 | 23.1517 | 19.6423 | 19.0882 | K7ERG9 | CFAD_HUMAN | Complement factor D | CFD |
| 22.1427 | 22.8337 | 20.4325 | 20.108 | G3V0E5 | G3V0E5_HUMAN | Transferrin receptor protein 1 | TFRC |
| 22.0475 | 22.8161 |  |  | Q8WUA8 | TSK_HUMAN | Tsukushin | TSKU |
| 22.6631 | 22.7573 | 23.5031 | 22.8446 | Q8TF72 | SHRM3_HUMAN | Protein Shroom3 | SHROOM3 |
| 23.7986 | 22.7546 |  |  | P55103 | INHBC_HUMAN | Inhibin beta C chain | INHBC |
| 22.6552 | 22.6318 | 21.0987 | 21.1932 | E7EUF1 | E5RIA2_HUMAN | Ectonucleotide pyrophosphatase/phosphodiesterase family member 2 | ENPP2 |
| 22.1072 | 22.6127 | 21.1401 | 20.4174 | E7ES19 | E7ES19_HUMAN | Thrombospondin-4 | THBS4 |
| 22.5902 | 22.4885 | 21.246 | 21.31 | Q96N23-2 | CFA54_HUMAN | Cilia- and flagella-associated protein 54 | CFAP54 |
| 21.83 | 22.3833 | 22.7911 | 23.9459 | P01861 | IGHG4_HUMAN | Ig gamma-4 chain C region | IGHG4 |
| 21.7445 | 22.3535 | 23.1292 | 23.3601 | A0A087WX17 | A0A087WU43_HUMAN | Cadherin-1 | CDH1 |
| 22.5059 | 22.3329 |  |  | Q5QPM7 | F5H4Z3_HUMAN | Proteasome inhibitor PI31 subunit | PSMF1 |
| 21.6625 | 22.3321 | 17.857 | 20.9317 | Q13790 | APOF_HUMAN | Apolipoprotein F | APOF |
| 22.0884 | 22.3134 | 20.3903 | 20.7261 | B4DQI1 | B4DQI1_HUMAN | Complement C2 | C2 |
| 21.3525 | 22.2101 |  |  | P22792 | CPN2_HUMAN | Carboxypeptidase N subunit 2 | CPN2 |
| 23.3649 | 22.1196 | 23.7239 | 23.462 | Q9Y6Z7 | COL10_HUMAN | Collectin-10 | COLEC10 |
| 22.8137 | 22.0173 | 23.3541 | 22.7804 | K7EKF6 | ANGL6_HUMAN | Angiopoietin-related protein 6 | ANGPTL6 |
| 23.5414 | 21.9409 | 23.2871 | 22.6578 | D6RGJ1 | A0A0A0MSV6_HUMAN | Complement C1q subcomponent subunit B | C1QB |
| 22.7836 | 21.87 |  |  | Q9UJJ9 | GNPTG_HUMAN | N-acetylglucosamine-1-phosphotransferase subunit gamma | GNPTG |
| 22.4226 | 21.8579 |  |  | Q92743 | HTRA1_HUMAN | Serine protease HTRA1 | HTRA1 |
| 21.6992 | 21.8395 | 19.5347 | 21.1748 | E7ETN3 | B4E1Z4_HUMAN | Complement factor B | CFB |
| 20.9225 | 21.7519 | 21.2909 | 21.7375 | P06858 | LIPL_HUMAN | Lipoprotein lipase | LPL |
| 21.1078 | 21.7261 | 20.867 | 21.2017 | P68366-2 | C9J2C0_HUMAN | Tubulin alpha-4A chain | TUBA4A |
| 20.7838 | 21.7204 |  |  | Q86U17 | SPA11_HUMAN | Serpin A11 | SERPINA11 |
| 20.8638 | 21.6794 | 22.8006 | 22.9958 | E7ENL6 | CO6A3_HUMAN | Collagen alpha-3(VI) chain | COL6A3 |
| 20.5492 | 21.5185 |  |  | B1AHL2 | B1AHL2_HUMAN | Fibulin-1 | FBLN1 |
| 22.5159 | 21.368 |  |  | H3BV48 | H3BR66_HUMAN | 72 kDa type IV collagenase | MMP2 |
| 19.2906 | 21.3272 | 21.6234 | 22.5005 | P01008 | ANT3_HUMAN | Antithrombin-III | SERPINC1 |
| 23.0264 | 21.3163 | 23.8076 | 24.1819 | P01700 | LV102_HUMAN | Ig lambda chain V-I region HA | IGLV1-47 |
| 19.4582 | 21.198 | 17.9843 | 18.6555 | P26572 | D6RF69_HUMAN | Alpha-1,3-mannosyl-glycoprotein 2-beta-N-acetylglucosaminyltransferase | MGAT1 |
| 22.0242 | 21.1711 |  |  | Q15485-2 | FCN2_HUMAN | Ficolin-2 | FCN2 |
| 21.976 | 20.8541 | 24.0582 | 22.6335 | E7EPG1 | E7EPG1_HUMAN | Multimerin-1 | MMRN1 |
| 22.0685 | 20.7618 | 25.9096 | 27.2007 | J3QLC9 | A0A087WU08_HUMAN | Haptoglobin | HP |
| 19.7853 | 20.6871 | 24.4499 | 26.0052 | P01023 | A2MG_HUMAN | Alpha-2-macroglobulin | A2M |
| 18.55 | 20.5909 |  |  | J3QS41 | A0A075B6R3_HUMAN | Probable helicase with zinc finger domain | HELZ |
| 19.6333 | 20.5725 | 20.1909 | 20.9618 | H0YAC1 | E9PBC5_HUMAN | Plasma kallikrein | KLKB1 |
| 19.3558 | 20.5199 |  |  | Q76LX8-3 | A0A0C4DFV8_HUMAN | A disintegrin and metalloproteinase with thrombospondin motifs 13 | ADAMTS13 |
| 19.3171 | 20.1055 | 24.5247 | 23.5271 | P03950 | ANGI_HUMAN | Angiogenin | ANG |
| 18.442 | 20.0889 | 17.6063 | 18.9142 | P01031 | CO5_HUMAN | Complement C5 | C5 |
| 19.1041 | 19.9446 | 20.7104 | 21.9197 | D6RF35 | D6RF35_HUMAN | Vitamin D-binding protein | GC |
| 18.8836 | 19.7249 | 14.3476 | 14.7504 | P04275 | VWF_HUMAN | von Willebrand factor | VWF |
| 18.0749 | 19.5624 | 25.3231 | 26.8527 | P02787 | TRFE_HUMAN | Serotransferrin | TF |
| 20.7425 | 19.1622 |  |  | Q9UNW1-4 | MINP1_HUMAN | Multiple inositol polyphosphate phosphatase 1 | MINPP1 |
| 18.4448 | 18.5262 | 21.737 | 21.3951 | P08514-3 | ITA2B_HUMAN | Integrin alpha-IIb | ITGA2B |
| 16.7138 | 18.2408 |  |  | P02743 | SAMP_HUMAN | Serum amyloid P-component | APCS |
| 21.241 | 16.8864 |  |  | P55290-5 | CAD13_HUMAN | Cadherin-13 | CDH13 |
| 16.5787 | 16.1469 | 23.6816 | 23.4411 | H0YH81 | ATPB_HUMAN | ATP synthase subunit beta | ATP5B |
|  |  | 24.4977 | 23.449 | P03951 | D6RB32_HUMAN | Coagulation factor XI | F11 |
|  |  | 24.31 | 22.9198 | E5RJZ5 | E5RJZ5_HUMAN | Clusterin | CLU |
|  |  | 23.9907 | 24.1158 | A0A0A0MT60 | A0A0A0MT60_HUMAN | Peptidyl-prolyl cis-trans isomerase | FKBP15 |
|  |  | 23.6468 | 23.5013 | O75594 | PGRP1_HUMAN | Peptidoglycan recognition protein 1 | PGLYRP1 |
|  |  | 23.4605 | 23.356 | F8VV32 | A0A0B4J259_HUMAN | Lysozyme | LYZ |
|  |  | 23.4136 | 22.915 | P23526-2 | SAHH_HUMAN | Adenosylhomocysteinase | AHCY |
|  |  | 23.4048 | 23.468 | H7BZ89 | CTSR2_HUMAN | Cation channel sperm-associated protein 2 | CATSPER2 |
|  |  | 23.3975 | 25.2762 | P02763 | A1AG1_HUMAN | Alpha-1-acid glycoprotein 1 | ORM1 |
|  |  | 22.8751 | 22.1172 | P25705-2 | ATPA_HUMAN | ATP synthase subunit alpha, mitochondrial | ATP5A1 |
|  |  | 22.4218 | 23.9366 | P04217-2 | A1BG_HUMAN | Alpha-1B-glycoprotein | A1BG |
|  |  | 21.1088 | 22.4169 | E9PFZ2 | CERU_HUMAN | Ceruloplasmin | CP |

| Table S3. Top 20 plasma proteins. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| ID | Gene | µM/L | % | pI | MW.(kDa) | GRAVY |
| P02768 | ALB | 650 | 40.39598 | 5.92 | 69.36668 | -0.354 |
| P01834 | IGKC | 109 | 6.774095 | 6.075 | 11.765 | -0.537 |
| P01857 | IGHG1 | 85 | 5.282551 | 7.778 | 36.106 | -0.428 |
| P0CG04 | IGLC2 | 60 | 3.72886 | 7.89 | 11.348 | -0.52 |
| P01859 | IGHG2 | 55 | 3.418121 | 7.66 | 35.901 | -0.419 |
| P02647 | APOA1 | 50 | 3.107383 | 5.56 | 30.77783 | -0.717 |
| P02652 | APOA2 | 45 | 2.796645 | 6.27 | 11.17502 | -0.084 |
| P02787 | TF | 35 | 2.175168 | 6.81 | 77.06389 | -0.336 |
| P01009 | SERPINA1 | 29 | 1.802282 | 5.37 | 46.73655 | -0.183 |
| P01876 | IGHA1 | 29 | 1.802282 | 6.08 | 37.65465 | -0.206 |
| P02766 | TTR | 22.5 | 1.398322 | 5.49 | 15.88703 | -0.029 |
| P00738 | HP | 20 | 1.242953 | 6.13 | 45.20531 | -0.421 |
| P02765 | AHSG | 19.5 | 1.211879 | 5.43 | 39.32468 | -0.196 |
| P02671 | FGA | 18.5 | 1.149732 | 5.7 | 94.97304 | -0.822 |
| P02675 | FGB | 18.5 | 1.149732 | 8.54 | 55.92815 | -0.758 |
| P02679 | FGG | 16.5 | 1.025436 | 5.37 | 51.51166 | -0.588 |
| P02790 | HPX | 14.5 | 0.901141 | 6.55 | 51.67637 | -0.434 |
| P02763 | ORM1 | 14.5 | 0.901141 | 4.93 | 23.51156 | -0.536 |
| P01871 | IGHM | 14.5 | 0.901141 | 6.35 | 49.30659 | -0.319 |
| P02656 | APOC3 | 13 | 0.80792 | 5.23 | 10.85231 | -0.086 |

Table S4. α-helix percentage calculation of ApoE and HSA.

|  | %α-helix |
| --- | --- |
| ApoE | 83% |
| Magnetosome:ApoE=1:6 | 92% |
| Magnetosome:ApoE=1:2 | 91% |
| Magnetosome:ApoE=1:1 | 97% |
| PEG-Fe3O4:ApoE=1:6 | 82% |
| PEG-Fe3O4:ApoE=1:2 | 78% |
| PEG-Fe3O4:ApoE=1:1 | 81% |
| HSA | 60% |
| Magnetosome:HSA=1:6 | 67% |
| Magnetosome:HSA=1:2 | 74% |
| Magnetosome:HSA=1:1 | 76% |
| PEG-Fe3O4:HSA=1:6 | 42% |
| PEG-Fe3O4:HSA=1:3 | 34% |
| PEG-Fe3O4:HSA=1:1 | 43% |

Table S5. GO molecular function enrichment of the abundant proteins on magnetosome corona.

| GO ID | GO Term | Term P Value* | GO Levels | % Associated Genes | Nr. Genes | Associated Genes Found |
| --- | --- | --- | --- | --- | --- | --- |
| GO:0005102 | signaling receptor binding | 7.28181E-08 | [3] | 0.77 | 13 | [APOA1, APOE, CLU, FGA, FGB, FGG, IGHG1, IGHG2, IGKC, KNG1, LBP, PF4, VTN] |
| GO:0005504 | fatty acid binding | 0.024462798 | [3, 6] | 5.56 | 2 | [ALB, APOC1] |
| GO:0034987 | immunoglobulin receptor binding | 0.002095056 | [4] | 4.48 | 3 | [IGHG1, IGHG2, IGKC] |
| GO:0004857 | enzyme inhibitor activity | 0.036052101 | [3] | 0.93 | 4 | [AHSG, APOC1, ITIH2, KNG1] |
| GO:0004866 | endopeptidase inhibitor activity | 0.030579127 | [5] | 1.71 | 3 | [AHSG, ITIH2, KNG1] |
| GO:0042277 | peptide binding | 0.012540383 | [3] | 1.28 | 4 | [APOA1, APOE, CLU, LBP] |
| GO:0043169 | cation binding | 0.043310294 | [3] | 0.51 | 6 | [ALB, APOA1, APOC1, APOE, CLU, KNG1] |
| GO:0008201 | heparin binding | 0.011718875 | [3, 4] | 2.46 | 3 | [APOE, KNG1, PF4] |
| GO:0017127 | cholesterol transporter activity | 0.009904793 | [4] | 9.09 | 2 | [APOA1, APOE] |
| GO:0060228 | phosphatidylcholine-sterol O-acyltransferase activator activity | 1.68739E-06 | [4] | 42.86 | 3 | [APOA1, APOC1, APOE] |
| GO:0070325 | lipoprotein particle receptor binding | 0.000356912 | [4] | 8.11 | 3 | [APOA1, APOE, CLU] |
| GO:0046911 | metal chelating activity | 0.034347695 | [5] | 100.00 | 1 | [APOE] |
| *: Corrected with Bonferroni step down |  |  |  |  |  |  |