Supporting Information

ADDITIONAL FIGURES

Figure S1: UV Vis spectra of Gd -Au complex under basic (black line i.e. Gd basic) and acidic (red line i.e. Gd acid) conditions in aqueous solution.

Figure S2. Changes in the UV-Vis absorption spectra of Gd@ AuNPs (NP1 NP2 NP3) when incubated in cell culture media (DMEM + 10% FBS)  respectively up to 72h. The absorption peak of nanoparticles was unchanged and the size and shape were not compromised

Figure S3: EDX microanalysis of Gd@AuNPs

Figure S4: (A) Percentage (%) of Gd (III) as Au-@Gd complex , released from NP3 overtime in PBS (37 °C) at pH = 4.0 (red dots).  (B) Variations of the Raman band intensity at 260 cm-1versus time. NP3 was incubated in PBS (37 °C) at pH 4.0 ; (C) TEM images and conformational shape modifications under PBS (37 °C) .

Figure S5: Spleen and kidney organs biodistribution recorded by In vivo DCE MRI at 7T.

ADDITIONAL TABLES

Table S1: z-potential and hydrodynamic diameter of NP1, NP2, NP3.

| Synthetic product | Zeta potential (mV) | Hydrodynamic diameter (nm) | PdI |
| --- | --- | --- | --- |
| NP1 | -25 ± 2 | 20 ± 2 | 0.3±2 |
| NP2 | -20 ± 1 | 40± 2 | 0.3±2 |
| NP3 | 23 ± 1 | 60± 2 | 0.3±2 |