Supplementary Data

Advanced Mg, Zn, Sr, Si multi-substituted hydroxyapatites for bone regeneration

Corina Garbo, Janis Locs,  Matteo D’Este, Gerard Demazeau†,  Aurora Mocanu, Cecilia Roman, Ossi Horovitz and Maria Tomoaia-Cotisel

Figure S1 Comparison of experimental XRD pattern for calcined HAPc-10%Sr with PDF 34-0484 for Ca9Sr(PO4)6(OH)2, red lines.

Table S1 Characteristic wave numbers (in cm-1) of the main absorption maxima in the FTIR spectra of the eight hydroxyapatites

| 1 HAP non calc. | 2 HAP calc. | 3 HAPc non calc. | 4 HAPc calc. | 5 HAPc- 5%Sr non calc. | 6 HAPc-5%Sr calc. | 7 HAPc- 10%Sr non calc. | 8 HAPc- 10%Sr calc. | Assignment of vibrations |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3570 3438 1635 - 1421 1094 1043 962 875 634 603 567 472 | 3571 3435 1631 1446 1415 1093 1043 962 - 633 604 567 473 | 3567 3430 1635 1457 1422 1097 1038 963 875 sh 604 565 (472) | 3569 3431 1632 1451 1416 1096 1037 963 876 630 604 566 473 | 3565 3420 1634 1452 1419 1096 1037 962 875 sh 604 565 472 | 3568 3430 1634 1448 1416 1095 1041 962 877 sh 604 565 472 | sh 3429 1633 1446 1419 1095 1040 961 875 sh 603 565 472 | 3568 3431 1637 1447 1417 1094 1038 961 876 sh 603 565 472 | stretching: structural O-H from HAP O-H…O stretching –abs. water with H-bonding absorbed water bending mode ν2 CO32- CO32- PO4 asymmetric stretching ν3 -“- PO4 symmetric stretching ν1 (forbidden in IR) CO32- structural OH – libration PO4 asymmetric bending ν4 -“- PO4 symmetric bending ν2 |

Abbreviations: sh = shoulder; abs. water = absorbed water; non calc. = non calcined lyophilized; calc. = calcined lyophilized; values for the highest absorption peak are listed in bold.

Figure S2 Calcined lyophilized HAPc-5%Sr (sample 6, in Table 1): distribution maps of individual elements, as given by EDX spectrum.

Figure S3 Specific surface areas of all investigated nano powders; error bars indicate the standard deviations.

Figure S4 Korsmeyer-Peppas regression lines for strontium release profiles from HAPc-5%Sr non calcined in water (a) and in SBF (c) as well as from HAPc-5%Sr calcined in water (b) and in SBF (d).