[image: image1.png]



Figure S1. Photographs of CEL-NPs solutions (in water) under laser beam irradiation. The concentration of the CEL-NPs solutions were (a) 2.0 mg mL-1, (b) 1 mg mL-1, and (c) 0.5 mg mL-1. 
[image: image2.png]B - ~v ~v ~v ad et ey ~v

125 115 105 9.5 8.5 7.5 6.5 5.5 4.5 3.5 2.5 1.5 0.5
Chemical shift (ppm)




Figure S2. Typical 1H NMR spectra of mPEG-PLL in D2O (A), CEL in DMSO-d6, (B) and CEL-NPs in D2O (C). 
[image: image3.png]Absorbance

1.0

0.8

0.6

0.4

0.2

0.0

350

400

— CEL

—— CEL-NPs

— mPEG-PLL

450 500
Wavelength (nm)

550

600




Figure S3. UV-Vis Spectra of mPEG-PLL, 15.6 μg mL-1 CEL, and 115 μg mL-1 CEL-NPs dissolved in DMSO. 
[image: image4.png]o o o o
n N » ©

(wu) J83awelqg

12 24

8 10

6
Time (h)




Figure S4. Sizes of the CEL-NPs in pH 7.4 PBS solution containing 10 % fetal bovine serum measured at different times. The data are presented as mean ± standard deviation (n = 3).
[image: image5.png]Q
7o)
N

(=

Q Q Q
Q T = To)
1

N

Alisuajul 14 abesany

1

Time (h)




Figure S5. The mean fluorescence intensities for the tested groups in the FCA images (Figure 3). The data are presented as mean ± SD (n = 3).

                  [image: image6.png]75

(= ) o
O < (op)

Ajisuap |eondo

To
~—

Time (h)




Figure S6. The mean fluorescence intensities of the tested groups in the CLSM images (Figure 4). The data are presented as mean ± SD (n = 3).

