Supplemental Materials
Antigen-conjugated silica solid sphere as nanovaccine for cancer immunotherapy
Ying Dong, Jing Gao,* Mengyue Pei, Xiaoli Wang,* Chuangnian Zhang, Yingjie Du,Yanjun Jiang
[image: image1.png]Si0:-OH
—— OVA@SIO:

———.N\__.,——"

3405

1098

P 470

4000 3500 3000 2500 2000 1500 1000

500

Wavenumber (cm'l)

B

RAW246.7

150F

100

50

Cell viability (%)

AV p H A% H DO
Y9 &

The concentration of nanoparticle (ug mL'l)

e 1040 Uptake of CpG

o

ok

Kk
EO.G-
= 0.4}¢
0.2F
0.0
co o« o XCQG
oV P S 1
0‘”"
lOO 106 10 10

+10° OVA@SiO,+CpG
.0 AT





Figure S1. (A) FTIR of SiO2-OH and OVA@SiO2. (B) The in vitro of stability in buffer solution of OVA from OVA@SiO2, Cell viability of RAW246.7 after incubating with OVA@SiO2 for 48 h, culture medium was used as control, the data are expressed as mean ± SD (n =5). (C) The uptake of CpG (A) estimated by MFI of DC2.4 cells, and their representative FACS histograms after incubation for 4 h with different formulations in the absence or presence of inhibitor including rottlerin (Rot), chlorpromazine (Chlor), filipin III (Fil III) and cytochalasin D (Cyt D). Data were the mean ± SD (n = 5), and the differences were analyzed by one way ANOVA with Tukey's Multiple Comparison Test.
[image: image2.png]Q
Q.
O
_I_
<
>
O
Q
=¥
O
—I_('\l
Q
AN
S
<
>
O
B
Q
Q.
O
_I_
<
>
O

A OVA@SIO+CpG

1

o
h
-

b
-
-

[—
h
-

Un
-

: 3
1

L )
OO 50 100 150 200 250 50 100 150 200 250

Intensity of CpG-Cy3 Intensity of CpG-Cy3

Intensity of Lamp





Figure S2. (A, B) CLSM images of BMDCs after incubating with soluble OVA+CpG, OVA@SiO2+CpG for 8h and 24 h, the endosomes/lysosomes were stained with Lamp-1-APC, the nucleus was stained with DAPI, OVA-FITC and CpG-Cy3 were used, (C) Quantitative colocalization analysis of CLSM images was performed by Zeiss Zen 2008 Software.
