Characterization of ZnO QDs

Transmission electron microscopy (TEM) images were measured with a TecnaiG2 F30 (FEI, USA). The size distribution and zeta potentials was determined using a BI-200SM (Brookhaven, USA). Fluorescence spectra were recorded on a RF-5301PC fluorescence spectrometer (Shimadzu, Japan). 

Results
The average diameter of ZnO QDs is approximately 5.4 nm according to transmission electron microscopy (TEM, Figure S1A) and dynamic light scattering (DLS, Figure S1B), and their strong fluorescence is centered at 525 nm and excitation maximum at 360 nm (Figure S1C). 
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Figure S1 Characterization of ZnO QDs. (A) TEM, (B) DLS, and (C) Fluorescence spectra
Abbreviations: QDS, quantum dots
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Figure S2 Venn diagram showing the overlapping GO terms between the liver and lung samples. 

Abbreviations: GO, Gene Ontology; Li, Liver; Lu, Lung.
