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Figure S1. The SEM images of crosslinked scaffolds after immersion in PBS. (A) Pure PCL, (B) PCL/PTMC-MA (3:1), (C) PCL/PTMC-MA (1:1), (D) PCL/PTMC-MA (1:3) and (E) PTMC-MA. Scale bar: 10 m.

Table S1. Average molecular weight and polydispersity index (PDI) of PTMC characterized by GPC.
	
	Mn (kg/mol)
	Mw (kg/mol)
	PDI

	PTMC
	21.90
	34.30
	1.56




Table S2. The optimum exposure time of pure PTMC-MA
	Exposure time/min
	5
	10
	15

	Dry mass-initial/g
	0.0268
	0.0159
	0.0318

	Dry mass-final/g
	0.0241
	0.0158
	0.0288

	Sol content 
	89.93%
	99.37%
	90.57%
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