Supplementary Data

Figure S1 Simple photo-batch catalytic oxidation reactor.

Figure S2 Williamson-Hall plots for MgO NP.

Table S1 Parameters obtained for MgO NP from XRD analysis

| Pos. 2θ (deg) | fwhm (deg) | hkl planes | β*cos(θ) | 4*sin(θ) | 4*tan(θ) | Williamson-Hall |  | Debye-Scherer |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | crystallite size (nm) | lattice strain | crystallite size (nm) | lattice strain |
| 36.811 | 0.12079 | 111 | 0.002 | 1.263 | 1.33 | 21.33 | 0.00004 | 69.31 | 0.0016 |
| 43.781 | 0.79776 | 200 | 0.013 | 1.491 | 1.61 |  |  | 10.73 | 0.0087 |
| 62.156 | 0.31893 | 220 | 0.005 | 2.065 | 2.41 |  |  | 29.08 | 0.0023 |
| Average |  |  |  |  |  | 21.33 | 0.00004 | 36.38 | 0.0042 |

2θ (degrees): Diffraction angle; hkl: The Miller indices define the reciprocal axial intercepts of a plane of atoms and fwhm: full width half maximum