Supporting Information

Hybrid nanoparticles modified by hyaluronic acid loading an Hsp90 inhibitor as a novel delivery system for subcutaneous and orthotopic colon cancer therapy

Chen-Wei Pan1#, Tiao-Tiao Zhang2,5#, Shao-Xun Li1,5#,  Zhi-Hua Xu2,5, Bin-Hui Pan2,5, Sheng Xu2,5, Shuang-Hong Jin1,5, Guang-Rong Lu2, Shou-Xing Yang2, Zhan-Xiong Xue2, Ping Chen6, Xian Shen3*, Fang-Yan Wang4* and Chang-Long Xu2,7*

Affiliations:

1 Department of Infectious Disease, The Second Affiliated Hospital and Yuying Children’s Hospital of Wenzhou Medical  University , Wenzhou, Zhejiang, 325000, China

2 Department of Gastroenterology, The Second Affiliated Hospital and Yuying Children's Hospital of Wenzhou Medical University, Wenzhou, Zhejiang, 325000, China

3 Department of Gastrointestinal Surgery, The Second Affiliated Hospital and Yuying Children's Hospital of Wenzhou Medical University, Wenzhou, Zhejiang, 325000, China

4 Department of Pathophysiology, School of Basic Medicine Science, Wenzhou Medical University, Wenzhou, Zhejiang, 325000, China

5 The Second School of Medicine, Wenzhou Medical University, Wenzhou, Zhejiang, 325000, China

6 Department of Infectious Disease, Shulan Hospital, Hangzhou, Zhejiang, 310012, China

7 Center for Diagnostics & Therapeutics, Institute for Biomedical Sciences, Georgia State University, Atlanta, GA 30302, USA

#These authors contribute equality to this work.

*corresponding author: Chang-Long Xu

Address: 109 College west road, Wenzhou, Zhejiang, 325000, China

Tel: +86-(0577)88002715; Fax: +86-(0577)88002715

E-mail: xchlong@163.com

Figure S1. The encapsulated efficiency of 17-AAG was quantified by HPLC using an Agilent® 1100 LC System (Agilent Technologies Inc., CA, USA). The detection wavelength was set at 254 nm.

Figure S2. The co-localization of NPs/DiL and HA-NPs/DiL with the endocytosis marker, Tf-FITC, in HT-29 cells were investigated. Cells cultured on slides were incubated with DiL-labeled HA-DOTAP/PLGA NPs for 4 h at 37°C, and then incubated with Tf-FITC for 15 min, after fixing with 4 % PFA, cells were examined under fluorescence microscopy. Yellow color (arrow) shows co-localization of HA-DOTAP/PLGA NPs/DiL and Tf-FITC. Scale bar: 10 m.

Figure S3. In vitro biocompatibility was evaluated using the MTT assays. A: HT-29 cells were incubated with DOTAP/PLGA and HA-DOTAP/PLGA NPs for 24 h, and viability was evaluated. B: HCT-116 cells were incubated with DOTAP/PLGA and HA-DOTAP/PLGA NPs for 24 h, and viability was evaluated. C: HT-29 cells were incubated with DOTAP/PLGA and HA-DOTAP/PLGA NPs for 48 h, and viability was evaluated. D: HCT-116 cells were incubated with DOTAP/PLGA and HA-DOTAP/PLGA NPs for 48 h, and viability was evaluated, (n=5).

Figure S4. In vitro biocompatibility of HA-DOTAP/PLGA NPs (HA-NPs) was also evaluated by colony formation assays.

Figure S5. The in vivo biocompatibility of HA-DOTAP/PLGA NPs (HA-NPs) was evaluated in mice by daily i.v. injection for 7 days. A. The spleen/body weight was compared at the end of the experiment (n=5). B. Pro-inflammatory cytokines (TNF-, IL-6 and IL-1β) levels in serum were compared. C. Representative H＆E-stained sections of heart, liver, spleen, lung, and kidney from the control and HA-NPs-treated mice were obtained.

Figure S6. Evaluation of apoptosis induced by HA-NPs/17-AAG in HCT-116 cells. (A)  Fluorescence imaging of HCT-116 cells treated with free 17-AAG or HA-NPs/17-AAG for 8 h and then co-stained with Annexin V-FTIC and PI. Scale bar: 10 m. (B) Flow cytometric analysis of apoptosis in HCT-116 cells treated with free 17-AAG or HA-NPs/17-AAG for 8 h. (C) Quantification of the Annexin V-FTIC/PI- cells from panel B, ***p<0.001 (n=5).

Figure S7. In vivo therapeutic efficacy of HA-NPs/17-AAG in Luc-HT-29 tumor-bearing mice. Xenograft tumors in each group were captured (n=5).

Figure S8. HA-NPs/17-AAG increases cell apoptosis in AOM/DSS-induced CAC. Apoptosis was quantified by TUNEL assay (green) and nuclei were stained with DAPI (blue), Scale bar: 20 µm.

Table S1. Safely evaluation of HA-DOTAP/PLGA nanoparticles (NPs) in vivo was evaluated by analyzing hematology and biochemistry parameters. (mean  S.D., n=5).

| Analytes | PBS group | NPs group |
| --- | --- | --- |
| WBC (109/L) | 7.66 1.96 | 6.97 0.45 |
| LYM (109/L) | 7.43 1.90 | 6.68 0.38 |
| MON (109/L) | 0.10 0.04 | 0.10 0.05 |
| NEU (109/L) | 0.14 0.07 | 0.13 0.07 |
| RBC (1012/L) | 9.31 0.35 | 9.87 0.23 |
| HGB (g/dL) | 14.07 0.32 | 14.90 0.36 |
| PLT (109/L) | 500.33 17.01 | 538.67 24.58 |
| ALT (U/L) | 35.67 3.51 | 38.00 1.73 |
| ALB (g/dL) | 3.47 0.12 | 3.60 0.26 |
| ALP (U/L) | 67.33 11.55 | 70.00 9.00 |
| AMY (U/L) | 1032.67 47.12 | 1140.67 96.13 |
| CA (mg/dL) | 10.60 0.44 | 10.47 0.45 |
| CRE (mg/dL) | 0.2 0.00 | 0.20 0.00 |
| GLOB (g/dL) | 2.03 0.06 | 2.10 0.20 |
| GLU (mg/dL) | 228.67 51.38 | 208.00 12.17 |
| PHOS (mg/dL) | 7.57 0.40 | 7.10 0.70 |
| K+ (mmol/L) | 7.97 0.23 | 7.73 0.35 |
| NA+ (mmol/L) | 156.67 3.06 | 154.33 0.58 |
| TBIL(mg/dL) | 0.30 0.00 | 0.33 0.06 |
| TP (g/dL) | 5.47 0.21 | 5.73 0.12 |
| BUN (mg/dL) | 22.33 2.08 | 22.33 1.53 |

Hematology parameters: WBC: Total white blood cell; LYM: Lymphocyte; MON: Monocyte; NEU: Neutrophil; RBC: Red blood cells; HGB: Hemoglobin; PLT: Platelet.

Biochemistry parameters: ALT: Alanine aminotransferase; ALB: Albumin; ALP: Alkaline phosphatase; AMY: Amylase; CA: Calcium; CRE: Creatinine; GLOB: Globulin; GLU: Glucose; PHOS: Phosphorus; TBIL: Total bilirubin; TP: Total protein; BUN: Urea nitrogen.