Supplementary materials

Magnetic fluid hyperthermia as treatment option for pancreatic cancer cells and pancreatic cancer organoids
Supplementary Figures

Supplementary Figure S1

Volume-weighted size distribution of ML dispersed in TES buffer solution obtained by DLS measurements using a Zetasizer Nano S (Malvern Instruments Ltd., Worcestershire, United Kingdom) at a wavelength of λ = 633 nm (detection angle of 173°) determined a mean hydrodynamic diameter of 100 ± 49 nm. For hydrodynamic diameter analysis fitting with the log-normal distribution probability density function (PDF): PDFd,μ,σ = 12πdσexp-lnd-μ2 2σ2 was employed. Here, d denotes the hydrodynamic diameter. The mean hydrodynamic diameter was calculated as dh = exp(μ+σ2/2) with the variance σdh2 = exp2μ+σ2expσ2-1 using the fitting parameters µ and σ.

Supplementary Figure S2

(A) TEM images of single ML cores dispersed in TES buffer solution using a Zeiss LEO 906 microscope (Carl Zeiss GmbH, Oberkochen, Germany) at a magnification of 100000.

(B) Core diameter distribution of magnetoliposomes depicted as a cumulative log-normal distribution probability density function CDFd,μ,σ = 12+1+erflnd-μ2σ for a number of n = 100 magnetoliposomes, where erf is the error function and d the core diameter of the magnetoliposomes. By fitting the parameters µ and σ were obtained allowing for mean core diameter calculation dcore = exp(μ+σ2/2) with the variance σdcore2 = exp2μ+σ2⋅expσ2-1 which was 11.1 ± 2.5 nm.

Supplementary Figure S3

(A) Analysis of magnetization properties of dispersed ML mixed with equal volume of 15%(w/w) mannitol solution in a polycarbonate (PC) capsule using a SQUID magnetometer MPMS 5S (LOT Quantum Design, San Diego, USA).

Determination of the saturation magnetization by fitting the Langevin function: L(ξ) = coth(ξ) -  1ξ where µ = VMMS denoted the particle magnetic moment, VM the mean magnetic volume (10.3 ± 2.9 nm), H the applied magnetic field and kB =  1.38·10- 23 J/K the Boltzmann constant revealed a saturation magnetization of 104 ± 1 Am2/kg(Fe).

(B) Peak temperature of the ZFC magnetization curve showed to be 266 ± 1 K.

Supplementary Figure S4

(A) Heating curves ΔT (Temperature increase with respect to a reference) of ML dispersed in TES buffer solution with different iron concentrations from 150 µg(Fe)/mL up to 900 µg(Fe)/mL. MFH measurements were performed using a custom-build hyperthermia setup (Trumpf Hüttinger GmbH + Co. KG, Freiburg, Germany). Dispersed ML of 1 mL were exposed to the AMF (270 kHz, 40 kA/m) for 30 min starting at an initial temperature of T0 = 37 °C.

(B) Corresponding SAR values of ML. SAR values were determined by fitting the Box-Lucas function: T(t) = ΔTmax(1-exp(-bt)) + T0. With fitting parameters (b, ΔTmax), c = 4.187 J(gK)-1 the specific heat capacity and ρ the iron mass fraction, the SAR values were calculated as: SLP = cρdTdt|t→0 = cρΔTmax b.