Double-Controlled Release of Poorly Water-Soluble Palliperidone Palmitate from Self-Assembled Albumin-Oleic Acid Nanoparticles in PLGA in situ Forming Implant

Yongjun Yua, Hai V. Ngoa, Gang Jina, Phuong H.L. Tranb, Thao T.D. Tranc,d, Van Hong Nguyene, Beom-Jin Leea,*

aCollege of Pharmacy, Ajou University, Suwon 16499, Republic of Korea

bDeakin University, School of Medicine, Geelong, Australia

cInstitute of Research and Development, Duy Tan University, Danang 550000, Vietnam

dThe Faculty of Pharmacy, Duy Tan University, Danang 550000, Vietnam

ePharmaceutical Engineering Laboratory, Biomedical Engineering Department, International University, Vietnam National University, Ho Chi Minh City 70000, Vietnam

Table S1

Stability profile of AONs after dispersion of AOC formulation (F2) in 2 mL NMP/water to the different volumes of PBS solution at room temperature for 2 weeks periods.

a) Particle size

| PBS solution | Initial (nm) | 1weeks (nm) | 2weeks (nm) |
| --- | --- | --- | --- |
| 5mL | 811.2 ± 43.1 | N.D | N.D |
| 10mL | 338.0 ± 9.9 | 350.7 ± 61.2 | 293.23 ± 1.27 |
| 20mL | 236.1 ± 1.0 | 411.8 ± 8.5 | 578.5 ± 24.22 |

N.D = Not detected, Mean ± SD (n=3)

b) Polydispersity index

| PBS solution | Initial | 1weeks | 2weeks |
| --- | --- | --- | --- |
| 5mL | 0.253 ± 0.016 | N.D | N.D |
| 10mL | 0.154 ± 0.042 | 0.26 ± 0.045 | 0.10 ± 0.005 |
| 20mL | 0.152 ± 0.034 | 0.22 ± 0.004 | - ± 0.011 |

N.D = Not detected, Mean ± SD (n=3)

c) Zeta potential

| PBS solution | Initial (mV) | 1weeks (mV) | 2weeks (mV) |
| --- | --- | --- | --- |
| 5mL | -17.14 ± 1.16 | N.D | N.D |
| 10mL | -10.37 ± 0.09 | -10.24 ± 1.02 | -12.47 ± 3.03 |
| 20mL | -14.97 ± 2.47 | -20.48 ± 1.01 | -16.75 ± 0.66 |

N.D = Not detected, Mean ± SD (n=3)