Supplement data

Table S1: Specifications and properties of contact lens materials used in the study

| Contact lens brand | Manufacturer | Oxygen transmissibility (-300) Dk/t x 10-9 barrer/cm | Material | Type | Main monomers | Water content (%) | FDA group | Surface treatment | Hydrophilicity/ Hydrophobicity | Ionicity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sof Eye 1 day | Vision Science, Korea | 30 | Polymacon | Hydrogel | HEMA | 42 | I | None | hydrophilic | non-ionic |
| Biomedics 1 day plus | CooperVision, USA | 19.6 | Ocufilcon D | Hydrogel | HEMA, NVP, MA | 55 | IV | None | hydrophilic | ionic |
| Maxim soft 1 day | Sauflon Pharmaceutical, UK | 86 | Somofilcon A (Filcon II 3) | Silicone hydrogel | co-polymer of silicone containing TEGDMA | 56 | II | None | hydrophilic | non-ionic |
| Biotrue 1 day | Bausch & Lomb, USA | 42 | Nesofilcon A | Hydrogel (Hypergel) | HEMA, NVP | 78 | II | None | hydrophilic | non-ionic |
| Sweety Plus | Dueba, Korea | 8.4 | Polymacon | Hydrogel | HEMA | 38 | I | Color printed | hydrophilic | non-ionic |

Abbreviations: HEMA, 2-hydroxyethyl methacrylate; MA, methacrylic acid; NVP, N-vinyl pyrrolidone; TEGDMA, tetraethylene glycol dimethacrylate

Table S2:  Contents and directions of multi-purpose disinfecting solution for CL care

| Disinfecting solution | Contents | Manufacturer's Instructions |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Drop | Rub (sec) | Rinse (sec) | Soakage (h) |
| Renu freshTM (MPS) | HYDRANATE® (hydroxyalkylphosphonate), boric acid, edetate disodium, poloxamine, sodium borate and sodium chloride; preserved with DYMED® (polyaminopropyl biguanide) 0.0001%. | 3 | 20 (rub) | 5 | ≥ 4 |
|  |  |  | - (no rub)* |  |  |
| Bausch & Lomb® Sensitive Eyes Daily Cleaner (MPDS+EDSA) | Hydroxypropyl methylcellulose, poloxamine, sodium borate and sodium chloride; preserved with edetate disodium (0.5%) and sorbic acid (0.25%) | 3 | 20 | 10 | N/A |
| Opti Free Aldox (MPDS+PoA) | Sodium citrate, sodium chloride, boric acid, sorbitol, aminomethylpropanol, TETRONIC® 1304†, with edetate disodium 0.05%, preserved with POLYQUAD (polyquaternium-1) 0.001% and ALDOX (myristamidopropyl dimethylamine) 0.0005% | Thoroughly wet | 20 (rub) | 10 | ≥ 6 |
|  |  |  | - (no rub)* |  |  |

*; the manufacturer provided the alternative no-rub regimen.

Determination of minimum inhibitory concentration (MIC) and minimum bactericidal concentration (MBC)

Multipurpose solution (MPS), MPDS+PoA, and MPDS+EDSA were used as antimicrobial agents in this study. Antibacterial activity was measured by broth microdilution method according to the Clinical & Laboratory Standards Institute (CLSI) guidelines (2018). In 96-well microtiter plate, 20 µL of the agents were separately added and diluted by the two-fold serial dilution from their original concentration. The total volume was made up to 100 µL by adding 80 µl of Mueller-Hinton broth in each well. 100 µl of bacterial suspension (106 CFU/mL) were inoculated in the broth containing the extract and incubated at 37°C for 18 h. saline solution (NSS, 0.9% sodium chloride: NaCl) was included for negative control.

Minimum bactericidal concentration (MBC) was determined subsequently to the MIC assay. A 100 µL of aliquot from the wells with MIC value was seeded in TSA plate and incubated at 37°C for 18 h. The plates were observed for an appearance of bacterial growth and determination of MBC value. The experiment was carried out in triplicate.

Results of MICs and MBCs

The MIC and MBC values of CL care solutions were expressed in the term of fold-reduction of its original concentration (Table S3). The MPS, MPDS+PoA and MPDS+EDSA were tested against bacterial growth. The MPDS+PoA demonstrated antibacterial activity against staphylococcal strains with MIC and MBC values ranged from 0.0312-0.0625 and 0.0625-0.125-fold of the original concentration, respectively. Gram-negative bacterial strains were inhibited by the disinfecting solution with the MIC and MBC values ranged of 0.125-0.256 and 0.256-0.5-fold of the original concentration, respectively. The MIC values of MPS and MPDS+EDSA against all tested isolates ware ranging from 0.0625-0.5 and 0.0312-0.256-fold of the original concentration, respectively. The MPS and MPDS+EDSA possessed bactericidal activity with the MBC values ranged from 0.125-0.5 and 0.0625-0.5-fold of the original concentration, respectively.

Table S3: MICs and MBCs (fold of original concentration) of CL care solutions against pathogenic bacterial strains

| Bacterial strains | MIC/MBC values of CL care solutions (fold of original concentration) |  |  |
| --- | --- | --- | --- |
|  | MPS | MPDS+PoA | MPDS+EDSA |
| S. aureus ATCC 29213 | 0.125/0.256 | 0.0625/0.0625 | 0.125/0.256 |
| S. aureus ATCC 25923 | 0.256/0.5 | 0.0625/0.125 | 0.256/0.256 |
| S. epidermidis ATCC 35984 | 0.0625/0.125 | 0.0312/0.0625 | 0.0312/0.0625 |
| E. coli ATCC 25922 | 0.256/0.5 | 0.125/0.256 | 0.256/0.5 |
| K. pneumoniae ATCC 700603 | 0.125/0.256 | 0.125/0.256 | 0.125/0.256 |
| P. aeruginosa ATCC 27853 | 0.5/0.5 | 0.256/0.5 | 0.125/0.256 |