Supplementary Material

This file includes:

- Standard curve of TCPP and Iso (Figure S1)

- UV-Vis spectrum and (b) FT-IR spectrum of combined NPs (Figure S2)

- Particle size (Rh) and size distribution (PDI) of nanoparticle at 10th day and 14th day (Table S1)

- Temperature evolution of TCPP-NPs (Figure S3)

Figure S1

Figure S1. (a) Standard curve of TCPP; (b) standard curve of Iso.

Figure S2

Figure S2. (a) UV-Vis spectrum and (b) FT-IR spectrum of combined NPs.

Table S1. Average Rh (hydrodynamic radius) and PDI of NPs at 10th day and 14th day

|  | NPs at 10th day |  | NPs at 14th day |  |
| --- | --- | --- | --- | --- |
|  | Rh nm | PDI | Rh nm | PDI |
| NP | 92.02 | 0.24 | 91.83 | 0.24 |

Figure S3

Figure S3. (a) Temperature evolution of TCPP-NPs solution under 650 nm laser irradiation (6.5 W·cm-2) at different TCPP concentrations; (b) Temperature evolution of TCPP-NPs solution with 3 cycles of laser on/off under 650 nm laser irradiation (6.5 W·cm-2) at different TCPP concentrations.