Supporting Information

for

Nano hydroxyapatite and nano silicate-reinforced injectable and biomimetic gelatin-methacryloyl hydrogel for bone tissue engineering

Zhe Shi1#, Qiang Zhong1#, Yuhang Chen1, Jian Gao1, Xin Pan1, Qiang Lian1, Rong Chen1, Pinkai Wang1, Jian Wang1, Zhanjun Shi1*, Hao Cheng1*

1 Department of Orthopedics, Nanfang Hospital, Southern Medical University, 1838 # Guangzhou North Avenue, Guangzhou, Guangdong Province, 510515, P. R. China

† These authors contributed equally to this work.

* Correspondence:

Professor Zhanjun Shi, Email: shizhanjun111@gmail.com

Dr. Hao Cheng, Email:haocool317@gmail.com

Figure S1. (a) Fabricated GelMA foam; (b-e) GelMA-HAP-SN hydrogel (uncrosslinked) injectability demonstrated using a 10mL syringe with various sizes of needles at room temperature.

Figure S2. Pore size of the GelMA-based hydrogels. *P<0.05.

Figure S3. (a) Compress modulus of the HAP-loaded GelMA with various HAP concentration with a 30-S UV radiation; (b) Compress modulus of the SN-loaded GelMA with various SN concentration with a 30-S UV radiation; (c) UV radiation time needed for the GelMA-based hydrogel to achieve preset compress modulus (~ 25 Kpa). *P<0.05.

Figure S4. Pore size of hydrogels in lyophilized and non-lyophilized status. *P<0.05.

| Gene | Forward primer sequence | Reverse primer sequence |
| --- | --- | --- |
| ALP | CAGCGGGTAGGAAGCAGTTT | CCCCTGCACCTCATCCCTGA |
| RUNX2 | CCATAACGGTCTTCACAAATCCT | TCTGTCTGTGCCTTCTTGGTTC |
| OCN | GGTGCAGACCTAGCAGACACCA | AGGTAGCGCCGGAGTCTATTCA |
| OPN | TTCCAAGTAAGTCCAACGAAAG | GTGACCAGTTCATCAGATTCAT |

Table S1. Primers used for qRT–PCR

| SN-loaded hydrogel | power law index (n) | consistency index (k) | correlation efficient |
| --- | --- | --- | --- |
| 1% GelMA-SN | 0.25 ± 0.02 | 24 ± 2.89 | 0.992 |
| 2% GelMA-SN | 0.22 ± 0.03 | 57 ± 4.33 | 0.990 |

Table S2. The power law index (n), consistency index (k) and the correlation coefficient (Corr. Coeff) values of 1% GelMA-SN and 2% GelMA-SN.