Supplementary Materials

Multifarious biological applications and toxic Hg2+ sensing potentiality of biogenic silver nanoparticles based on securidaca inappendiculata Hassk stem extract

Figure S1 Base peak chromatogram of elute from S. inappendiculata stem bark extract analysed in negative electrospray ionization mode.

Table S1 Putative identities of chemical components present in S. inappendiculata stem bark extract obtained by LC-ESI-QTOF analysis

| S/N | Rt (min) | m/z | Accurate mass (Da) | Mass Diff (ppm) | Calculated mass (Da) | Predicted Formula | Score (DB) | Tentative identity of compound |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 6.201 | 537.1846 | 478.1707 | -4.34 | 478.1686 | C20 H30 O13 | 90.29 | Kelampayoside A |
| 2 | 6.452 | 259.0829 | 260.0902 | -2.36 | 260.0896 | C11 H16 O7 | 97.99 | 3-Furanmethanol glucoside |
| 3 | 6.602 | 517.1564 | 472.1583 | -0.53 | 472.1581 | C21 H28 O12 | 98.74 | 1-O-Cinnamoyl-beta-D-gentiobiose |
| 4 | 6.866 | 585.2195 | 540.2211 | -0.79 | 540.2207 | C26 H36 O12 | 98.59 | Sambacin |
| 5 | 6.929 | 313.0933 | 314.1005 | -1.1 | 314.1002 | C14 H18 O8 | 98.82 | 2-O-Acetylarbutin |
| 6 | 7.255 | 783.235 | 784.2425 | 0.06 | 784.2426 | C35 H44 O20 | 99.12 | Rhamnazin 3-isorhamninoside |
| 7 | 7.707 | 567.2088 | 568.2146 | 1.67 | 568.2156 | C27 H36 O13 | 80.55 | Citrusin B |
| 8 | 7.732 | 339.1092 | 340.1164 | -1.71 | 340.1158 | C16 H20 O8 | 82.99 | Oenanthoside A |
| 9 | 7.908 | 435.0951 | 436.1023 | -3.96 | 436.1006 | C20 H20 O11 | 92.66 | Irisxanthone |
| 10 | 7.958 | 741.2637 | 742.2708 | -3.25 | 742.2684 | C34 H46 O18 | 92.74 | Acanthoside D |
| 11 | 8.071 | 569.1878 | 570.1951 | -0.35 | 570.1949 | C26 H34 O14 | 99.59 | 2''-Methoxy-(S)-oleuropein |
| 12 | 8.234 | 683.2228 | 684.2302 | 2.49 | 684.2319 | C37 H36 N2O11 | 87 | Citbismine C |
| 13 | 8.31 | 723.2172 | 724.2238 | -3.26 | 724.2215 | C33 H40 O18 | 90.24 | Natsudaidain 3-(4-O-3-hydroxy-3-methylglutaroylglucoside) |
| 14 | 8.46 | 693.2044 | 694.2114 | -0.67 | 694.2109 | C32 H38 O17 | 98.76 | Neocuscutoside C |
| 15 | 8.535 | 593.1506 | 594.1588 | -0.5 | 594.1585 | C27 H30 O15 | 82.94 | Vitexin 4'-O-galactoside |
| 16 | 8.711 | 621.1831 | 622.1905 | -1.23 | 622.1898 | C29 H34 O15 | 98.28 | Pectolinarin |
| 17 | 8.837 | 697.2365 | 652.2384 | -2.54 | 652.2367 | C31 H40 O15 | 95.71 | (-)-Matairesinol 4'-[apiosyl-(1->2)-glucoside] |
| 18 | 8.937 | 521.1318 | 522.1391 | -3.31 | 522.1373 | C24 H26 O13 | 93.86 | Centaurein |
| 19 | 8.987 | 597.1828 | 598.1908 | -1.73 | 598.1898 | C27 H34 O15 | 84.78 | 10-Acetoxyoleuropein |
| 20 | 9.389 | 355.1046 | 356.1118 | -3.05 | 356.1107 | C16 H20 O9 | 95.27 | 1-O-2'-Hydroxy-4'-methoxycinnamoyl-b-D-glucose |
| 21 | 9.59 | 411.1304 | 412.1375 | -1.39 | 412.1369 | C19 H24 O10 | 98.58 | Methylpicraquassioside A |
| 22 | 9.716 | 547.1455 | 548.1529 | 0.21 | 548.153 | C26 H28 O13 | 98.88 | Mirificin |
| 23 | 9.929 | 365.0881 | 366.0954 | -0.82 | 366.0951 | C17 H18 O9 | 99.39 | Furocoumarinic acid glucoside |
| 24 | 10.64 | 303.0502 | 304.0574 | 2.95 | 304.0583 | C15 H12 O7 | 95.61 | Pratenol B |
| 25 | 10.77 | 329.234 | 330.2412 | -1.73 | 330.2406 | C18 H34 O5 | 98.67 | 11,12,13-trihydroxy-9-octadecenoic acid |
| 27 | 11.12 | 303.0512 | 304.0584 | -0.38 | 304.0583 | C15 H12 O7 | 99.62 | Alphitonin |
| 28 | 11.6 | 287.0569 | 288.0642 | -2.73 | 288.0634 | C15 H12 O6 | 96.81 | Eriodictyol |
| 29 | 12.28 | 307.1911 | 308.1987 | 0.19 | 308.1988 | C18 H28 O4 | 91.32 | 5-O-Methylembelin |
| 30 | 12.38 | 227.035 | 228.0423 | -0.32 | 228.0423 | C13 H8 O4 | 99.21 | Euxanthone |
| 31 | 13.16 | 293.1763 | 294.1836 | -1.52 | 294.1831 | C17 H26 O4 | 98.79 | Embelin |
| 32 | 17.7 | 563.3443 | 518.3459 | -0.84 | 518.3455 | C27 H50 O9 | 97.29 | 3-O-L-rhamnosyl-3-hydroxydecanoyl-3-hydroxydecanoic acid |

Rt: retention time

a

b

c

b

a

c

Figure S2 UV-vis absorption spectra of (a) AgNO3 salt (b) AgNO3 and NaOH mixture (c) SISE, AgNO3 and NaOH mixture

Figure S3 UV-Vis absorption spectra of SISE AgNPs synthesis at optimal conditions

Figure S4 Plot of Absorbance at 423 nm of SISE AgNPs vs synthesis time (min)

Figure S5 Histogram showing the distribution of particles sizes of SISE AgNPs acquired on an Image J software

Figure S6 EDS spectrum of as-synthesized SISE AgNPs

Figure S7 Elemental mapping of SISE AgNPs showing, the presence of Ag, C and O

A

B

Fig.S6: A. Thermogravimetric analysis plot and B. Differential thermogravimetric plot of SISE

Figure S8 (A) Thermogravimetric analysis plot and (B) Differential thermogravimetric plot of SISE AgNPs

Table S2: TGA data of SISE AgNPs

| Sample | Stages | Onset Temperature (C) | Temperature ranges (C) | IDT (C) | IPDT (C) | Mass loss (%) | Ash (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SISE AgNPs | I | 41.75 | 41.75-169.81 | 41.75 | 1010.00 | Y = 0.71 | 59.5 |
|  | II | 169.71 | 169.71-662.22 |  |  | Y = 13.06+18.95 |  |
|  | III | 662.22 | 662.22-1010.00 |  |  | Y = 4.93+2.85 |  |
|  |  |  |  |  |  | Total = 40.50 |  |

IDT = Initial decomposition temperature; IPDT = Integral procedural decomposition temperature.

Blank                             Hg2+

A

B

Figure S9 (A)  UV-Vis absorption spectra of SISE AgNPs in the presence of metal ions; Blank, K+, Fe3+, Ca2+, Fe2+, Co2+, Cd2+, Cu2+, Ni2+, Mg2+, Pb2+, Zn2+, Ba2+, Al3+, Hg2+, inset shows the photo images of the corresponding plots, and (B) Plot of A385/A423 vs metal ions, Concentration of Hg2+ =20.0 μM, while other metal ions were 50.0 μM.

Table S3: Comparison of SISE AgNPs probe with reported methods for Hg2+ detection.

| Detection probe | LOD (nM) | Linear range (µM) | References |
| --- | --- | --- | --- |
| Electrochemical (DPV) | 0.009 | 0.001 – 0.5 | [1] |
| Colorimetry (β-CD-AgNPs) | 37.5 | 0.2 – 2.6 | [2] |
| Colorimetry (AuNPs) | 0.275 | 0.1 – 0.5 | [3] |
| Colorimetry (CMC-AgNPs) | 5.0 | 0.0025 – 0.25 | [4] |
| Colorimetry (SA-AgNPs) | 5.29 | 0.025 – 60.0 | [5] |
| Colorimetry (AuNPs-MBT) | 6.0 | 0.05 – 1.0 | [6] |
| Colorimetry (Chlorophyll-AgNPs) | 2700 | 0.10 - 200 | [7] |
| Fluorescence | 33.0 | 0.05 – 5.8 | [8] |
| Fluorescence | 14.0 | 0.0 – 100.0 | [9] |
| SISE AgNPs | 26.5 | 0.10 – 10.0 | This work |

DPV = Differential pulse voltammetry; β-CD = Beta cyclodextrin; CMC = Carboxymethyl cellulose; SA= Sodium alginate.

References

1. Mahmoudian MR, Basirun WJ, Alias Y, et al. Investigating the effectiveness of g-C3N4 on Pt/g-C3N4/polythiophene nanocomposites performance as an electrochemical sensor for Hg2+ detection. J Environ Chem Eng. 2020;8(5):104204. Doi:10.1016/j.jece.2020.104204

2. Rajamanikandan R, Ilanchelian M. β-cyclodextrin functionalised silver nanoparticles as a duel colorimetric probe for ultrasensitive detection of Hg2+ and S2− ions in environmental water samples. Mater Today Commun. 2018;15:61-69. Doi:10.1016/j.mtcomm.2018.02.024

3. Amanulla B, Perumal KN, Ramaraj SK. Chitosan functionalized gold nanoparticles assembled on sulphur doped graphitic carbon nitride as a new platform for colorimetric detection of trace Hg2+. Sens Actuators B: Chem. 2019;281:281-287. Doi:10.1016/j.snb.2018.10.039

4. Sakly N, Marzouk W, Ouada HB, et al. Enhancing performances of colorimetric response of carboxymethylcellulose-stabilized silver nanoparticles: a fully eco-friendly assay for Hg2+ detection. Sens Actuators B: Chem. 2017;253:918-927. Doi:10.1016/j.snb.2017.07.035

5. Faghiri F, Ghorbani F. Colorimetric and naked eye detection of trace Hg2+ ions in the environmental water samples based on plasmonic response of sodium alginate impregnated by silver nanoparticles. J Hazard Mater. 2019;374:329-340. Doi:10.1016/j.jhazmat.2019.04.052

6. Jin W, Huang P, Wei G, et al. Visualization and quantification of Hg2+ based on anti-aggregation of label-free gold nanoparticles in the presence of 2-mercaptobenzothiazole. Sens Actuators B: Chem. 233 (2016) 223-229. Doi:10.1016/j.snb.2016.04.071

7. Yılmaz DD, Demirezen DA, Mıhçıokur H. Colorimetric detection of mercury ion using chlorophyll functionalized green silver nanoparticles in aqueous medium. Surf Interfaces. 2021;22:100840. Doi:10.1016/j.surfin.2020.100840

8. Wang S, Chen H, Xie H, et al. A novel thioctic acid-carbon dots fluorescence sensor for the detection of Hg2+ and thiophanate methyl via S-Hg affinity. Food Chem. 2021;346:128923. Doi:10.1016/j.foodchem.2020.128923

9. Wang P, Yan Y, Zhang Y, et al. An Improved Synthesis of Water-Soluble Dual Fluorescence Emission Carbon Dots from Holly Leaves for Accurate Detection of Mercury Ions in Living Cells. Int J Nanomed. 2021;16:2045. Doi: 10.2147/IJN.S298152