Supplementary materials

Figure S1. Synthetic scheme for preparation of DSPE-PEG-Folate. Reagents and conditions.

Figure S2. The mass spectra of DSPE-PEG2000-Folate.

Figure S3. Infrared spectra of Fe3O4 Magnetic nanoparticles (MNPs).

Figure S4. Magnetic hysteresis loop of the MNPs measured at room temperature.

Figure S5. Capture efficiencies of MNPs at different attraction times with a commercial magnetic scaffold.

Figure S6. XRD patterns of GNRs obtained by using seed mediated growth method.

Note: Data from Nikoobakht and El-Sayed1 was used for comparison.

Figure S7. Schematic diagram of chip structure.

Figure S8. Size distribution of FA-TMLs, FA-TMLs@MNPs-GNRs, and FA-TMLs@MNPs-GNRs-DOX.

Table S1. Particle size distribution of liposomes (n=3)

| Liposome | Size (nm) | PDI |
| --- | --- | --- |
| FA-TMLs | 95 ± 4 | 0.02 |
| FA-TMLs@MNPs-GNRs | 210 ± 5 | 0.14 |
| FA-TMLs@MNPs-GNRs-DOX | 234 ± 5 | 0.11 |

Figure S9. The effects of GNRs concentration on encapsulation efficiency and loading efficiency of DOX in FA-TMLs@MNPs-GNRs-DOX.

Figure S10. The Cytotoxicity of DOX with various concentrations towards bladder cancer cells.

Figure S11. Standard curve of DOX.

Figure S12. Hemolytic activity of FA-TMLs@MNPs-GNRs.

Reference:

1. Nikoobakht, B.; El-Sayed, M. A. Preparation and Growth Mechanism of Gold Nanorods (NRs) Using Seed-Mediated Growth Method. Chem. Mater. 2003, 15, 1957-1962.