Supporting Information

Antitumor activity of α-linolenic acid-paclitaxel conjugate nanoparticles: in vitro and in vivo

Mei-Qi Xu1,2, Yan-Li Hao1,2, Jing-Ru Wang1,2, Zhuo-Yue Li1,2, Hui Li1, Zhen-Han Feng1,2, Hui Wang1,2, Jing-Wen Wang1,2, Xuan Zhang 1,2 *

1 Beijing Key Laboratory of Molecular Pharmaceutics and New Drug Delivery Systems, School of Pharmaceutical Sciences, Peking University, Beijing 100191, China; 2 Department of Pharmaceutics, School of Pharmaceutical Sciences, Peking University, Beijing 100191, China

Correspondence: Dr. Xuan Zhang Professor

Department of Pharmaceutics, School of Pharmaceutical Sciences, Peking University, Xueyuan Road 38, Beijing 100191, China

Tel: +86-10-82805765

Fax: +86-10-8280576

Email: xuanzhang@bjmu.edu.cn

Table S1 HPLC gradient elution condition for ALA-PTX.

| Time (min) | Mobile phase A (%) | Mobile phase B (%) |
| --- | --- | --- |
| 0→10 | 60 | 40 |
| 10→12 | 60→100 | 40→0 |
| 12→28 | 100 | 0 |
| 28→30 | 100→60 | 0→40 |
| 30→40 | 60 | 40 |

Table S2 Concentrations of the endocytosis inhibitors.

| Inhibitors | Function | Concentration |
| --- | --- | --- |
| EIPA | Inhibitor of macropinocytosis | 20 μM |
| CPZ | Inhibitor of clathrin | 30 μM |
| Filipin | Inhibitor of lipid raft | 0.5 μg/mL |
| Hypertonic sucrose | Inhibitor of clathrin | 0.4 M |

Figure S1  Particle size (a) and zeta potential (b) of DiO&DiI-ALA-PTX NPs.