Supplementary Methods

Title: Emodin-conjugated PEGylation of Fe3O4 Nanoparticles for FI/MRI dual-modal imaging and therapy in pancreatic cancer

Shuai Ren*, Lina Song, Ying Tian, Li Zhu, Kai Guo, Huifeng Zhang, Zhongqiu Wang*

Department of Radiology, Jiangsu Province Hospital of Chinese Medicine, Affiliated Hospital of Nanjing University of Chinese Medicine, Nanjing, Jiangsu Province, China 210029

S1.1. Calculate the number of Fe3O4-PEG-Cy7-EMO nanoparticles and the surface area of Fe3O4-PEG-Cy7-EMO nanoparticles

The number of Fe3O4-PEG-Cy7-EMO nanoparticles was measured and calculated as follows:

m1 = 4 3π (D2)3Fe3O4

mFe3O4= m2 × MFe3O43 × MFe

NFe3O4= mFe3O4m1

The surface area of Fe3O4-PEG-Cy7-EMO nanoparticle was measured and calculated as follows:

S1 = πD2

SFe3O4 = S1×NFe3O4

Where 𝑚1 represents the weight of one Fe3O4 nanoparticle, Fe3O4is the density of the Fe3O4. mFe3O4and m2 represent the total weight of Fe3O4 nanoparticles and Fe in 1 mL solution; S1 represents the superficial area of one Fe3O4 nanoparticle, SFe3O4  represents the total superficial area of Fe3O4 nanoparticle in 1 mL solution.

S1.2. Calculate the conjugation efficacy of EMO to Fe3O4-PEG-Cy7-EMO nanoparticles

The conjugation efficacy of EMO to Fe3O4-PEG-Cy7-EMO nanoparticles was measured and calculated as follows:

nEMO = mEMOMEMO×NA

NEMO = nEMOSFe3O4

nEMO represents the total amount of EMO in 1 mL solution, NEMO represents the conjugation efficacy of EMO to Fe3O4-PEG-Cy7-EMO nanoparticle.

Supplementary Results

S2.1. Calculation of Fe3O4-PEG-Cy7-EMO nanoparticles number and the surface area of Fe3O4-PEG-Cy7-EMO nanoparticles

The number of Fe3O4-PEG-Cy7-EMO nanoparticles was measured and calculated as follows:

m1 = 4 3π (D2)3Fe3O4= 4 3π × (4.95 × 10-7cm)3 × 5.18g/cm3 = 2.63× 10-18g

mFe3O4= m2 × MFe3O43 × MFe  = 1mg ×232g/mol56g/mol = 1.38mg

NFe3O4= mFe3O4m1 = m2 × MFe3O43 × MFe × 4 3π(D2)3Fe3O4 = 1.38mg2.63 × 10-15mg = 0.52 × 1015

The surface area of Fe3O4-PEG-Cy7-EMO nanoparticle was measured and calculated as follows:

S1 = πD2 = π×(9.9nm)2=307.75nm2

SFe3O4 = S1×NFe3O4= 307.75nm2× 0.52 × 1015 = 1.6×1017nm2

Where 𝑚1 represents the weight of one Fe3O4 nanoparticle, Fe3O4is the density of the Fe3O4. mFe3O4and m2 represent the total weight of Fe3O4 nanoparticles and Fe in 1 mL solution; S1 represents the superficial area of one Fe3O4 nanoparticle, SFe3O4  represents the total superficial area of Fe3O4 nanoparticle in 1 mL solution.

S2.2. Calculation of the conjugation efficacy of EMO to Fe3O4-PEG-Cy7-EMO nanoparticles

The conjugation efficacy of EMO to Fe3O4-PEG-Cy7-EMO nanoparticles was measured and calculated as follows:

nEMO = mEMOMEMO×NA= 120×10-3gml × 1ml270g/mol × 6.02 ×1023 = 2.68 × 1020

NEMO = nEMOSFe3O4=2.68 × 10201.6 ×1017nm2= 1675/nm2

nEMO represents the total amount of EMO in 1 mL solution, NEMO represents the conjugation efficacy of EMO to Fe3O4-PEG-Cy7-EMO nanoparticle.

Supplementary Table 1

The hemolysis experiments in vitro

| Tube No. | 1 | 2 | 3 | 4 | 5 |
| --- | --- | --- | --- | --- | --- |
| 2% RBC suspension (mL) | 2.5 | 2.5 | 2.5 | 2.5 | 2.5 |
| sterile saline (mL) | 2.45 | 2.45 | 2.4 | 2.5 | / |
| distilled water | / | / | / | / | 2.5 |
| reagent (mL, 1mg/mL) | 0.05 | 0.05 | 0.1 | / | / |
| 15 min | - | - | - | - | + |
| 30 min | - | - | - | - | + |
| 45 min | - | - | - | - | + |
| 1 h | - | - | - | - | + |
| 2 h | - | - | - | - | + |
| 4 h | - | - | - | - | + |

Notes: RBC, red blood cells.