Supporting Information

Hybrid membrane nanovaccines combined with immune checkpoint blockade to enhance cancer immunotherapy

Peiqi Zhao1#*, Yuanlin Xu2#, Wei Ji3, Lanfang Li1, Lihua Qiu1, Shiyong Zhou1, Zhengzi Qian1, Huilai Zhang1*

1 Department of Lymphoma, Tianjin’s Clinical Research Center for Cancer, Key Laboratory of Cancer Prevention and Therapy, National Clinical Research Center for Cancer, Tianjin Medical University Cancer Institute and Hospital, Tianjin Medical University, Tianjin, 300060, China.

2 Department of Lymphatic Comprehensive Internal Medicine, Affiliated Cancer Hospital of Zhengzhou University, Zhengzhou, 450001, Henan, China.

3 Public Laboratory, Tianjin’s Clinical Research Center for Cancer, Key Laboratory of Cancer Prevention and Therapy, National Clinical Research Center for Cancer, Tianjin Medical University Cancer Institute and Hospital, Tianjin Medical University, Tianjin, 300060, China.

#Peiqi Zhao and Yuanlin Xu contributed equally to this work.

Corresponding author: Email: peiqizhao@126.com; zhanghltch@163.com

Materials and Methods

Preparation of hybrid cell membrane. Hybrid cell membrane was firstly prepared using a previous method [1]. The collected cells were first washed with cooled phosphate buffered saline (PBS) for twice, resuspended in a hypotonic lysis buffer containing membrane protein extraction reagent and then incubated in an ice-bath for 10 min. The cells in the above solution were broken using a repeated freeze-thaw method for three times and further centrifuged (1000 g, 10 min) at 4 °C. To collect cell membrane debris, the supernatant was further centrifuged (14,000 g, 30 min). The hybrid cell membrane is lyophilized and stored at -80°C. The lyophilized membrane materials are rehydrated in ultrapure water prior to use.

Synthesis of R837@MSN. Mesoporous silica nanoparticle (MSN) was synthesized according to the reference [2]. R837@MSN was manufactured as previously reported. Briefly, 50 mg MSN (10 mg/mL) was dissolved in dimethyl formamide with 200 μg of R837 (1 mg/mL) and then 1 mL of polyvinylpyrrolidone (PVP) solution (5% w/v) was added into the MSN mixture followed by sonication. After that, 2 mL of PVP solution was added dropwise into the resulting solution and stirred at room temperature for 24 h. The obtained crude product was centrifuged, washed thoroughly with water until the upper liquid is colorless, and dried under vacuum.

Physicochemical characterization. The particle size and zeta potential of R837@HM-NPs was tested with Zetasizer Nano ZP (Malvern Instruments Ltd., UK). The encapsulation efficiency (EE) and loading efficiency (LE) of R837@HM-NPs was determined using reverse phase high performance liquid chromatography (RP-HPLC). To evaluate the release behavior of R837 in vitro, 3 mg of R837@MSN and R837@HM-NPs powder were dissolved with 1 mL of PBS (pH5.0 or pH7.4) and placed in a dialysis bag which was immersed in 10 ml PBS at 37℃, and the R837 concentration in dialysate was measured at regular intervals. The percentage of the R837 entrapped in the R837@MSN and R837@HM-NPs was calculated as follows:

LE (%) = (amount of the drug in particles / amount of the feeding material and drug) ×100%

EE (%) = (amount of the drug in particles / amount of the feeding drug) ×100%

Western blotting. Marker proteins from hybrid cell lysate and hybrid cell membrane were first extracted and protein concentrations were determined by applying the BCA protein concentration assay kit (Beyotime, China). The proteins were separated by sodium dodecyl sulfate polyacrylamide gel electrophoresis and then transferred to polyvinylidene fluoride membranes. The membranes were blocked with 5% fat-free milk and then incubated with primary antibody and horseradish peroxidase-labeled secondary antibody at appropriate ratios. Specific proteins (Lamin B1, Calnexin, HSP 60, Pan Cadherin, GAPDH and Na+/K+-ATPase) were detected by an enhanced chemiluminescence detection assay (Santa Cruz Biotechnology, Inc.).

In vitro biocompatibility studies. BMDCs and 4T1 cells at a concentration of 1×105 cells/mL were co-incubated with the MSN and HM-NPs at different concentrations for 48 h. The cytotoxicity of the MSN and HM-NPs was assayed by a MTT method according to the manufacturer’s protocol.

Reference

1.	Liu WL, Zou MZ, Liu T, Zeng JY, Li X, Yu WY, et al. Cytomembrane nanovaccines show therapeutic effects by mimicking tumor cells and antigen presenting cells. Nat Commun. 2019;10(1):3199. doi: 10.1038/s41467-019-11157-1.

2.	Zhao P, Qiu L, Zhou S, Li L, Qian Z, Zhang H. Cancer Cell Membrane Camouflaged Mesoporous Silica Nanoparticles Combined with Immune Checkpoint Blockade for Regulating Tumor Microenvironment and Enhancing Antitumor Therapy. Int J Nanomedicine. 2021;16:2107-21. doi: 10.2147/IJN.S295565.

Figure S1. Western blotting analysis of marker proteins from hybrid cell lysate (A) and hybrid cell membrane (B).

Figure S2. Particle diameter distribution of R837@HM-NPs in RPMI 1640 medium containing 10% FBS at different time points.

Figure S3. Cell viability of 4T1 cells incubated with PBS, MSN and HM-NPs at different concentrations measured at 48 h.

Figure S4. Representative data of CD3+CD8+T cells after in vitro incubation of T cells with PBS, R837, R837@MSN, HM-NPs, or R837@HM-NPs for 24 h. *P < 0.05, **P < 0.01.

Figure S5. In vitro cytotoxicity of the T lymphocytes activated by hybrid membrane nanovaccine-treated DCs to HBL-100, 4T1, and B16F10 cells. *P < 0.05, **P < 0.01.

Figure S6. Representative statistical data to show BMDCs maturation in lymph nodes induced by different treatments in vivo. *P < 0.05, **P < 0.01.

Figure S7. Representative data of CD3+CD8+T cells in tumors after different treatments. *P < 0.05, **P < 0.01.

Figure S8. Tumor growth inhibition ratios of R837@HM-NPs in combination with αPD-1 against tumors on the 24th day of treatment. *P < 0.05, **P < 0.01.

Figure S9. Tumor growth curves of individual mice in different groups of the 4T1 tumor-bearing BALB/c mice model (right flank tumor).