Table S1. Basic chemical and biological information of CPD 23

| Contents | CPD 23a |
| --- | --- |
| Name | 2-(5-Methoxy-1-methyl-1H-indol-3-yl)-N-(5-(4-(6-(2-(3-(trifluoromethoxy)phenyl)acetamido)pyridazin-3-yl)butyl)-1,3,4-selenadiazol-2-yl)acetamide |
| Molecular weight | 701.15 |
| Appearance | Reddish brown powder, loose texture |
| Solubility (25 ± 2 ℃) | 0.31 μg/mL (water) 50 mg/mL (DMSO) |
| CLogP b | 4.58 (ALOGPS2.1) 4.77 (ChemBioDraw14.0) |
| Enzymatic activity (IC50) | 0.01 μM (kidney-type glutaminase) ＞13 μM (glutaminase dehydrogenase) |
| Cell inhibition (IC50) | 4.05 μM (H22 cells) 0.01 μM (A549 cells) 0.02 μM (HCT116 cells) 0.02 μM (Caki-1 cells) |
| Xenograft mice model inhibition | 37% (10 mg/kg, SC) |

Notes: a: data of enzymatic activity, cell inhibition and xenograft mice model inhibition were cited from the previous work (reference: Chen Z, Li D, Xu N, et al. Novel 1,3,4-Selenadiazole-containing kidney-type glutaminase inhibitors showed improved cellular uptake and antitumor activity. J Med Chem. 2019;62(2):589-603.); b: CLogP: calculated LogP, which was assessed by ALOGPS2.1 (http://www.vcclab.org/lab/alogps/) and ChemBioDraw14.0.

Table S2. The tumor cell growth Inhibition by free CPD 23, CPD 23@SOL micelles and blank SOL micelles

| Tested samples | H22 (IC50: μM) | A549 (IC50: μM) |
| --- | --- | --- |
| Free CPD 23 | 2.94 ± 0.04 | 0.008 ± 0.001 |
| CPD 23@SOL micelles | 1.83 ± 0.02 | 0.042 ± 0.06 |
| Blank SOL micelles | ＞ 30 | ＞ 30 |

Note: Data were presented as Mean ± SD, n=3.

Abbreviations: H22: mouse hepatoma cells; A549: human non-small cell lung cancer cells.

Figure S1. The leakage of CPD 23@SOL micelles at CPD 23:SOL mass ratios 1:10 and 1:20 (37 ± 2 ℃) at 37 ℃.

Notes: **, P＜0.01; Data were presented as Mean ± SD, n=3.

Abbreviations: SOL: Soluplus®.

Figure S2. The biodistributions of CPD 23@SOL micelles and CPD 23 vehicle in tissues via intravenous administration at the dose of 20 mg/kg (CPD 23).

Notes: By IV administration, the total amounts of CPD 23 distributed in brain, heart, liver, spleen, lung and kidney in CPD 23@SOL micelles group (A) and CPD 23 vehicle group (B) were quantified within 24 h. Data were presented as Mean ± SD, n=3.

Abbreviations: IV: intravenous; WCPD 23: the weight of CPD 23 in tissue; Wtissue: the weight of tissue.