Supramolecular hydrogel based post-surgical implant system for hydrophobic drug delivery against glioma recurrence

[image: image1.png]MV

10.00

®
=)

o
=)

I
o

ol e
T SR SRV PRI SRR SR

o
o
=]

T
15.00

T
20.00

T T T
30.00 35.00 40.00

T T
25.00 50.00

Minutes

GPC Results

Mw

MP

Poly dispersity

2488

6527

6384

2.62





Figure.S1 – Gel Permeation Chromatography graph obtained by dissolving polymer in THF and analysed on Styragel column.
[image: image2.png]PEG-PCL-PEG-PCL-PEG PCL-PEG-PCL-PEG-PCL

-616

-941

|
@
@
|
©
2
&

S
E
<
3
>
2
s
c
[}

Energy (kJ/mol)

|
@
S
S

|

©

2

&

-622+ T T T T T T J -947+ T T T 1
0 5 10 15 20 25 30 35 40 45 S0

5 10 15 Zb 2‘5 3‘0 35 40 as 50
Time(ns) Time(ns)





Figure.S2 – Final micelle conformation Energy graph at 370C for 50 ns 

[image: image3.jpg]Intensity Distribution ACF
z g
] H
£ §
oo o R
Distribution Results (Contin) CumulantsResults
— Diameter (@ 5971 (nm)
Pelﬂk D'aTeZ‘fS’ 5]"’“) S;dl-%e;- Polydispersity Index (P.L) :0.281
H et e DiffusionConst. (D) :8.238009  (cm2/sec)
2 e ey Measurement Condition
4 00 00
Temperature 1250 0
5 00 00 5
A S5 Eo 5570 Diluent Name :WATER
L g b Refractive Index 113328
Viscosity {08878 ()
Residual 6.085¢-003 (0K Scattering Intensity 8171 (cps)





Figure. S3- Dynamic Light Scatteringanalysis of PCL-PEG hydrogel. Cumulant result diameter 597.1nm and polydispersity index 0.281 at 25C in water.

[image: image4.png]FOM 2} 104109

*v@;: 93d10d

d %. WM 93d10d
»

oo 9 05U00
)

" PR 93d10d

M | 021U0)

22 Kioreuwweyu jo saquiny





Figure. S4 : Number of inflammatory cells present at the site of surgery and implant in Rat brain cortex at following time points : 1 week, 6 week, 12 week in control (PBS) and PCL-PEG hydrogel implant. 
[image: image5.png]Hoescht 33342 Cleaved Caspase 3 Merged Merged without DIC

-
2
5

e
S
S8

s 5
CU

£ a
£
3
3
g
5

o





Figure S5: U251 cells treated with Curcumin (as it has autofluorescence) for 48 hours and with secondary antibody alone without cleaved Caspase 3 antibody and Hoescht 33342

[image: image6.png]Merged

r.
()
£
©
o)
£
o
<
£
3
=
ey
re)
w

Calcein

ulwnaan)
aunsnwie) ulnaJan) + dunsnwuie)





Figure S6  :U251 cells treated with Carmustine and Curcumin and Combination for 72 h and stained with Live Dead assay kit to asses combination efficacy against glioma cells.
[image: image7.emf]%  

C

y

t

o

t

o

x

i

c

i

t

y

(

E

t

h

i

d

i

u

m

 

p

o

s

i

t

i

v

e

 

c

e

l

l

s

)

C

o

n

t

r

o

l

 

T

r

e

a

t

e

d

C

o

n

t

r

o

l

 

T

r

e

a

t

e

d

C

o

n

t

r

o

l

 

T

r

e

a

t

e

d

0

20

40

60

80

100

24 Hrs

48Hrs

72Hrs

**

****


Figure S7 : Live dead assay analysis of U251 cells treated with Carmustine Curcumin loaded PCL-PEG hydrogel

[image: image8.png]Normal spleen

Splenomegaly

Control
PEG-PCL hydrogel

IV Carmustine + Curcumin

Carmustine + Curcumin
loaded PEG-PCL hydrogel

n=5

n=5

n=5

n=5




Figure S8 A :Splenomegaly observed in NOD-SCID mice after tumor implantation and aggressive recurrence of tumor post-surgical resection
[image: image9.jpg]S =

e N
|oaju 191183 93d-10d  (AI) Snug 2314 Bnap yum 93d-1D





Figure S8 B : H and E staining of Heart, Brain, Liver. Kidney, Lungs and Spleen of control, PCL-PEG carrier, Drug (IV) and Drug loaded PCL-PEG hydrogel.
