HA-DOPE Modified Honokiol-Loaded liposomes Targeted Therapy for Osteosarcoma
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Supplementary Figure
Figure S1 FT-IR spectra of hyaluronic acid (HA), dioleoyl phosphoethanolamine (DOPE), and HA-conjugated DOPE (HA-DOPE).
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HA and HA-DOPE were identified by HPLC. Briefly, BioCore SEC column was used for identifying the HA conjugated DOPE, and the composition of the mobile phase was 0.1M phosphate buffered saline (pH=7.0): methanol (80:20, v/v), the flow rate was 1.0 mL/min, and the detection wavelength was 214 nm, the BioCore SEC Column temperature was set at 30°C. 

Figure S2 High Performance Liquid Chromatograms of (A) HA and (B) HA-DOPE.
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Figure S3 FT-IR spectra of (A) HNK, (B) blank liposomes, (C) physical mixture (SPC, CHO, HA-DOPE and HNK) and (D) HA-DOPE@Lips/HNK.
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