Supporting information

Cytotoxicity and genotoxicity of polystyrene micro- and nanoplastics with different size and surface modification in A549 human lung cells

Xiaorui Shi1, Xinan Wang1, Rong Huang1, Chu Tang1, Chong Hu1, Pengbo Ning1*, Fu Wang1, 2, 3*

- Engineering Research Center of Molecular and Neuro Imaging, Ministry of Education, School of Life Science and Technology, Xidian University, Xi’an 710071, China

- Xianyang Key Laboratory of Molecular Imaging and Drug Synthesis, School of Pharmacy, Shaanxi Institute of International Trade & Commerce, Xianyang 712046, Shaanxi, China

- School of Basic Medical Sciences, Xi’an Jiaotong University, Xi’an 710061, China

*To whom correspondence should be addressed:

Fu Wang, E-mail: fwang@xidian.edu.cn

Pengbo Ning, E-mail: pbning@xidian.edu.cn

Supplemental Table S1. Zeta potential and average particle size characterization of all PS plastics dispersed in water. The size of the particles was expressed as intensity-based average hydrodynamic diameter. PDI: polydispersity index.

| MPs type | Water |  |  |
| --- | --- | --- | --- |
|  | Zeta Potential (Zp, mV) | Hydrodynamic Size (HDS, nm) | PDI |
| PS-NPs (80 nm) | -38.50±0.929 | 101.5±0.681 | 0.102±0.017 |
| PS-MPs (2 μm) | -31.23±1.415 | 2145±238.9 | 0.355±0.139 |
| PS | -24.3±0.723 | 104.1±1.514 | 0.0743±0.010 |
| PS-COOH | -20.2±1.430 | 97.2±1.490 | 0.128±0.024 |
| PS-NH2 | -22.6±2.600 | 91.2±1.450 | 0.0510±0.018 |

Supplemental Table S2. Zeta potential and average particle size characterization of all PS plastics dispersed in DMEM with or without FBS. The size of the particles was expressed as intensity-based average hydrodynamic diameter. PDI: polydispersity index.

| MPs type | DMEM without FBS |  |  | DMEM with FBS |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Zeta Potential (Zp, mV) | Hydrodynamic Size (HDS, nm) | PDI | Zeta Potential (Zp, mV) | Hydrodynamic Size (HDS, nm) | PDI |
| PS-NPs (80 nm) | -19.53±1.332 | 203.0±3.959 | 0.178±0.019 | -8.210±0.488 | 123.9±1.852 | 0.280±0.005 |
| PS-MPs (2 μm) | -10.39±0.927 | 3494±406.8 | 1.000±0.000 | -3.623±0.416 | 2423±424.1 | 0.529±0.150 |
| PS | -23.4±1.150 | 169±4.58 | 0.137±0.032 | -7.06±0.933 | 131±4.500 | 0.172±0.016 |
| PS-COOH | -20.3±1.100 | 200±2.65 | 0.164±0.012 | -7.51±0.631 | 114±3.350 | 0.188±0.006 |
| PS-NH2 | -22.0±0.458 | 160±1.41 | 0.151±0.014 | -7.07±1.350 | 111±4.000 | 0.221±0.006 |

Supplemental Figure S1. Scanning electron microscopy (SEM) images of 80 nm PS-NPs and 2 μm PS-MPs in ddH2O.

Supplemental Figure S2. Uptake of three kinds of red fluorescent PS-NPs by A549 cells was assessed using inverted fluorescence microscope. A549 cells were seeded in 6-well plates and incubated with three kinds of PS-NPs (200 μg/mL) separately for 24 h. Blue color indicates fluorescent PS-NPs under white light illumination and red color indicates fluorescent PS-NPs excited by green fluorescence. Scale bar, 50 μm for all images.