Supplementary material

Figure S1 In vitro cytotoxicity assessment of Dermaseptin-PP with different concentrations (n=6).

Figure S2 In vitro cytotoxicity assessment of PTX alone with different concentrations or in combination with Dermaseptin-PP (0.2 μg/ml).

Notes: Data were presented as mean ± standard deviation (n = 6; **** P < 0.0001).

Figure S3 Residence time of different gels in tumor after intratumoral injection under in vivo imaging technology (n=3).

Notes: (A) Free IR780 group. (B) IRL@gel group. (C) Der/IRL@gel group.

Table S1 Difference between cell inhibition ratio of PTX alone with different concentrations and that of PTX combined with Dermaseptin-PP (0.2 μg/ml).

| Concentration of PTX (μg/ml) | Difference of cell inhibition ratio (%) |
| --- | --- |
| 0.001 | 13.20 |
| 0.01 | 13.44 |
| 0.1 | 10.72 |
| 1 | 15.32 |
| 5 | 8.17 |
| 10 | 6.02 |

Table S2 The characterization of PTXL.

|  | Size (nm) | PDI | Zeta potential (mV) |
| --- | --- | --- | --- |
| 1 | 148.70 | 0.21 | -1.17 |
| 2 | 149.20 | 0.20 | -1.29 |
| 3 | 149.00 | 0.21 | -0.58 |
| Mean | 148.97 | 0.21 | -1.01 |
| SD | 0.21 | 0.01 | 0.31 |