Supplementary Materials

Bioactive Nanocomposite Microsponges for the Reconstruction of Critical-sized Calvarial Defects in Rats

Mohan Wang1, 2, Zheyuan Gu2, Beibei Li2, Jingyi Zhang2, Lu Yang2, Xianyu Zheng2, Faming Pan1,*, Jiacai He1,2,*

1 Department of Epidemiology and Biostatistics, School of Public Health, Anhui Medical University, Hefei, 230032, China

2 ﻿Stomatologic Hospital & College, Anhui Medical University, Key Laboratory of Oral Diseases Research of Anhui Province, Hefei 230032, China.

* Correspondence: famingpan@ahmu.edu.cn (F. P.), hejiacai@ahmu.edu.cn (J.H.)

Figure S1. Digital photographs show the produced lyophilized CS-HAP microsponges.

Figure S2. The pore size distribution of the CS-HAP microsponges, obtained by calculating them from SEM image, where at least 60 measurements were taken.

Figure S3. The swelling ratio of the CS-HAP microsponges, reaching up to ~ 1900%.

Figure S4. The volume change of the lyophilized CS-HAP microsponges after absorption in water. (a) Lyophilized CS-HAP microsponge. (b) The soaked CS-HAP microsponge.

Figure S5. OPM images of the CS-HAP microsponges after being treated with lysozyme solution for different times.

Figure S6. Fluorescent images of live/dead bacteria (green: live bacteria, red: dead bacteria). (a) S. aureus. (b) E. coli.

Figure S7. Adhesion efficiency of rBMSCs on the surface of CS-HAP microsponges.

Figure S8. The immunohistochemical images of the representative osteogenic-related gene markers. (a) Representative micrographs of OPN expression. (b) Representative micrographs of BMP-2 expression.