Supplementary Materials

Table S1: Comparative release of verapamil HCl loaded composite NFs (N6) and (Z5) after 2 and 24 hr.

|  | % Drug release from NF formulations |  | p |
| --- | --- | --- | --- |
|  | PVA-Z (Z5) | PVA-SA (N6) |  |
| 2 hours |  |  | 0.027* |
| Mean ± SD | 19.0 ± 1.0 | 29.7 ± 1.15 |  |
| 24 hours |  |  | 0.026* |
| Mean ± SD | 68.0 ± 1.0 | 93.7 ± 2.08 |  |

(*) Significant

Figure S1: Comparative verapamil HCl release from loaded composite NFs (N6) and (Z5) after 2 hr and 24 hr.

|  | Grp 0 Control | Grp 1 Verapamil HCl conventional gel | Grp 2 Placebo PVA-SA NFs (N2) | Grp 3 Placebo PVA-Z NFs (Z4) | Grp 4 Verapamil loaded PVA-SA NFs (N6) | Grp 5 Verapamil loaded PVA-Z NFs (Z5) | Test of significance (p) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| % Wound healing |  |  |  |  |  |  |  |
| Day 7 |  |  |  |  |  |  |  |
| Mean ± SD | 23±6.08 | 28±3 | 33±3 | 27±8.1 | 54±4 | 33±4.3 | (F=13.8, P<.001*) |
| Sig. between groups | Sig between Grp 4 Vs {control, Grp (1,2,3,5)} |  |  |  |  |  |  |
| Day 14 |  |  |  |  |  |  |  |
| Mean ± SD | 69±5.3 | 73±3 | 90±5 | 67±2 | 100±2 | 100±5 | (F=13.8, P<.001*) |
| Sig. between groups | Sig between {Grp 0 Vs Gp(2,4,5) }& {Gp1 vs Gr(2,4,5)} &{ Gp2 vs Gr (0,1,3)}& {Grp3 Vs Grp(2,4,5)}&{Grp 4 vs Grp (0,1,3)}&{Grp 5 vs Grp(0,1,3)} |  |  |  |  |  |  |

Table S2: Comparative % wound healing results for different treatment groups after 7 and 14 days.

(*)  Significant

F; One Way ANOVA based on boot strapping technique

Figure S2: Comparison between % wound healing of different treatment groups after 7 and 14 days.