Supplementary

# Materials and Methods

# Characterization of the GO Scaffolds

# Surface characteristics of the scaffolds were recorded using an FTIR spectrometer (Thermo Scientific, Nicolet iS50R, Waltham, America) and a Raman spectrometer (LabRAM, HR800, Horiba JobinYvon, France). FTIR was measured at a resolution of 4 cm−1 in the frequency range of 400–5000 cm−1, while the Raman spectra analysis was performed using a scanning range of 100–4000 cm−1. The excitation source was a 30 mW diode laser with a 532 nm wavelength. The X-ray diffraction (XRD) analysis was determined using an X-ray diffractometer (XRD, Empyrean, Netherlands) with Cu-Kα radiation in the range of 5°–90° (2θ).

# Hemocompatibility Tests of the Scaffolds in vitro

# The hemocompatibility of the nanofibrous membranes was measured through a hemolysis activity assay. In brief, blood from SD rats was collected and stabilized with heparin. The erythrocytes were extracted by centrifugation and re-suspended with PBS. Then, 6 mg fibrous membranes were mixed with 1mL erythrocytes in a tube at room temperature for 4 h. A negative control (PBS) and a positive control (water) were also included in the experiment to calculate the degree of hemolysis. All of the samples were centrifuged at 3500 rpm for 5 min and the upper solution was taken to detect the absorbance at 545 nm by microplate reader.

# Loading Efficiency of NAC on the Scaffolds

# The loading efficiency of NAC on the fiber surface was calculated with the following equation:

# Drug loading efficiency %=actual drug loading%theoretical drug loading % X 100

# The actual drug loading was expressed as the mass fraction of the entrapped drug relative to the mass of the nanoparticles, and was calculated using the following equation:

# Actual loading efficiency %=mass of loaded drugmass of particles obtained X 100

# The theoretical drug loading was the mass ratio of the drug used to the mixture of gelatin and drug in the solution that was used for the preparation of gelatin nanoparticles:

# Theoretical loading efficiency %=mass of drug usedmass of gelatin+drugused X 100

# ROS Level Measurement of the NAC-loaded Scaffolds in vitro

# Reactive oxygen species assay kit (Solarbio, China) was used to monitor the intracellular ROS level. Briefly, HDFs was treated with Rosup (0.05 mg/mL) to produce intracellular ROS, and washed by PBS for three times. Then the cells were incubated with scaffolds for 12 h at 37℃. Subsequently, DCFH-DA (10 μM) in serum-free medium was added for 15 min, and washed again. A negative control and a positive control were also included in the experiment. Finally, the cells were observed with a fluorescence microscope.

# Results

Morphology and Physiochemical Characterization of the GO Scaffolds

The transmission electron microscopy (TEM) of GO is presented in Figure S1A. Fourier-transform infrared spectroscopy (FTIR) spectra of different scaffolds are shown in Figure S1B, and all scaffolds exhibited similar FTIR spectra, in which the absorption peak of amide A, amide I, amide II, and amide III occurred respectively at 3286 cm-1, 1631 cm-1, 1535 cm-1, 1240 cm-1. Specifically, GO exhibited the characteristic peaks at 1732cm-1 (carboxylic acid C=O stretching), 1613cm-1 (C=C stretching), 1227cm-1 (C-OH stretching) and 1052cm-1 (C-O stretching), which was in line with the previous description. Figure S1C showed the Raman spectrum of the GO, which presents as characteristic peaks of the D band at 1356cm-1 and the G band at 1604cm-1. The X-ray diffraction (XRD) spectra of GO, Gel, NAC-Gel, GO-Gel, and NAC-GO-Gel scaffolds is analyzed in Figure S1D, and obvious peaks around 2θ=15° and 2θ=22° were observed in the GO spectra. No diffraction peak was observed in any other scaffolds, indicating that GO powder was dispersed uniformly in GO-Gel scaffolds.

In vitro Hemocompatibility the Scaffolds

# No apparent hemolysis was observed when the erythrocytes suspension was treated with fibrous mats in vitro. As shown in Figure S2, the relative hemolysis percentage of positive control (water) is 100%, while the negative control (PBS) is 0%. The relative hemolysis percentages of the fibrous membranes were all less than 5%, suggesting that all the nanofibrous membranes show excellent hemocompatibility.

# Loading Efficiency of NAC on the Scaffolds

# Based on the actual drug loading and theoretical drug loading, we calculated the NAC loading efficiency of the NAC-GO-Gel scaffolds and the NAC-Gel scaffolds were 85.9% and 73.6%, respectively.

# In vitro ROS Level Measurement of the NAC-loaded Scaffolds

# DCFH-DA immunofluorescence staining was used to evaluate the intracellular ROS scavenging capability of cells in the treatment groups with oxidative stress damage (Figure S3). Rosup is a wildly used agent to increase the ROS level in cell. With the exposure to Rosup, remarkable DCFH-DA staining was observed in the positive control group, suggesting the cellular oxidative was successfully induced. Notably, compared with the non-loading scaffolds, the fluorescent signals were decreased in co-cultured with NAC-loading scaffolds groups, to a little higher level as those in cells that were not stimulated by Rosup. This confirmed our hypothesis that treatment with NAC-loading scaffolds could improve the resisting oxidative stress ability.

# Figure legends

Figure S1. Characterization of nanofibrous scaffolds. (A) TEM image of GO (scale bar: 500nm); (B) FTIR spectroscopy; (C) Raman spectroscopy; (D) XRD spectroscopy.

Figure S2. Hemolysis test of different scaffolds exposure. The relative hemolysis percentages of the nanofibrous membranes were all less than 5%, suggesting that all these membranes show excellent hemocompatibility.

Figure S3. Fluorescence images of intracellular ROS reduction of Rosup-stimulated HDFs cells cultured under standard conditions or co-cultured with different scaffolds (scale bar: 100 μm).