Cellular Uptake of Differently Charged Mesoporous Bioactive Glass Nanoparticles to Enable Intracellular Delivery of Therapeutic Agents

Negar Hassani Besheli1, Juul Verbakel1, Maryam Hosseini1, Lea Andrée1, Ben Joosten2, X. Frank Walboomers1, Alessandra Cambi2, Fang Yang1, Sander C. G. Leeuwenburgh1

1 Department of Dentistry – Regenerative Biomaterials, Radboud Institute for Molecular Life Sciences, Radboudumc, Philips van Leydenlaan 25, 6525 EX Nijmegen, The Netherlands

2 Department of Cell Biology, Radboud Institute for Molecular Life Sciences, Radboud University Medical Center, Geert Grooteplein Zuid 26-28, 6525 GA Nijmegen, The Netherlands

Table S 1 Chemical composition of ALF.

| Reagent |  | Concentration (g/L) |
| --- | --- | --- |
| Magnesium chloride (MgCl2) | 0.050 |  |
| Sodium chloride (NaCl) | 3.210 |  |
| Disodium hydrogen phosphate (Na2HPO4) | 0.071 |  |
| Sodium sulfate (Na2SO4) | 0.039 |  |
| Calcium chloride dihydrate (CaCl2·2H2O) | 0.128 |  |
| Sodium citrate dihydrate (C6H5Na3O7·2H2O) | 0.077 |  |
| Sodium hydroxide (NaOH) | 6.000 |  |
| Citric acid (C6H8O7) | 20.800 |  |
| Glycine (H2NCH2COOH) | 0.059 |  |
| Sodium tartrate dihydrate (C4H4O6Na2·2H2O) | 0.090 |  |
| Sodium lactate (C3H5NaO3) | 0.085 |  |
| Sodium pyruvate (C3H3O3Na) | 0.086 |  |

Note: Reprinted from Acta Biomater, 66, Naruphontjirakul P, Porter AE, Jones JR. In vitro osteogenesis by intracellular uptake of strontium containing bioactive glass nanoparticles. 67–80, Copyright 2018, with permission from Elsevier.31

Supplemental Figures

Figure S 1 (A) Representative EDX spectrum and (B)  elemental distribution of synthesized Cu-MBGNs displaying the presence of  Si, Ca, and Cu.

Figure S 2 Linear relationship between fluorescence intensity and concentration of differently charged Cu-MBGNs.

Figure S 3  Zeta potential measurement of the nanoparticles after 24 h of incubation in media containing FBS.

Figure S 4 Zeta potential measurement of the nanoparticles after (A) 4 h and (B) 24h of incubation in water.

Supplemental movies

Movie S1 Confocal Z-stack movie of internalized negatively charged Cu-MBGNs into MC3T3-E1 cells.

Movie S2 Confocal Z-stack movie of internalized neutrally charged Cu-MBGNs into MC3T3-E1 cells.

Movie S3 Confocal Z-stack movie of internalized positvely charged Cu-MBGNs into MC3T3-E1 cells.

Movie S4 Confocal Z-stack movie of internalized negatively charged Cu-MBGNs into RAW 264.7 cells

Movie S5 Confocal Z-stack movie of internalized neutrally charged Cu-MBGNs into RAW 264.7 cells.

Movie S6 Confocal Z-stack movie of internalized positvely charged Cu-MBGNs into RAW 264.7 cells.