Table S1. Mn ratio in the MnOx-CeO2 NPs

|  | Molar ratio of Mn/(Mn+Ce) |  |
| --- | --- | --- |
|  | Experimental design (%) | ICP-MS (%) |
| MnOx-CeO2 NPs | 0 | 0.0 |
|  | 10 | 3.0 |
|  | 20 | 3.8 |
|  | 30 | 4.0 |
|  | 40 | 4.4 |

Figure S1. The ·OH scavenging effect of MnOx-CeO2 NPs.

Figure S2. The TEM image of SiO2 NPs, SiO2@ MnOx-CeO2 NPs and MnOx-CeO2 NPs.

Figure S3. In vivo saefty of MnOx-CeO2 NPs 28 days after i.v. injection. (A) blood analysis, (B) H&E staining of different organs.

Figure S4. In vivo bioditribution of MnOx-CeO2 NPs after i.v. injection.