Supplementary Material

# Short-term intravenous administration of carbon nano-onions is non-toxic in female mice

Yi Zhen Tan1, Lucy R Thomsen1, Nensi Shrestha1, Adalberto Camisasca2, Silvia Giordani2, Rhonda Rosengren1 *

1 Department of Pharmacology and Toxicology, University of Otago, Dunedin 9016, New Zealand.

2 School of Chemical Sciences, Dublin City University, Glasnevin, D09 NA55 Dublin, Ireland.

*Correspondence:

Rhonda Rosengren

Department of Pharmacology and Toxicology, 18 Frederick Street, Dunedin 9016, New Zealand.

Tel: +64 3 479 9141

Fax: +64 3 479 9140

Email: rhonda.rosengren@otago.ac.nz

## Methods

### Size characterization

Dynamic light scattering was performed on the Zetasizer® Nano ZS (ZEN3600, Malvern Instrument) with an He-Ne laser (wavelength, λ= 633 nm) and measurement angle of 173° (non-invasive blackscatter, NIBS® system). The oxi-CNO dispersion was transferred (without filtration) to a disposable acrylic semi-micro cuvette. A refractive index of 1.333 and viscosity of 1.0 cP were set for ultrapure water, while a refractive index of 1.400 and viscosity of 32.0 cP were set for 50% w/v PEG. The samples were allowed to equilibrate for a duration of 120 s at 20°C prior to measurement. All samples were analyzed by the Zetasizer® software (version 7.03, Malvern Instrument) to determine the hydrodynamic diameter (Z-average size) and intensity-weighted size distribution. Each sample was examined in triplicate consecutively, with an average of 14 runs per measurement.

Table S1: Body weight and organ weight of the mice following treatment with oxi-CNOs

|  | Unt | Veh | 125 µg | 250 µg | 500 µg |
| --- | --- | --- | --- | --- | --- |
| Single-dose |  |  |  |  |  |
| ∆ Body weight a | 0.76±0.22 | -0.06±0.26 | -0.28±0.21 | 0.08±0.38 | 0.14±0.22 |
| ∆ Body weight | 3.94±1.23 | -0.29±1.37 | -1.56±1.21 | 0.41±1.97 | 0.69±1.12 |
| Liver | 4.40±0.13 | 4.70±0.18 | 4.60±0.09 | 4.60±0.04 | 4.60±0.04 |
| Spleen | 0.35±0.01 | 0.37±0.02 | 0.39±0.01 | 0.37±0.01 | 0.37±0.01 |
| Lungs | 1.57±0.11 | 1.65±0.05 | 1.48±0.11 | 1.37±0.03 | 1.61±0.15 |
| Kidneys | 1.33±0.08 | 1.30±0.04 | 1.25±0.05 | 1.32±0.02 | 1.25±0.04 |
| Multiple-dose |  |  |  |  |  |
| ∆ Body weight a | 1.16±0.16 | -0.36±0.29 * | -0.02±0.17 * | -0.68±0.13 * | -0.62±0.41 * |
| ∆ Body weight | 5.82±0.83 | -1.71±1.40 * | -0.08±0.96 * | -3.65±0.63 * | -2.71±1.74 * |
| Liver | 4.94±0.05 | 4.65±0.15 | 4.79±0.16 | 4.92±0.10 | 5.08±0.05 |
| Spleen | 0.37±0.02 | 0.37±0.02 | 0.41±0.02 | 0.41±0.01 | 0.40±0.01 |
| Lungs | 1.50±0.04 | 1.37±0.18 | 1.51±0.05 | 1.54±0.05 | 1.41±0.13 |
| Kidneys | 1.21±0.03 | 1.33±0.02 | 1.27±0.04 | 1.33±0.04 | 1.34±0.05 |

Notes: Data are presented as the mean ± SEM of values expressed as % body weight unless stated otherwise, with n=5 mice per group. aValues expressed as g. Significance was determined with a one-way ANOVA coupled with a Tukey’s post-hoc test. *significantly decreased compared to untreated mice, p<0.05.

Abbreviations: Unt, untreated; Veh, vehicle control.

Table S2: Hydrodynamic diameter obtained from DLS measurements of oxi-CNOs dispersed in ultrapure water

| Dispersant | Concentration (µg/mL) | Z-average size (d. nm) |
| --- | --- | --- |
| 50% w/v PEG | 125 | 47.3±1.84 |
|  | 250 | 73.5±1.40 |
|  | 500 | 54.8±1.82 |
| Ultrapure water | 50 | 136.8±0.26 |
|  | 100 | 138.1±0.38 |
|  | 200 | 143.6±0.33 |

Notes: Hydrodynamic diameter is expressed in terms of Z-average size ± SEM. Each sample was run in triplicate consecutively, with the accumulation of an average of 14 runs per measurement.

Figure S1: Intensity-weighted size distribution of oxi-CNOs dispersed in 50% w/v PEG or ultrapure water. Each sample was run in triplicate consecutively, with the accumulation of an average of 14 runs per measurement.

Figure S2: Quantification of CNO aggregates accumulated in the organs following treatment with a single dose of oxi-CNOs. Data are presented as the mean ± SEM, with n=5 mice per group. Significance was determined with a two-way ANOVA coupled with a Tukey’s post-hoc test. ¤significantly increased compared to all other organs at the same concentration, p<0.01. #significantly increased compared to the lung at the same concentration, p<0.001. ϕsignificantly different from all other concentrations in the same tissue, p<0.05.

Abbreviations: Unt, untreated control; Veh, vehicle control.

Figure S3: H&E staining of kidney section. Kidney section (12 µm) from mice following treatment with three iv doses of 500 µg oxi-CNOs. The accumulation of CNO aggregates is indicated with black arrows. The representative images from n=5 mice per group are shown. Images are shown at 20x magnification. Scale bar, 100 µm.