Supporting Information

Supplementary Figure S1. The hydrodynamic diameters of prepared Gd@BSA NPs when changing the BSA feed to 75 mg/mL a), 112.5mg/mL b), 150mg/mL c), and 300mg/mL d) respectively, or at an elevated pH environment (pH = 12 or 13 ) e, f).

Supplementary Figure S2. The zeta potential of Gd@BSA NPs.

Supplementary Figure S3. XRD pattern of Gd@BSA NPs and JCPDS files of Gd2O3. (* Position of the characteristic peaks).

Supplementary Figure S4. The hydrodynamic diameters of Gd@BSA NPs after incubated in H2O a) , FBS b) .

Supplementary Figure S5. a) Photo of MRA scanning using rabbit models. b) Photo of the double-barrel high pressure syringe.

Supplementary Figure S6. The 3D-reformed images of cardiac arteries and their branches, abdominal aorta from the rabbits after injected with Gd-DTPA.

Supplementary Figure S7. The angiographic images of cardiovascular systems of the rabbits after injected with Magnevist nanoparticles.

Supplementary Figure S8. CNR and SNR corresponding to the angiographic images at different times after injection of Gd@BSA NPs. The regions of interest used to calculate CNR and SNR of (a,b) were main cardiac vessels. ****P<0.0001.

Supplementary Table S1. Measurement of Gd excretion rates of from the rabbits injected with Gd@BSA.

|  | 1d | 3d | 5d | 7d |
| --- | --- | --- | --- | --- |
| Feces (%) | 25.70 | 2.74 | 1.01 | 0.94 |
| Urine (%) | 49.35 | 9.50 | 4.40 | 1.09 |

.

Supplementary Figure S9. HeLa cell viability determined by MTT assay after incubation with different concentrations of Gd@BSA NPs (0–1100 µg/mL).

Supplementary Figure S10. RAW264.7 cells viability via MTT assay after incubation with different concentrations of Gd@BSA NPs (0–1000 µg/mL).

Supplementary Figure S11. Changes in the rabbit body weights during the 14-day observation period.

Supplementary Table S2. Hematology indexes from the rabbits injected with Gd-DTPA during a 14-day observation period (n=3).

|  | Pre | 5 min | 15 min | 30 min | 1h | 2h | 4h | 6h | 1d | 3d | 7d | 14d |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| WBC(109/L) | 5.93 | 5.93 | 6.43 | 1.03 | 1.13 | 1.20 | 2.03 | 1.67 | 6.43 | 3.27 | 3.78 | 5.54 |
| RBC(1012/L) | 4.12 | 4.12 | 4.27 | 3.26 | 1.67 | 2.54 | 2.68 | 2.73 | 5.29 | 2.63 | 2.60 | 1.66 |
| PLT(109/L) | 201.33 | 201.33 | 179.67 | 38.00 | 26.00 | 42.00 | 55.67 | 30.00 | 336.00 | 46.00 | 127.50 | 91.00 |
| HGB(g/L) | 328.67 | 328.67 | 319.33 | 285.25 | 352.00 | 367.67 | 345.67 | 339.00 | 217.67 | 335.67 | 375.50 | 436.20 |
| NE(109/L) | 4.43 | 4.43 | 5.07 | 0.80 | 0.97 | 1.00 | 1.57 | 1.37 | 5.40 | 2.63 | 2.75 | 4.68 |