Supplementary Information for
Preparation and Characterization Evaluation of Poly(L-glutamic acid)-g-methoxy poly(ethylene glycol)/combretastatin A4/BLZ945 Nanoparticles for Cervical Cancer Therapy 

Dongmei Guoa, Yue Huangb*, Kun Wangb, Chenguang Yangb, Lili Mab, Yu Zhangb, Haiyang Yub, Manhua Cuia*, Zhaohui Tangb
aDepartment of Gynecology and Obstetrics, The Second Hospital of Jilin University, Changchun 130041, Jilin Province, PR China
bKey Laboratory of Polymer Ecomaterials, Changchun Institute of Applied Chemistry, Chinese Academy of Sciences, Changchun 130022, PR China
[image: image1.png]AN My
I’R
OO0
NH  © 1-Hexylamine o o o
DMF, 25 oC N mPEGSK/
@Ac,0 TN '}“r(cm(a%)rausu(b%)
n o
o ® HBr/ACOH T 2as
DCA, 25 °C Ho! Trichlorobenzoyl
Chloride/ TEAIDMAP \

BLG-NCA PLG, 1




* Corresponding author at: Department of Gynecology and Obstetrics, The Second Hospital of Jilin University, Changchun, Jilin Province, PR China. 

E-mail address: cuimanhua@126.com
Key Laboratory of Polymer Ecomaterials, Changchun Institute of Applied Chemistry, Chinese Academy of Sciences, Changchun 130022, P. R. China. Tel./Fax: +86 431 85262116 (Y. Huang)

E-mail address: huangyue@ciac.ac.cn  
Supplementary caption
Scheme S1. Synthetic routes of API. 
Figure S1. 1H NMR, GPC, and HPLC spectra of API. 
1. Synthesis and Characterization
[image: image3.png]10

min

20

a PO 0y o u o N b
N N‘)_S/N N N
H 0.052 0.875 0.047 0.026 [160°0
[o} © [o} ~, (o} R
5 on  § 4 /o " NH
(o} s
< s
3 LG
\ 0~ [o) Solvent f Solvent
A \ : v
\NW, 2 0. P jHkH d+etm+o
3 e N thstr gy chvw ——
T ~NH P — mhath
1 PNV VTN
API
(PLGIGO_g_mPEGS.SO/C A47.50/BLZ9454.20) .0 85 8.0 75 7.0 65 6.0 55 ?io(pp:{]ﬁ 35 3.0 25 20 15 1.0
C d CA4
2500 I
2000
BLZ945
16.00
§ 10.00
5.00
00— o
-5.00
200 40 &M 80 1000 1200 40 1600 1800 2000 200 200 2500 20 200
min





Scheme S1. Synthetic routes of API (PLGn-g-mPEGx/CA4y /BLZ945z).

1.1 Synthesis of poly(L-glutamic acid)s (PLGn)
Poly(L-glutamic acid)s (PLGn) were synthesized as reported in our previous work 
 ADDIN EN.CITE 
1
. Briefly, γ-Benzyl-L-glutamate-N-carboxyanhydride (BLG-NCA) was dissolved in anhydrous DMF under a nitrogen atmosphere. Then n-hexylamine in anhydrous DMF was added. The polymerization was carried out at 25 ℃ for 3 days. At the end of 3 days, acetic anhydride was added to further react for 24 h at 25 ℃. Reaction mixture was precipitated into the excessive ether. A white solid poly(γ-benzyl L-glutamate) (PBLG) was obtained after drying under vacuum at room temperature for 24 h. 1H NMR (300M, CF3COOD) of PBLG: δ 7.24 ppm (br, 5H, -CH2C6H5), 5.11 ppm (br, 2H, -CH2C6H5), 4.66 ppm (br, 1H, -CH<), 2.48 ppm (br, 2H, -CH2COO-), 2.13 and 1.96 ppm (br, 2H, -CHCH2-). The PBLG was dissolved in dichloroacetic acid (DCA) and then HBr/acetic acid (33 wt%) was added (Weight of PBLG/Volume of DCA/Volume of HBr/acetic acid = 1 g/10 mL/4 mL). The solution was stirred at 30 ℃ for 1 h before precipitation into the excess ether. After drying under vacuum, the precipitate was dialyzed (MWCO 3500) against distilled water and freeze-dried to give the PLG product in white powders. 1H NMR (400M, NaOD/D2O) of PLG: δ 4.10 ppm (t, 1H, -CH<), 2.06 ppm (m, 2H, -CH2COOH), 1.82 and 1.72 ppm (m, 2H, -CHCH2-). PLGn with a certain polymerization degree was produced by calculated the feed ratio of monomer to initiator. Here “n” represents the molar ratio of BLG-NCA to n-hexylamine in feed. According to our screening work, when “n” was 160, PLG performed perfect properties for the next grafting operation.

1.2 Synthesis of poly(L-glutamic acid)-g-methoxy poly(ethylene glycol)/combretastatin A4/BLZ945 (PLG160-g-mPEG8.30/CA47.50/BLZ9454.20)
PLG160-g-mPEG8.30/CA47.50/BLZ9454.20 were prepared by the Yamaguchi reaction of PLG with mPEG, CA4 and BLZ945. The content determination of CA4 and BLZ945 had been discussed in our previous work
 ADDIN EN.CITE 
2
. Typically, PLG, dried mPEG, CA4 and BLZ945 were dissolved in anhydrous DMF by heating at 40 ℃ for 2 hours. After the temperature was cooled to 25 ℃, 2,4,6-trichlorobenzoyl chloride, triethylamine and DMAP were added in succession. After stirring at 25 ℃ for 24 h, the reaction mixture was precipitated into the excess ether and washed twice with ether. After drying under vacuum, the precipitate was dialyzed (MWCO 3500) against distilled water and freeze-dried to give the PLG160-g-mPEG8.30/CA47.50 /BLZ9454.20 product as active pharmaceutical ingredients (API). 1H NMR (300M, D2O/NaOD/DMSO-d6), GPC (DMF), and HPLC spectra of API were shown in Fig. S1.

[image: image2]
Figure S1. The structure (a), 1H NMR (b), GPC (c), and HPLC (d) spectra of API. 

2. Reference
1.
Wang, Y.; Shen, N.; Wang, Y.; Zhang, Y.; Tang, Z.; Chen, X., Self-Amplifying Nanotherapeutic Drugs Homing to Tumors in a Manner of Chain Reaction. Adv Mater 2021, 33 (7), e2002094.

2.
Huang, Y.; Yang, C.; Lv, J.; Zhang, Y.; Wang, K.; Ma, L.; Liu, Z.; Yu, H.; Li, M.; Tang, Z., Formula Optimization and In Vivo Study of Poly(L-glutamic acid)-g-methoxy poly(ethylene glycol)/combretastatin A4/BLZ945 Nanoparticles for Cancer Therapy. Int J Pharm 2023, 636, 122849.



