The Supplementary Information

Supplementary Figure 1. Conditions for Calculating Hydrogen Bonding

Supplementary Figure 2. Comparison of the Hydrogen Bond (H-bond) Graphs of the Complex System During Molecular Dynamics Simulations

Supplementary Table 1. The Molecular Docking Interaction between Ritonavir and Polymers

| No | Polymer | Binding Energy (kcal/mol) | Hydrogen bond distance (Å) |
| --- | --- | --- | --- |
| 1 | Hypromellose (HPMC) | -5.28 | 2.03 |
| 2 | Hypromellose phthalate (HPMCP) | -2.75 | 2.16 |
| 3 | Hypromellose acetate succinate (HPMCAS) | -2.25 -5.11 | 2.20 2.02 |
| 4 | Polyvinylpyrrolidone (PVP) | -4.16 | 2.03 |
| 5 | Polyvinyl acetate (PVA) | -5.84 | 1.99 |
| 6 | Co-povidone (PVPVA) | -3.28 | 2.00 |
| 7 | Eudragit | -5.06 | 2.07 |
| 8 | Polyvinyl acetate phthalate (PVAP) | -0.38 -4.78 | 2.00 2.14 |
| 9 | Methyl cellulose | -5.91 -3.53 | 1.99 1.99 |
| 10 | Ethyl cellulose | -3.05 | 2.16 |
| 11 | Natrium alginate | -5.59 -2.30 | 2.05 2.17 |
| 12 | Carbomer | -2.55 | 2.09 |
| 13 | PEG | -6.61 | 1.93 |
| 14 | Chitosan | -2.55 -3.28 -4.14 -0.60 | 2.20 1.86 2.07 2.17 |
| 15 | Water soluble chitin | -6.06 | 1.99 |
| 16 | Soluplus | -5.44 | 2.06 |
| 17 | Locust bean gum | -5.21 | 2.10 |
| 18 | Cellulose acetate phthalate (CAP) | -4.64 | 2.13 |
| 19 | Poloxamer 188 | -5.64 -5.58 | 2.10 1.98 |
| 20 | D-ɑ-tocopheryl polyethylene glycol succinate (TPGS) | -3.36 | 2.11 |
| 21 | 5-carboxypentyl hydroxypropyl cellulose (5-CHC) | -2.06 -7.84 | 2.13 1.78 |

Supplementary Table 2. Interaction Dynamics of the RTV and PLX During Molecular Dynamics Simulations

| Melt-Cooling-A | Interaction | Category | Distance |
| --- | --- | --- | --- |
| 0 ns Temperature: 0oC Hydrogen Bond: 7 interactions Poloxamer: 4 molecules | RIT - POL9:O3 RIT - POL9:O3 POL15:H29 - RIT POL23:H29 - RIT1:O6 RIT - POL23:O2 RIT - POL24:O3 POL23:H22 - RIT | Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond | 2.05 Å 3.02 Å 2.04 Å 1.89 Å 2.61 Å 2.89 Å 2.40 Å |
| 250 ns Temperature: 140oC Hydrogen Bond: 15 interactions Poloxamer: 7 molecules | RIT - POL9:O3 RIT - POL3:O3 POL3:H29 - RIT POL13:H29 - RIT POL20:H29 - RIT RIT - POL20:O3 RIT - POL15:O3 RIT - POL11:O1 RIT - POL3:O2 POL11:H13 - RIT POL11:H22 - RIT POL13:H15 - RIT POL18:H27 - RIT POL18:H28 - RIT POL20:H23 - RIT | Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond | 2.15 Å 2.13 Å 1.72 Å 2.27 Å 1.86 Å 2.27 Å 2.76 Å 2.98 Å 2.44 Å 2.59 Å 2.75 Å 2.64 Å 3.03 Å 2.97 Å 2.90 Å |
| 500 ns Temperature: 0oC Hydrogen Bond: 2 interactions Poloxamer: 2 molecules | POL11:H29 - RIT POL26:H29 - RIT | Hydrogen Bond Hydrogen Bond | 2.12 Å 2.34 Å |

Supplementary Table 2. Interaction Dynamics of the RTV and PLX During Molecular Dynamics Simulations (Cont.)

| Melt-Cooling-A | Interaction | Category | Distance |
| --- | --- | --- | --- |
| 0 ns Temperature: 0oC Hydrogen Bond: 11 interactions Poloxamer: 7 molecules | RIT - POL26:O3 POL20:H29 - RIT POL24:H29 - RIT RIT - POL24:O3 RIT - POL14:O2 RIT - POL4:O3 POL14:H12 - RIT POL20:H23 - RIT POL22:H22 - RIT POL25:H22 - RIT POL26:H14 - RIT | Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond | 2.16 Å 2.04 Å 2.07 Å 2.55 Å 2.85 Å 2.74 Å 2.63 Å 2.56 Å 2.64 Å 2.79 Å 2.64 Å |
| 250 ns Temperature: 140oC Hydrogen Bond: 1 interaction Poloxamer: 1 molecule | POL8:H13 - RIT | Hydrogen Bond | 2.67 Å |
| 500 ns Temperature: 0oC Hydrogen Bond: 7 interactions Poloxamer: 2 molecules | RIT - POL4:O3 POL4:H29 - RIT RIT - POL18:O1 RIT - POL18:O3 POL4:H14 - RIT POL4:H27 - RIT POL4:H28 - RIT | Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond | 1.99 Å 2.01 Å 2.52 Å 2.75 Å 2.45 Å 2.91 Å 2.99 Å |

Supplementary Table 2. Interaction Dynamics of the RTV and PLX During Molecular Dynamics Simulations (Cont.)

| Melt-Cooling-A | Interaction | Category | Distance |
| --- | --- | --- | --- |
| 0 ns Temperature: 0oC Hydrogen Bond: 13 interactions Poloxamer: 6 molecules | RIT - POL20:O3 RIT - POL10:O2 RIT - POL3:O3 POL2:H29 - RIT POL10:H29 - RIT POL19:H29 - RIT RIT - POL10:O2 RIT - POL3:O3 RIT - POL9:O1 RIT - POL2:O3 POL3:H28 - RIT POL19:H28 - RIT POL20:H23 - RIT | Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond | 1.89 Å 1.97 Å 2.11 Å 2.68 Å 1.98 Å 1.75 Å 2.58 Å 2.60 Å 2.49 Å 2.57 Å 2.49 Å 2.80 Å 2.33 Å |
| 250 ns Temperature: 140oC Hydrogen Bond: 7 interactions Poloxamer: 5 molecules | RIT - POL7:O3 POL17:H29 - RIT RIT - POL20:O2 X: POL17:H16 - RIT X: POL17:H28 - RIT X: POL21:H22 - RIT X: POL18:H29 - RIT | Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond | 2.37 Å 1.84 Å 2.40 Å 2.98 Å 2.82 Å 2.66 Å 2.81 Å |
| 500 ns Temperature: 0oC Hydrogen Bond: 6 interactions Poloxamer: 2 molecules | RIT - POL17:O2 POL17:H29 - RIT RIT - POL17:O3 POL17:H12 - RIT POL17:H27 - RIT POL21:H27 - RIT | Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond Hydrogen Bond | 2.67 Å 1.76 Å 2.62 Å 2.69 Å 2.85 Å 2.96 Å |

Supplementary Table 2. Interaction Dynamics of the RTV and PLX During Molecular Dynamics Simulations (Cont.)

| Melt-Cooling-A | Interaction | Category | Distance |
| --- | --- | --- | --- |
| 0 ns Temperature: 0oC Hydrogen Bond: 0 interaction Poloxamer: 0 molecule | - | - | - |
| 50 ns Temperature: 20oC Hydrogen Bond: 1 interaction Poloxamer: 1 molecule | POL741:H27 - RIT | Hydrogen Bond | 2.66 Å |
| 200 ns Temperature: 80oC Hydrogen Bond: 0 interaction Poloxamer: 0 molecule | - | - | - |