Supplementary information

PDADMAC/ALGINATE-COATED GOLD NANOROD FOR ERADICATION OF STAPHYLOCOCCUS AUREUS BIOFILMS

Malarmugila Manimaran1,a, , Yin Yin Teo2, James Chen Yong Kah3, Adilet Beishenaliev1, Yean Leng Loke2, Yiing Yee Foo1, Shiow-Fern Ng4, Chin Fei Chee5, Sek Peng Chin6, Farid Nazeer Faruqu1, Chia-Yu Chang7, Misni Misran2, Lip Yong Chung6, Bey Fen Leo8,a, Shih-Hwa Chiou9,10, Chia-Ching Chang7,11,12,13,*, Sun Tee Tay14, Lik Voon Kiew1,7*

1Department of Pharmacology, Faculty of Medicine, Universiti Malaya, Kuala Lumpur, Malaysia

2Department of Chemistry, Faculty of Science, Universiti Malaya, Kuala Lumpur, Malaysia

3Department of Biomedical Engineering, College of Design and Engineering, National University of Singapore, Singapore, Singapore

4Centre for Drug Delivery Technology and Vaccine, Faculty of Pharmacy, Universiti Kebangsaan Malaysia, Kuala Lumpur, Malaysia

5Nanotechnology Catalysis Research Centre, Universiti Malaya, Kuala Lumpur, Malaysia

6Department of Pharmaceutical Chemistry, Faculty of Pharmacy, Universiti Malaya, Kuala Lumpur, Malaysia

7Department of Biological Science and Technology, National Yang Ming Chiao Tung University, Hsinchu, Taiwan, Republic of China

8Department of Molecular Medicine, Faculty of Medicine, Universiti Malaya, Kuala Lumpur, Malaysia

9Department of Medical Research, Taipei Veterans General Hospital, Taipei, Taiwan, Republic of China

10Institute of Pharmacology, National Yang Ming Chiao Tung University, Taipei, Taiwan, Republic of China

11Department of Electrophysics, National Yang Ming Chiao Tung University, Hsinchu, Taiwan, Republic of China

12Center for Intelligent Drug Systems and Smart Bio-devices, National Yang Ming Chiao Tung University, Hsinchu, Taiwan, Republic of China

13Institute of Physics, Academia Sinica, Nankang, Taipei, Taiwan, Republic of China.

14Department of Medical Microbiology, Faculty of Medicine, Universiti Malaya, Kuala Lumpur, Malaysia

a These authors contributed equally to this work.

* Corresponding authors:

Chia-Ching Chang, ccchang01@nycu.edu.tw

Lik-Voon Kiew, lvkiew@um.edu.my

A. Concentration of Gold Nanorods (GNR)

The concentration of the GNR was estimated from the UV-visible spectra of the GNR using a technique derived from a previous study. The extinction coefficient value of GNR was obtained through the equation:

y=1.23×107x-5.02×109,

where x is the wavelength in the UV-visible spectra, and y is the extinction coefficient. Thus, the concentration1 of GNR was calculated based on the equation: nM=Absy, where absorbance value2 was obtained from the UV-visible spectrophotometer, and y is the extinction coefficient.3

B. Effects of PDADMAC on bacterial biofilms

Graph of PDADMAC solution alone without the combination of GNR doesn’t show significant biofilm eradication but poses below 35% of eradication even at a high concentration of 5 mg/mL.

Figure S1. Poly(diallyldimethylammonium chloride) (PDADMAC) at working concentrations (5 mg/mL) did not cause a significant biofilm eradication after 24 hours of incubation, suggesting the PDADMAC/alginate-coated gold nanorods (GNR/Alg/PDADMAC)’s ability in biofilm eradication was not due to PDADMAC solely. Data are represented as mean ± SD (n = 3).

C. Calculation of the percentage of biofilm eradication

The percentage of biofilm eradication was calculated using the formula:

1. Absorbance value - Average sterility control absorbance value = Normalised absorbance value.

2. 100 × (1-normalised absorbance value/Average growth control absorbance value) = % Biofilm Eradication.

3. Plot concentration (x- axis) against average value of biofilm eradication (y-axis) + standard deviation.

*MBEC 50 = Minimum biofilm eradication concentration that eradicates 50% of biofilm

Figure S2. (A) microtiter well pictures after CV staining of untreated and GNR/Alg/PDADMAC-treated biofilms of MRSA and MSSA, showing less CV stain in both MRSA and MSSA biofilms after exactly 16.5 minutes and 17 minutes of GNR/Alg/PDADMAC treatment. (B) Microscopic picture further enhanced the ability of GNR/Alg/PDADMAC at 0.15 nM to eradicate 50% (MBEC50) of MRSA and MSSA biofilm within 16.5 and 17 minutes, respectively. Pictures A and B manifest that the composition of both GNR/Alg/PDADMAC-treated MRSA and MSSA biofilms were reduced significantly at a shorter time, 16.5 minutes and 17 minutes.

D. Effects of GNR/Alg/PDADMAC on the biofilms of Gram-negative bacteria

The effects of GNR/Alg/PDADMAC on the biofilms of Gram-negative bacteria, i.e. Pseudomonas aeruginosa, Escherichia coli, and Klebsiella pneumonia was performed. Results revealed that GNR/Alg/PDADMAC was ineffective in eradicating the biofilms of the Gram-negative bacteria at the concentration range tested (0.002 – 0.3 nM) although similar concentration range was effective in eradicating Gram-positive MRSA and MSSA biofilms (Figure S3). This suggests the avenues of further improvement onto the GNR/Alg/PDADMAC to expand its biofilm eradication spectrum. Meanwhile the positive control triclosan at high concentration (345 µM) showed effective eradication of Gram-Positive MRSA and MSSA biofilms as well as the biofilms of Gram-negative Klebsiella pneumonia and Escherichia coli, but not the biofilms of Pseudomonas aeruginosa (Figure S4)

Figure S3. PDADMAC/alginate-coated gold nanorod (GNR/Alg/PDADMAC) showing inefficient Klebsiella pneumonia, Pseudomonas aeruginosa and Escherichia coli biofilm eradication but effectively remove Gram-positive bacteria (MRSA and MSSA) at increasing concentration. Data are represented as mean ± SD (n = 3).

Figure S4. Triclosan at high concentration (345 µM) showed effective eradication of the biofilms of the Gram-Positive MRSA and MSSA as well as Gram-negative Klebsiella pneumonia and Escherichia coli, but not the biofilms of Gram-negative Pseudomonas aeruginosa (Figure S4).

E. Effects of GNR/Alg on the biofilms of MRSA and MSSA

The effects of GNR/Alg on the biofilms of MRSA and MSSA was performed. Results revealed that GNR/Alg was ineffective in eradicating the biofilms of the MRSA and MSSA at the concentration range tested (0.002 – 0.3 nM) (Figure S5).

Figure S5. GNR/Alg was ineffective in eradicating the biofilms of the MRSA and MSSA at the concentration range tested (0.002 – 0.3 nM). Data are represented as mean ± SD (n = 3).

F. CLSM studies:

Figure S6 displays CLSM pictures comparing the reduction in biofilm and cell death between the GNR/Alg/PDADMAC-treated strains of MRSA and MSSA with the control strain.

Figure S6. Two-dimensional (2D) CLSM images of MRSA and MSSA strains under 40 magnification, manifesting the viability of both PDADMAC/alginate-coated gold nanorod (GNR/Alg/PDADMAC)-treated MRSA and MSSA biofilms were reduced significantly (Scale bar = 50 µM).

REFERENCES

1.	Selvaraj, A.; Jayasree, T.; Valliammai, A.; Pandian, SK., Myrtenol attenuates MRSA biofilm and virulence by suppressing sarA expression dynamism. Frontiers in Microbiology  2019, 10, 2027.

2.	Nikoobakht, B.; El-Sayed, MA., Preparation and growth mechanism of gold nanorods (NRs) using seed-mediated growth method. Chemistry of Materials 2003, 15 (10), 1957-1962.

3.	 Orendorff, CJ.; Murphy, CJ., Quantitation of metal content in the silver-assisted growth of gold nanorods. The Journal of Physical Chemistry B, 2006, 110 (9), 3990-3994.