Table S1. Material composition of all prepared transdermal nanocarriers formulation.

| Group | Tween 80 (wt%) | Limonene (wt%) | D.D Water (wt%) |
| --- | --- | --- | --- |
| TD-71 | 70 | 10 | 20 |
| TD-41 | 40 | 10 | 50 |
| TD-11 | 10 | 10 | 80 |
| TD-12 | 10 | 20 | 70 |
| TD-13 | 10 | 30 | 60 |
| TD-14 | 10 | 40 | 50 |
| TD-15 | 10 | 50 | 40 |
| TD-16 | 10 | 60 | 30 |
| TD-18 | 10 | 80 | 10 |

Abbreviations: TD = transdermal nanocarriers

Table S2 Nano emulsion system of transdermal nanocarrier formula.

| Group | Size (nm) |  |  | PDI |  | Zeta (mV) |  | T:L (wt%) |  | Appearance |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TD-71 | X |  |  | X |  | X |  | 1:0.14 |  | Precipitate |  |
| TD-41 | 94.6 ± 0.79 |  |  | 0.547 ± 0.01 |  | -7.13 ± 0.32 |  | 1:0.25 |  | Light milky |  |
| TD-11 | 202.7 ± 6.79 |  |  | 0.452 ± 0.02 |  | -12.7 ± 0.40 |  | 1:1 |  | Light milky |  |
| TD-12 | 187.5 ± 4.01 |  |  | 0.282 ± 0.03 |  | -14.8 ± 0.30 |  | 1:2 |  | Milky |  |
| TD-13 | 415.8 ± 7.25 |  |  | 0.492 ± 0.01 |  | -13.5 ± 0.57 |  | 1:3 |  | Light milky |  |
| TD-14 | 333.0 ± 16.55 |  |  | 0.448 ± 0.01 |  | -11.1 ± 0.51 |  | 1:4 |  | Milky |  |
| TD-15 | 334.5 ± 8.10 |  |  | 0.591 ± 0.03 |  | -13.6 ± 0.61 |  | 1:5 |  | Turbidity |  |
| TD-16 | 294.0 ± 12.05 |  |  | 0.399 ± 0.02 |  | -14.6 ± 0.42 |  | 1:6 |  | Turbidity |  |
| TD-18 | 275.1 ± 64.83 |  |  | 0.453 ± 0.11 |  | -12.8 ± 0.44 |  | 1:8 |  | Turbidity |  |
| Group |  | Tween80 : Limonene (wt%) | CBD (mg) | Size (nm) | PDI |  | Zeta (mV) |  | EE (%) |  | DL (%) |
| CTD-41 |  | 1 : 0.25 | 200 | 174.1 ± 0.87 | 0.195 ± 0.01 |  | -18.9 ± 0.47 |  | 87.83 ± 3.24 |  | 30.25 ± 1.12 |
| CTD-12 |  | 1 : 2 | 200 | 333.4 ± 0.26 | 0.234 ± 0.02 |  | -44.2 ± 0.27 |  | 89.01 ± 1.02 |  | - ± 3.44 |

Abbreviations: PDI, Polydiseperse Index; EE%, Encapsulation Efficiency; DL%, Drug Loaded ratio; TD = Transdermal nanocarriers; CTD = Cannabidiol loaded transdermal nanocarriers; CBD = Cannabidiol.

Table S3. Comparison CTD-12 with other studies CBD formulation system transdermal ability.

| Formulation system | Performance | Ref |
| --- | --- | --- |
| Micellar vesicular nanocarriers | CTD-12 0-24 hr: 3521.45 ± 200.86 mcg = 11918.26 ± 638.74 nmol Flux: 83.07 ± 4.74 mcg/hr∙cm2 = 264.16 ± 15.07 nmol/hr∙cm2 |  |
| Gel + Penetration enhancer | Twice dosage(12hr/times) 4 % CBD gel 0-24 hr: 87.5 ± 19.5 nmol Flux: 2.9 ± 0.6 nmol/hr∙cm2 | US20100273895A174 CA2760460C75 |
| CBD + Penetration enhancer | CBD 0-48 hr: 193.21 ± 22.77 nmol Flux: 6.13 ± 0.43 nmol/hr∙cm2 CBD + transcutol hp (TC-HP) 0-48 hr: 503.98 ± 109.94 nmol Flux: 14.81 ± 1.08 nmol/hr∙cm2 CBD + super refined® novol nf(OA) 0-48 hr: 688.09 ± 154.27 nmol Flux: 14.69 ± 1.7 nmol/hr∙cm2 CBD + labrafil® m1944 cs (LF) 0-48 hr: 670.54 ± 184.73 nmol Flux: 614.9 ± 3.02 nmol/hr∙cm2 | US8435556B276 |
| Microneedle drug delivery system | CBD 0-48 hr: 0 ± 0 nmol Flux: 0 ± 0 nmol/hr∙cm2 ALL00179 0-48 hr: 3110.7 ± 686.0 nmol Flux: 63.2 ± 11.4 nmol/hr∙cm2 | US9533942B277 |
| NLC | CBD-NLC1 Flux: 15.56 ± 1.22 mcg/hr∙cm2 CBD-NLC2 Flux: 16.47 ± 1.81 mcg/hr∙cm2 CBD-NLC3 Flux: 11.00 ± 1.02 mcg/hr∙cm2 CBD-NLC4 Flux: 12.52 ± 2.71 mcg/hr∙cm2 | 78 |
| Transfersome and Micelle system | Transfersome Flux: 0.07 ± 0.02 mcg/hr∙cm2 Micelle system Flux: 0.19 ± 0.10 mcg/hr∙cm2 | 79 |
| Micelles-in-Liposome Systems | DiMiL system 0-24 hr: < 1.8 mcg/cm2 24 hr in skin: 4.67 ± 1.23 mcg/cm2 | 80 |
| Oil-in-water nano emulsions | Oil-in-water nanoemulsions 0-30 hr: 572.56 ± 211.11 mcg/cm steady-state flux: 403.37 ± 130.09 mcg/hr∙cm2 Oil-in-water nano emulsion-filled hydrogels 0-30 hr: 709.22 ± 220.62 mcg/cm steady-state flux: 475.68 ± 162.57 mcg/hr∙cm2 | 81 |
| Pickering emulsion | Formulation 1 - olive oil 24 hr Stratum corneum: 105.92 ± 12.95 mcg/cm2 viable epidermis and dermis: 38.06 ± 8.05 mcg/cm2 Receptor fluid: 4.06 ± 1.01 mcg/cm2 Residual sample (skin surface): 2846.02 ± 104.41 mcg/cm2 Formulation 2 - liquid paraffin 24 hr Stratum corneum: 123.11 ± 17.59 mcg/cm2 viable epidermis and dermis: 35.67 ± 7.50 mcg/cm2 Receptor fluid: 3.78 ± 1.00 mcg/cm2 Residual sample (skin surface): 2785.30 ± 139.75 mcg/cm2 Formulation 3 - olive oil 24 hr Stratum corneum: 77.47 ± 12.33 mcg/cm2 viable epidermis and dermis: 19.79 ± 4.67 mcg/cm2 Receptor fluid: 0.80 ± 1.03 mcg/cm2 Residual sample (skin surface): 2579.72 ± 55.07 mcg/cm2 Formulation 4 - liquid paraffin 24 hr Stratum corneum: 64.82 ± 9.770 mcg/cm2 viable epidermis and dermis: 15.34 ± 5.37 mcg/cm2 Receptor fluid: 0.64 ± 0.77 mcg/cm2 Residual sample (skin surface): 2546.36 ± 104.93 mcg/cm2 | 82 |

Abbreviations: CTD = Cannabidiol loaded transdermal nanocarriers; CBD = Cannabidiol.

Table S4. Comparison of CBD pharmacokinetics of PCTD-12 and other studies.

| Method | Performance | Ref |
| --- | --- | --- |
| Self-assembled Nanoparticle | PK- PCTD-12 C max: 189.16 ± 4.46 ng/ml T max: 4 hr AUC 0-8 hr : 1338.8 ± 69.22 ng/ml∙hr AUC 0-24 hr : 3522.81 ± 191.25 ng/ml∙hr |  |
| Zein and Whey Protein Co-solvent with anti-solvent precipitation | PK- Oral 12mg C max: 0.47 mcg/ml = 470 ng/ml T max: 2 hr AUC 0-12 hr : 2.42 mcg/ml∙hr = 2420 ng/ml∙hr AUC 0-limit hr : 2.91 mcg/ml∙hr = 2910 ng/ml∙hr | 50 |
| transdermal delivery formulation | PK- AEM.CBD006 (78.69 mg/kg) C max: 427.149 ng/ml T max: 2 hr AUC 0-8 hr : 1758 ng/ml∙hr PK- AEM.CBD007 (76.61 mg/kg) C max: 360.351 ng/ml T max: 2 hr AUC 0-8 hr : 1563 ng/ml∙hr PK- AEM.CBD010 (155.24 mg/kg) C max: 602.168 ng/ml T max: 4 hr AUC 0-8 hr : 3067 ng/ml∙hr PK- AEM.CBD011 (75.76 mg/kg) C max: 331.560 ng/ml T max: 1 hr AUC 0-8 hr : 1410 ng/ml∙hr | US10842758B190 US11026896B291 US20230038462A192 |

Abbreviations: AUC0-t hr = area under the curve-time curve from 0 to the time point; CBD = Cannabidiol; PCTD = patch of cannabidiol loaded transdermal nanocarriers.

Figure S1 Appearance of TD series (A)precipitate, (B)turbidity, (C)Milky.

Figure S2 the properties of the prototype CTD-NCs AMPS gel. The appearance of (A) AMPS-gel (B) CTD-NCs-AMPS gel. The contact angle and water contain of (C) AMPS-series gel (D) CTD-NCs-AMPS gel. The black arrow indicates the gel boundary position, which used to cut to confirm whether curing is complete. Red arrow indicates incomplete curing part of the gel.