Supplementary information

Ion doped hollow silica nanoparticles as promising oligonucleotide delivery systems to mesenchymal stem cells

Chloe Trayford1, Dina M. Ibrahim1 and Sabine van Rijt1*

1MERLN Institute for Technology-Inspired Regenerative Medicine, Maastricht University, P.O. Box 616, 6200 MD Maastricht, the Netherlands

Figure S1. TEM images of HSN doped with Mg and Mn (a) without and (b) with DNA-FAM encapsulation. Scale bars are 200 nm.

Figure S2. Rhodamine b isothiocyanate (RITC) and Fluorescein deoxyribose nucleic acid (DNA-FAM) standard curves for the determination of DNA-FAM and RITC concentration in HSN.

Figure S3. EDX spectra characterizing ion doping in HSN where (a) Ca-HSN (b) Ca-HSND (c) Cu-HSN (d) Cu-HSND (e) Zn-HSN (f) Zn-HSND (g) Se-HSN (h) Se-HSND (i) Sr-HSN and (j) Sr-HSND

Figure S4. Size comparison of HSN and HSN with encapsulated DNA. Statistical significance is determined comparing HSN and DNA encapsulated HSN pairs where **** = p<0.0001, *** = p<0.001, ** = p<0.01 and * = p<0.05.

Figure S5. Surface potential comparison of HSN and HSN with encapsulated DNA. Statistical significance is determined comparing HSN and DNA encapsulated HSN pairs where **** = p<0.0001 and ** = p<0.01.

Figure S6. Quantification of DNA-FAM in HSN where (a) Number of molecules of DNA-FAM in 1mg of HSN and (b) Encapsulation efficiency of DNA-FAM in HSN.

Figure S7. Comparison of the RITC concentration in HSN and HSN with encapsulated DNA. Statistical significance is determined comparing HSN and DNA encapsulated HSN pairs where **** = p<0.0001.

Figure S8. Comparison of the ion doping efficiency in HSN and HSN with encapsulated DNA. Statistical significance is determined comparing HSN and DNA encapsulated HSN pairs where **** = p<0.0001.

Figure S9. Absorbance spectra showing shifting absorbance maxima of (a) ssDNA-FAM, (b) ssDNA-FAM in Cu2+ solution and (c) ssDNA-FAM released from Cu-HSND.

Figure S10. TEM images showing morphology of DNA encapsulated HSN[1, 2] after 7 d in 0mM GSH (-GSH) and 3mM GSH (+GSH) at 1mg/mL. Scale bars are 200 nm.

Figure S11. TEM images showing morphology of DNA encapsulated HSN after 7 d in 0mM GSH (-GSH) and 3mM GSH (+GSH) at 1mg/mL. Scale bars are 50 nm.

Figure S12. Flow cytometry uptake histograms after 24 hr incubation with 100µg/mL HSN where (a) HSN and (b) HSND

5. References

[1]	J. Saha et al., "Investigation of Fluorescence Resonance Energy Transfer between Fluorescein and Rhodamine 6G," Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, vol. 149, pp. 143-149, 2015/10/05/ 2015, doi: https://doi.org/10.1016/j.saa.2015.04.027.

[2]	M. Zhu, X. Wang, D. Liu, Z. Yin, F. Li, and J. Zhao, "Fluorescence enhancement of rhodamine B and fluorescein immobilized on optimized ZrO2 nano-porous films," Journal of Physics and Chemistry of Solids, vol. 157, p. 110198, 2021/10/01/ 2021, doi: https://doi.org/10.1016/j.jpcs.2021.110198.