Table S1. List of Abbreviations

| ABBREVIATIONS | DETAILS |
| --- | --- |
| Ag-NPs | Silver Nanoparticles |
| AMR | Anti-Microbial Resistance |
| °C | Degree Centigrade |
| EDXA | Energy-Dispersive X-Ray Spectroscopy Analysis |
| FTIR | Fourier-Transform Infrared Spectroscopy |
| H | Hours |
| HCl | Hydrochloric acid |
| MDR | Multidrug Resistance |
| Mg | Milligram |
| MICs | Minimum Inhibitory Concentration |
| mL | Milliliter |
| mM | Milli-Mole |
| PBS | Phosphate Buffer Saline |
| OD | Optical Density |
| Rpm | Revolution Per Minutes |
| SDS | Sodium Dodecyl Sulfate |
| SEM | Scanning Electron Microscopy |
| µL | Microliter |
| UV–visible spectrophotometry | Visible Ultra Violet Spectroscopy |
| v/v | Volume By Volume |
| w/v | Weight By Volume |
| XRD | X-Ray Diffraction |
| ZOAE | Aqueous Extract of Z. officinale |
| ZOEE | Organic Or Ethanol Extract of Z. officinale |
| ZO-Ag-NPs | Biosynthesized Silver Nanoparticles Using Extract of Z. offocinale |
| ZOAE-Ag-NPs | Synthesized Silver Nanoparticles Using Aqueous Extract of Z. officinale |
| ZOEE-Ag-NPs | Synthesized Silver Nanoparticles Using Organic Or Ethanol Extract of Z. officinale |
| + | Positive |
| - | Negative |

Table S2. EDX Result shows the percentage of element in ZOAE-AgNPs

| Element | Line Type | Apparent Concentration | k Ratio | Wt% | Wt% Sigma |
| --- | --- | --- | --- | --- | --- |
| C | K series | 1.86 | 0.01864 | 4.94 | 0.57 |
| O | K series | 0.93 | 0.00313 | 4.08 | 1.2 |
| Ag | L series | 42.57 | 0.4257 | 90.97 | 1.27 |
| Total: |  |  |  | 100 |  |

Table S3. EDX Result shows the percentage of element in ZOEE-AgNPs.

| Element | Line Type | Apparent Concentration | k Ratio | Wt% | Wt% Sigma |
| --- | --- | --- | --- | --- | --- |
| C | K series | 8.92 | 0.08919 | 21.42 | 0.69 |
| O | K series | 0.29 | 0.00098 | 1.23 | 1.24 |
| Ag | L series | 36.16 | 0.36162 | 77.34 | 1.16 |
| Total |  |  |  | 100 |  |

Figure S1: Schematic illustration of biosynthesized AgNPs capped by photoconstituents carboxyl, hydroxyl, and silver interactions.

Figure S2 (A) The chromatogram of the standard phenolic compounds. (B) The chromatogram of the standard flavonoid compounds

Key: AuU= absorbance unit, mAU- mili absorbance unit

Figure S3 The chromatogram of the phenolic and flavonoid compounds from Z. officinale (organic extract) detection at 280 nm and 360 nm respectively

Figure S4 Mechanism of the silver ions reduction to metallic AgNPs via quercitin as reducing agent in Z. officinale rhizome extract solution.

Figure S5 Structure of phenolic constituents