Supplementary Tables

Supplementary Table 1. Repeated measure ANOVA comparison between surface microhardness, elemental analysis (calcium, phosphorus and fluoride weight percentage) at baseline, after demineralization, and after remineralization at all three time points for both EMD-agarose and n-HA-EMD-agarose hydrogels.

| Assessment method | Material | Duration (days) | Difference of Levels (timematerial) | F-Value | Adjusted p-value |
| --- | --- | --- | --- | --- | --- |
| Microhardness | EMD-agarose | 2 | Baseline | 4.23 | 0.004* |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 4 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 6 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  | n-HA-EMD-agarose | 2 | Baseline | 3.15 | 0.019* |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 4 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 6 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  |  | After remineralization |  |  |
| Calcium weight percentage | EMD-agarose | 2 | Baseline | 1.98 | 0.106 |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 4 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 6 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  | n-HA-EMD-agarose | 2 | Baseline | 21.70 | 0.000* |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 4 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 6 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
| Phosphorous weight percentage | EMD-agarose | 2 | Baseline | 11.89 | 0.000* |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 4 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 6 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  | n-HA-EMD-agarose | 2 | Baseline | 27.93 | 0.000* |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 4 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 6 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
| Fluoride weight percentage | EMD-agarose | 2 | Baseline | 60.65 | 0.000* |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 4 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 6 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  | n-HA-EMD-agarose | 2 | Baseline | 121.22 | 0.000* |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 4 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |
|  |  | 6 | Baseline |  |  |
|  |  |  | After demineralization |  |  |
|  |  |  | After remineralization |  |  |

Significance level p<0.05 repeated measures of two-way analysis of variance; *statistically significant; EMD, enamel matrix derivative; n-HA, nano-hydroxyapatite.

Supplementary Table 2. Descriptive statistics and comparison of calcium weight percentage between groups at baseline, after demineralization, and after remineralization.

| Assessment groups | Material | Duration (days) | Mean±(SD) | Std. Error | Min | Max |  | Two-way ANOVA |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Time | Material | Materialtime |
| At baseline | EMD-agarose | 2 | 42.817±(2.267) | 0.756 | 39.89 | 47.11 | p-value | 0.649 | 0.773 | 0.793 |
|  |  | 4 | 42.157±(1.35) | 0.450 | 40.27 | 43.78 |  |  |  |  |
|  |  | 6 | 43.257±(2.214) | 0.738 | 39.58 | 46.02 |  |  |  |  |
|  | n-HA-EMD-agarose | 2 | 43.002±(2.183) | 0.728 | 39.54 | 46.73 |  |  |  |  |
|  |  | 4 | 42.780±(1.981) | 0.660 | 40.50 | 46.98 |  |  |  |  |
|  |  | 6 | 42.938±(2.283) | 0.761 | 38.99 | 46.07 |  |  |  |  |
| After demineralization | EMD-agarose | 2 | 36.790±(1.371) | 0.457 | 34.57 | 38.28 | p-value | 0.079 | 0.940 | 0.720 |
|  |  | 4 | 37.233±(2.078) | 0.693 | 34.31 | 39.7 |  |  |  |  |
|  |  | 6 | 37.824±(1.121) | 0.374 | 35.99 | 39.74 |  |  |  |  |
|  | n-HA-EMD-agarose | 2 | 36.381±(2.0) | 0.667 | 33.45 | 39.12 |  |  |  |  |
|  |  | 4 | 37.667±(1.178) | 0.393 | 35.95 | 39.34 |  |  |  |  |
|  |  | 6 | 37.702±(1.46) | 0.489 | 34.99 | 39.78 |  |  |  |  |
| After remineralization | EMD-agarose | 2 | 36.637±(2.242)B | 0.747 | 33.45 | 39.34 | p-value | 0.000* | 0.000* | 0.000* |
|  |  | 4 | 38.933±(1.838)B | 0.613 | 36.89 | 42.36 |  |  |  |  |
|  |  | 6 | 39.713±(0.958)B | 0.319 | 38.51 | 41.08 |  |  |  |  |
|  | n-HA-EMD-agarose | 2 | 37.09±(1.79)B | 0.598 | 33.85 | 38.86 |  |  |  |  |
|  |  | 4 | 44.88±(3.55)A | 1.18 | 40.12 | 49.32 |  |  |  |  |
|  |  | 6 | 46.31±(2.78)A | 0.929 | 42.03 | 49.58 |  |  |  |  |

*Statistically significant (significance level p < 0.05), Materialtime; interaction between material and time, means with different superscript letters (B, A) indicate a significant difference in multiple comparison tests (Tukey's post-hoc test), EMD; enamel matrix derivative, n-HA; nano-hydroxyapatite, SD; standard deviation.

Supplementary Table 3. Descriptive statistics and comparison of phosphorous weight percentage between groups at baseline, after demineralization, and after remineralization.

| Assessment groups | Material | Duration (days) | Mean±(SD) | Min | Max |  | Two-way ANOVA |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | Time | Material | Materialtime |
| At baseline | EMD-agarose | 2 | 20.18±(0.634) | 19.070 | 21.060 | p value | 0.824 | 0.862 | 0.423 |
|  |  | 4 | 20.24±(0.974) | 18.570 | 21.850 |  |  |  |  |
|  |  | 6 | 20.63±(0.808) | 19.270 | 21.620 |  |  |  |  |
|  | n-HA-EMD-agarose | 2 | 20.41±(0.79) | 19.090 | 21.860 |  |  |  |  |
|  |  | 4 | 20.48±(0.76) | 19.470 | 21.670 |  |  |  |  |
|  |  | 6 | 20.27±(0.65) | 19.380 | 21.590 |  |  |  |  |
| After demineralization | EMD-agarose | 2 | 17.17±(1.09) | 15.63 | 18.68 | p value | 0.351 | 0.073 | 0.162 |
|  |  | 4 | 17.12±(1.042) | 15.04 | 18.26 |  |  |  |  |
|  |  | 6 | 18.23±(0.934) | 16.77 | 19.64 |  |  |  |  |
|  | n-HA-EMD-agarose | 2 | 18.06±(1.513) | 15.78 | 19.81 |  |  |  |  |
|  |  | 4 | 18.16±(1.096) | 16.28 | 19.78 |  |  |  |  |
|  |  | 6 | 17.96±(0.83) | 16.67 | 19.44 |  |  |  |  |
| After remineralization | EMD-agarose | 2 | 15.1±(1.673)D | 13.260 | 18.620 | p value | 0.000* | 0.000* | 0.028* |
|  |  | 4 | 18.45±(0.923)C | 17.050 | 19.890 |  |  |  |  |
|  |  | 6 | 19.64±(1.092)C | 17.940 | 21.910 |  |  |  |  |
|  | n-HA-EMD-agarose | 2 | 17.78±(0.961)C | 16.390 | 19.060 |  |  |  |  |
|  |  | 4 | 22.29±(2.352)B | 19.090 | 25.790 |  |  |  |  |
|  |  | 6 | 24.92±(0.826)A | 23.820 | 26.180 |  |  |  |  |

*Statistically significant (significance level p < 0.05), Materialtime; interaction between material and time, means with different superscript letters (D, C, B, A) indicate a significant difference in multiple comparison tests (Tukey's post-hoc test), EMD; enamel matrix derivative, n-HA; nano-hydroxyapatite, SD; standard deviation.

Supplementary Table 4. Descriptive statistics and comparison of fluoride weight percentage between groups at baseline, after demineralization, and after remineralization.

| Assessment method | Material | Duration (days) | Mean ± (SD) | Min | Max |  | Two-way ANOVA |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | Time | Material | Materialtime |
| At baseline | EMD-agarose | 2 | 0.253±(0.088) | 0.12 | 0.35 | p value | 0.800 | 0.663 | 0.897 |
|  |  | 4 | 0.230±(0.0709) | 0.13 | 0.33 |  |  |  |  |
|  |  | 6 | 0.233±(0.0814) | 0.11 | 0.35 |  |  |  |  |
|  | n-HA-EMD-agarose | 2 | 0.25±(0.0504) | 0.17 | 0.31 |  |  |  |  |
|  |  | 4 | 0.25±(0.0656) | 0.17 | 0.36 |  |  |  |  |
|  |  | 6 | 0.24±(0.0658) | 0.15 | 0.35 |  |  |  |  |
| After demineralization | EMD-agarose | 2 | 0.194±(0.0534) | 0.13 | 0.28 | p value | 0.682 | 0.567 | 0.895 |
|  |  | 4 | 0.19±(0.0495) | 0.13 | 0.26 |  |  |  |  |
|  |  | 6 | 0.188±(0.0574) | 0.11 | 0.28 |  |  |  |  |
|  | n-HA-EMD-agarose | 2 | 0.21±(0.0535) | 0.14 | 0.29 |  |  |  |  |
|  |  | 4 | 0.19±(0.0428) | 0.14 | 0.26 |  |  |  |  |
|  |  | 6 | 0.19±(0.0381) | 0.13 | 0.24 |  |  |  |  |
| After remineralization | EMD-agarose | 2 | 0.1433±(0.0543)F | 0.07 | 0.23 | p value | 0.000* | 0.000* | 0.002* |
|  |  | 4 | 0.4422±(0.0429)D | 0.37 | 0.49 |  |  |  |  |
|  |  | 6 | 0.7033±(0.0624)B | 0.61 | 0.83 |  |  |  |  |
|  | n-HA-EMD-agarose | 2 | 0.254±(0.033)E | 0.21 | 0.32 |  |  |  |  |
|  |  | 4 | 0.518±(0.064)C | 0.43 | 0.59 |  |  |  |  |
|  |  | 6 | 0.909±(0.053)A | 0.83 | 0.99 |  |  |  |  |

*Statistically significant (significance level p < 0.05), Materialtime; interaction between material and time, means with different superscript letters (F, D, B, E, C, A) indicate a significant difference in multiple comparison tests (Tukey's post-hoc test), EMD; enamel matrix derivative, n-HA; nano-hydroxyapatite, SD; standard deviation.