### Supplementary materials

### Stability of Nanocomposites

The stability of nanocomposites were assessed by measurements of zeta potential by electrophoretic light scattering (ELS) over time 0, 8, 12, 24 and 48h using a Zeta Sizer Nano-ZS90 analyzer (Malvern Instruments, Malvern, UK) quadruplicate, at room temperature.

Figure S1 Zeta potentials of nanocomposites in time. All measurements were performed four times. Zp is the mean value of each sample’s zeta potential.

### Chemical analysis of nanocomposites formed

Chemical analysis of nanocomposites was performed using a Quanta 250 FEG FEI scanning electron microscope with an energy dispersive X-ray (SEM-EDX) detector. Nanocomposites were centrifuged (12 000 rpm, 10 mins) and the supernatant was separated from the pellets. The pellets were suspended in ultrapure water. Then, the droplets (0.05-0.1 μL) of hydrocolloids were placed 10x on the Silicon Wafer (Siegert Wafer, Wafer Specialist) and dried successively in a vacuum-dried Vacucell 55 (MMM Group) at 30°C. The following parameters were used: spot 4.5, 20 kV.

Table S1 EDX analysis of created nanocomposites: GOAg, GOCu, GOZnO.

| GOAg |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| supernatnat |  |  | pellet |  |  |
| Element | Weight % | Atomic % | Element | Weight % | Atomic % |
| C K | 20.97 | 38.12 | C K | 8.62 | 16 |
| O K | 0.93 | 1.27 | O K | 43.8 | 61.05 |
| SiK | 77.89 | 60.56 | SiK | 22.33 | 17.73 |
| AgL | 0.21 | 0.04 | AgL | 25.26 | 5.22 |

| GOCu |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| supernatnat |  |  | pellet |  |  |
| Element | Weight % | Atomic % | Element | Weight % | Atomic % |
| C K | 22.01 | 39.23 | C K | 12.77 | 21.15 |
| O K | 2.73 | 3.65 | O K | 38.02 | 47.29 |
| SiK | 74.68 | 56.92 | SiK | 40.86 | 28.95 |
| CuK | 0.58 | 0.19 | CuK | 8.35 | 2.62 |

| GOZnO |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| supernatnat |  |  | pellet |  |  |
| Element | Weight % | Atomic % | Element | Weight % | Atomic % |
| C K | 16.43 | 31.48 | C K | 22.34 | 40.26 |
| O K | 0.83 | 1.19 | O K | 31.53 | 42.65 |
| SiK | 81.75 | 66.98 | SiK | 4.16 | 3.2 |
| ZnK | 0.99 | 0.35 | ZnK | 41.97 | 13.89 |

### Bacterial biofilm formation

Section completely described in the main manuscript.

Figure S2 Z-stack images (confocal microscopy visualization) of biofilm structure of S. aureus, S. enterica, and P. aeruginosa created on the surface of nanofilms.